# Submission ID #: 69215

# Scriptwriter Name: Pallavi Sharma

# Project Page Link: https://review.jove.com/files_upload.php?src=21110623

Title: Fabrication and Optimization of Type II Silicon Clathrate Films

# Authors and Affiliations:

Malad-Chadi Ettobi¹,², Charif Tamin³, Anil Kumar Bharwal¹, Stéphane Roques¹, Céline Chevalier³, Abdelilah Slaoui¹, Aziz Dinia², Alain Fave³, Erwann Fourmond³, Daniel Stoeffler², Thomas Fix¹*

¹ICube Laboratory, University of Strasbourg, CNRS (Centre National de la Recherche Scientifique)

²IPCMS Laboratory (Institut de Physique et Chimie des Matériaux de Strasbourg), University of Strasbourg, CNRS

³Institut des Nanotechnologies de Lyon (INL), UMR 5270, École Centrale de Lyon, Institut National des Sciences Appliquées (INSA) Lyon, Université Claude Bernard Lyon 1

# Corresponding Authors:

Thomas Fix			(thomas.fix@unistra.fr)

# Email Addresses for All Authors:

Thomas Fix			(thomas.fix@unistra.fr)

Malad-Chadi Ettobi		(malad-chadi.ettobi@etu.unistra.fr)

Charif Tamin			(charif.tamin@insa-lyon.fr)

Anil Kumar Bharwal		(anilbharwal@gmail.com)

Stéphane Roques		(stephane.roques@unistra.fr)

Céline Chevalier		(celine.chevalier@insa-lyon.fr)

Abdelilah Slaoui		(abdelilah.slaoui@unistra.fr)

Aziz Dinia			(aziz.dinia@ipcms.unistra.fr)

Alain Fave			(alain.fave@insa-lyon.fr)

Erwann Fourmond		(erwann.fourmond@insa-lyon.fr)

Daniel Stoeffler		(daniel.stoeffler@ipcms.unistra.fr)

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

2. Interview statements: Which interview statement filming option is the most appropriate for your group? Please select one.

☒ 	Interviewees self-record interview statements. JoVE can provide support for this option.

3. Proposed interview filming date: Please indicate the proposed date that your group will self-film interviews: MM/DD/YYYY

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps:  16

Number of Shots:  24

# Introduction

INTRODUCTION:

What is the scope of your research? What questions are you trying to answer?

  - Malad-Chadi Ettobi: We present a protocol for synthesizing type II silicon clathrate films that involves two thermal annealing steps and does not require a glove box. This approach is straightforward and cost-effective.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.  Suggested B roll: 2.7

What are the current experimental challenges?

  - Thomas Fix: Currently, a few laboratories produce silicon clathrate films. Our goal is to share this simple two-furnace fabrication method with the scientific community, emphasizing adherence to all specified experimental safety measures.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

CONCLUSION:

What significant findings have you established in your field?

  - Malad-Chadi Ettobi:  We successfully fabricated type II SiCL films and improved their properties through two post-synthesis treatments: thermal pressing and reactive ion etching process.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 3.2

What research gap are you addressing with your protocol?

  - Malad-Chadi Ettobi:  We employed multiple characterization techniques, including XRD, photoluminescence, and Raman spectroscopy, to confirm the successful formation of the clathrate semiconducting phase.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: Figure 3

How will your findings advance research in your field?

  - Malad-Chadi Ettobi: We believe that this work is a stepping stone for further applications of silicon clathrates into semiconductor technology.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

# Protocol

- Preparation and Synthesis of SiCL

Demonstrator: Stéphane Roques

  - Begin by immersing the silicon substrate in a 10 percent hydrofluoric acid solution for exactly 2 minutes to remove the native silicon dioxide present on the substrate surface [1-TXT].

    - LAB MEDIA: Scene 5 (Experiment).MOV:  01:38 – 01:46, 03:44 – 03:54 TXT: Use 48 % HF acid for preparing the working solution

  - After exposure to hydrofluoric acid, rinse the silicon substrate thoroughly with deionized water to remove any residual acid [1]. Using a nitrogen gun, blow-dry the substrate to eliminate remaining water droplets and prevent surface residue [2].

    - LAB MEDIA:  Scene 5 (Experiment).MOV: 03:56 – 04:04

    - LAB MEDIA: Scene 5 (Experiment).MOV: 05:07-05:17

  - Using a cutter, carefully cut a piece of metallic sodium to obtain a small rectangular slice weighing approximately 0.22 grams [1].

    - LAB MEDIA: Scene 4 (Experiment).MOV: 01:00-01:10

  - Immediately place the sodium slice in an airtight glass container filled with anhydrous cyclohexane. Ensure that the sodium is fully immersed in the cyclohexane to prevent oxidation [1].

    - LAB MEDIA: Scene 4 (Experiment).MOV: 01:13-01:22.

  - Now, place the previously prepared sodium slice into a cleaned Inconel alloy boat [1]. Then, position the silicon wafer directly above the sodium slice with its polished surface facing downward toward the boat [2].

    - LAB MEDIA: Scene 8 (Experiment).MOV: 00:57-01:01. 01:12-01:17

    - LAB MEDIA: Scene 8 (Experiment).MOV: 01:33-01:43

  - Carefully insert the prepared assembly into the center of a sealed stainless-steel tube and an O-ring seal, situated inside a programmable horizontal tube furnace [1].

    - LAB MEDIA: Scene 8 (Experiment).MOV: 01:51-02:03

  - Insert a high-purity tantalum wire with a diameter of 0.5 millimeters, a length of 3.4 centimeters, and 99.95 percent purity into the tube to capture trace oxygen [1]. Seal both ends of the stainless-steel tube using fittings that allow circulation of only argon [2].

    - LAB MEDIA: Scene 8(Experiment).MOV: 00:30-00:48

    - LAB MEDIA: Scene 8(Experiment).MOV: 02:57-03:01, 03:20-03:30

  - Purge the sealed tube with argon at a constant pressure of 1.6 bar for 15 minutes to establish an inert atmosphere throughout the reaction [1].

    - LAB MEDIA: Scene  9 (Experiment).MOV

  - Then, raise the temperature of the furnace at a ramp rate of 5 degrees Celsius per minute until it reaches 600 degrees Celsius and maintain it for 19 hours [1-TXT].

    - LAB MEDIA: Scene  13 (Experiment).MOV: 00:00-00:16 TXT: Allow the system to cool for 7 h

  - When the furnace and tube have cooled back to room temperature, flush the system with a continuous flow of argon [1]. Transfer the obtained samples as quickly as possible into a quartz tube and connect the tube to a dynamic vacuum furnace [2].

    - LAB MEDIA: Scene  9 (Experiment).MOV: 00:00 – 00:09

    - LAB MEDIA: Scene 15 (Experiment).MOV: 00:42-00:54

  - After connecting the quartz tube to the pumping system, first evacuate the system using the primary pump. Then, activate the turbomolecular pump and continue pumping until a high vacuum of 5 × 10⁻⁷ millibar is achieved [1].

    - LAB MEDIA: Scene 16 (Experiment).MOV: 00:33-01:03

  - Ramp the furnace temperature to 400 degrees Celsius over 30 minutes and hold for 4 hours [1]. Then, switch off the tubular furnace and allow the sample to cool naturally to room temperature. After cooling, unload the sample from the furnace [2].

    - LAB MEDIA: Scene 17 (Experiment).MOV

    - LAB MEDIA: Scene 19 (Experiment).MOV: 00:45-00:52, 01:25-01:31

- Post-treatment of the Prepared SiCL

  - Lift the lower plate to gradually increase the force until the applied pressure reaches approximately 2 kilonewtons [1]. Then, release the applied pressure [2].

    - LAB MEDIA: Scene 22 (Experiment).mp4: 00:00 – 00:05

    - LAB MEDIA: Scene 24 (Experiment).mp4: 00:02 – 00:05

  - Place the cleaned sample onto the lower electrode inside the reactive ion etching system [1]. Pump down the chamber until a base pressure of 5 × 10⁻⁷ millibar is reached [2].

    - LAB MEDIA: Scene 25 (Experiment).MOV: 00:00 – 00:22

    - LAB MEDIA: Scene 25 (Experiment).MOV: 00:27 – 00:37

  - Once the etching process is complete, turn off both the inductively coupled plasma and radiofrequency power supplies to stop the plasma [1]. Evacuate any remaining process gases from the chamber. Then, slowly vent the chamber back to atmospheric pressure [2].

    - LAB MEDIA: Scene 27 (Experiment).MOV: 00:24 – 00:31

    - LAB MEDIA: Scene 27 (Experiment).MOV:  02:47 – 02:58

  - Finally, remove the etched sample from the chamber [1].

    - LAB MEDIA: Scene 27 (Experiment).MOV: 03:35-03:47

# Results

- Results

  - The X-ray diffraction pattern confirmed the formation of the type II Silicon clathrate phase in both the pressed and pressed-etched samples, with sharp peaks matching the ICDD 01-089-5534  (I-C-D-D-zero-One-Zero-Eight-Nine-Five-Five-Three-Four) [1], and weak reflections indicating the presence of a minor type 1 silicon clathrate secondary phase [2]. After etching, the peak positions remained unchanged but showed a slight reduction in intensity [3].

    - LAB MEDIA: Figure 3. Video editor: Highlight the peaks in both the “Pressed sample” and “Pressed-etched sample” .

    - LAB MEDIA: Figure 3. Video editor: Highlight the small peaks in both patterns that align with the blue Na8Si46 markers.

    - LAB MEDIA: Figure 3. Video editor: Compare the peak heights of the “Pressed-etched sample” to those of the “Pressed sample”

  - Raman spectroscopy revealed that both pressed and pressed-etched samples exhibited characteristic peaks near 185, 290, and 460 inverse centimeters, corresponding to the Si20 (S-I-Twenty) and Si28 (S-I-Twenty-Eight) cages in the type II clathrate structure [1].

    - LAB MEDIA: Figure 4. Video editor: Highlight the Raman peaks labeled Eg, T2g, and A1g in both sample curves.

  - Photoluminescence measurements showed a broad emission band centered around 1.75 electron volts in both pressed and pressed-etched samples, consistent with the quasi-direct band gap of semiconducting silicon clathrates [1].

    - LAB MEDIA: Figure 5.

  - SEM (S-E-M) top-view images of the pressed sample revealed a smoother surface with significantly reduced grain boundaries [1], while cross-sectional views showed improved film density and structural connectivity [2].

    - LAB MEDIA: Figure 6. Video editor: Highlight 6A.

    - LAB MEDIA: Figure 6. Video editor: Highlight 6B

  - After SF6 dry etching, SEM top-view images showed a transformation to a textured surface morphology [1], and cross-sectional images confirmed changes in surface structure compared to the unetched film [2].

    - LAB MEDIA: Figure 6. Video editor: Highlight 6C

    - LAB MEDIA: Figure 6. Video editor: Highlight 6D