# Submission ID #: 69270

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=21127398

# Title: Light-Induced Patterning and Grafting for Slippery Surfaces Based on Silane-Coated Nanoporous Structures

# Authors and Affiliations:

# Woo Young Kim*1, Seong Min Yoon*2, Seo Na Yoon2, Chae Hyeok Yoon2, Seo Rim Park2, Young Tae Cho2

# 1Global Institute for Advanced Nanoscience & Technology, Changwon National University

# 2Department of Smart Manufacturing Engineering, Changwon National University

# *These authors contributed equally

# Corresponding Authors:

Young Tae Cho	ytcho@changwon.ac.kr

# Email Addresses for All Authors:

Woo Young Kim	wooyoung0329@changwon.ac.kr

Seong Min Yoon	20247165@gs.cwnu.ac.kr

Seo Na Yoon		20215157@gs.cwnu.ac.kr

Chae Hyeok Yoon	20225153@gs.cwnu.ac.kr

Seo Rim Park		qkrtjflakr@changwon.ac.kr

Young Tae Cho	ytcho@changwon.ac.kr

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes

If Yes, we will need you to record using screen recording software.

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

As these files are necessary for finalizing your script, please upload all screen-captured video files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=21127398

3. Filming location: Will the filming need to take place in multiple locations?   No

4. Testimonials (optional): Would you be open to filming two short testimonial statements live during your JoVE shoot? These will not appear in your JoVE video but may be used in JoVE’s promotional materials. No

Current Protocol Length

Number of Steps: 13

Number of Shots: 31

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

INTRODUCTION:

What is the scope of your research? What questions are you trying to answer?

  - Seo Na Yoon: Our research introduces a DLP-based technique to fabricate spatially patterned SLIPS, addressing limitations in achieving selective wettability control.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

What are the current experimental challenges?

  - Seo Na Yoon: Key experimental challenges include fabricating SLIPS on complex geometries—existing methods are time-consuming, multi-step, and lack high resolution or selective wettability.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

CONCLUSION:

What significant findings have you established in your field?

  - Young Tae Cho: UV-grafted nanoporous surfaces shows slippery properties with minimal contact angle hysteresis and enable selective droplet patterning.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

What advantage does your protocol offer compared to other techniques?

  - Young Tae Cho: The DLP-based protocol enables rapid, single-step, high-resolution patterning on flexible substrates, significantly reducing fabrication time and complexity versus conventional multi-step methods.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

How will your findings advance research in your field?

  - Young Tae Cho: By enabling spatial control of surface wettability, our work supports progress in directional droplet transport, microfluidics, antifouling surfaces, and water-harvesting technologies.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

- Fabrication of Nanoporous and Patterned Slippery Surfaces using UV Curing and Surface Functionalization

Demonstrator: Seong Min Yoon

  - To begin, mix the photocurable polyurethane acrylate resin with PEG-200 (P-E-G-Two-Hundred) at a weight ratio of 50 percent [1]. Using a magnetic stirrer, stir the mixture at 500 revolutions per minute for 5 minutes [2].

    - WIDE: Talent mixing polyurethane acrylate resin with polyethylene glycol-200.

    - Talent placing the mixture on a magnetic stirrer set at 500 revolutions per minute.

  - Dispense the mixed solution as sessile droplets onto a polyethylene terephthalate film [1]. Cover the droplets with a fluorinated ethylene propylene film [2] and apply uniform pressure using a roll-to-plate system to ensure even spreading [3].

    - Talent dispensing the mixed resin onto the polyethylene terephthalate film.

    - Talent placing a fluorinated ethylene propylene film over the sessile droplets.

    - Talent using the roll-to-plate system to apply uniform pressure and spread the resin.

  - Expose the polyurethane acrylate resin to ultraviolet light at 365 nanometers using a light-emitting diode ultraviolet-curing system [1-TXT]. After polymerization, remove the fluorinated ethylene propylene films from the surface [2].

    - Talent initiating ultraviolet exposure of the sample using the ultraviolet-curing system. TXT: Energy dose: 180 mJ/cm²

    - Talent removing the fluorinated ethylene propylene films after polymerization.

  - Now, immerse the cured specimen in deionized water for 1 hour to extract unreacted PEG-200 [1]. Dry the sample in an oven at 70 degrees Celsius for 1 hour to remove residual water and complete fabrication of the nanoporous surface [2].

    - Talent placing the cured sample into a container filled with deionized water.

    - Talent transferring the sample into a 70-degree Celsius oven for drying.

  - Perform ultraviolet ozone treatment at 185 and 254 nanometers to introduce hydroxyl groups as pretreatment for self-assembled monolayer formation [1-TXT].

    - Talent setting up the ultraviolet ozone treatment with specified wavelength and intensity. TXT: UV intensity: 25 mW/cm², 20 min, RT under atmospheric pressure

    - Talent running the system at room temperature and atmospheric pressure.

  - Next, place a hot plate inside a nitrogen-filled glovebox [1]. Position a clean beaker on the hot plate [2] and dispense 1 milliliter of OTS (O-T-S) solution as a sessile droplet at the bottom [3-TXT].

    - Talent setting the hot plate in the nitrogen-filled glovebox.

    - Shot of a clean beaker being placed on the hot plate.

    - Talent dispensing 1 milliliter of OTS solution into a beaker as a sessile droplet. TXT: OTS: Octadecyltrichlorosilane

  - Secure the PET (pet) film specimens onto glass slides [1]. Place the slides face down over the beaker to initiate vapor-phase deposition of OTS [2]. Heat the setup to 120 degrees Celsius for 40 minutes [3].

    - Talent mounting polyethylene terephthalate film samples onto glass slides.

    - Talent inverting the slides and placing them over the beaker inside the glovebox.

    - Talent setting the system to heat to 120 degrees Celsius for 40 minutes.

  - Now remove the specimens from the glovebox [1]. Clean the beaker using a lint-free wipe to eliminate any residual OTS [2].

    - Talent retrieving the specimens from the nitrogen-filled glovebox.

    - Talent cleaning the beaker interior thoroughly using a lint-free wipe.

  - For light induced grafting, perform ultraviolet ozone treatment at 185 and 254 nanometers on the OTS-coated surface [1-TXT]. Now, apply 20 microliters per square centimeter of 10 centistokes silicone oil to the surface by sessile droplet deposition [2].

    - Talent placing the treated samples under ultraviolet ozone. TXT: UV intensity: 25 mW/cm², 20 min, RT under atmospheric pressure

    - Talent applying silicone oil to the surface using a micropipette.

  - Irradiate the specimen for 15 minutes with a high-intensity ultraviolet lamp placed 15 centimeters above the surface [1-TXT]. Then tilt the specimen at a 30-degree angle and hold the position for 5 minutes to allow excess silicone oil to drain off the surface [2].

    - Talent positioning the high-intensity ultraviolet lamp 15 centimeters above the sample. TXT: Perform multiwavelength exposure at 207, 214, 296, 317, and 321 nm, T: 103 °C

    - Talent tilting the sample to a 30-degree angle and maintaining the position for drainage.

  - To fabricate the patterned slippery structure, first design the desired shapes using CAD (Cad) software and export as stereolithography files [1]. Load the files into slicing software [2] and generate two-dimensional projection images for digital light processing [3]. Transfer the files to the three-dimensional printer [4].
Authors: Please create screen capture videos of the shots labeled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=21127398

    - SCREEN: A shape is being created in CAD software and exported as stereolithography format.

    - SCREEN: The stereolithography files are being loaded into slicing software.

    - SCREEN: Two-dimensional projections are being generated.

    - Talent transferring the files are to the 3D printer via USB.

  - Place the polymer-coated film onto the digital light processing printer window [1]. Expose the film to 365 nanometers ultraviolet light at 180 millijoules per square centimeter with the digital projection pattern to selectively cure the resin [2].

    - Talent mounting the polymer-coated film onto the printer platform.

    - Talent initiating ultraviolet projection using the digital pattern.

  - Submerge the exposed sample in deionized water for 1 hour to extract PEG-200 [1]. Then dry the sample at 70 degrees Celsius for 1 hour to remove residual water and complete the nanoporous structure [2]. Conduct OTS treatment and light induced grafting to complete the fabricated of the patterned slippery surfaces [3].

    - Talent placing the cured film into deionized water for soaking.

    - Talent drying the film in a 70 degree Celsius oven.

    - Shot of the final patterned sample.

# Results

- Results

  - The nanoporous surfaces fabricated via polymerization-induced phase separation exhibited a dominant pore size distribution of 60 to 100 nanometers [1].

    - LAB MEDIA: Figure 2. Video editor: Highlight the tallest three bars h between 60 and 100 on the x-axis labeled “Pore diameter [nm]” in 2 B

  - The static water contact angle measured on the porous surface was 84.4 degrees [1]. After silanization, the surface became hydrophobic [2], but a second ultraviolet-ozone treatment temporarily reduced the contact angle [3]. This reduction was reversed by PDMS brush layer formation, which restored hydrophobicity [4].

    - LAB MEDIA: Figure 3A. Video editor: Highlight the bar labeled “Step 1”

    - LAB MEDIA: Figure 3A. Video editor: Highlight the bar labeled “Step 3”

    - LAB MEDIA: Figure 3A. Video editor: Highlight the bar labeled “Step 4”

    - LAB MEDIA: Figure 3A. Video editor: Highlight the bar labeled “Step 6”

  - The slippery behavior of four representative liquids—deionized water, octane, honey, and artificial human saliva—was validated by contact angle [1], sliding angle [2], sliding speed [3], and contact angle hysteresis measurements [4].

    - LAB MEDIA: Figure 3 C-F	Video Editor: Please highlight C

    - LAB MEDIA: Figure 3 C-F	Video Editor: Please highlight D

    - LAB MEDIA: Figure 3 C-F	Video Editor: Please highlight E

    - LAB MEDIA: Figure 3 C-F	Video Editor: Please highlight F

  - Printed line width measurements from the PEG–PUA resin showed high fidelity at the minimum feature size of 50 micrometers, with increasing deviations at larger widths [1].

    - LAB MEDIA: Figure 4. Video editor: Highlight the dashed lines

  - Patterned nanoporous surfaces were fabricated with graphical and lettered designs using digital light processing, including maze, gear, and “JoVE” logos [1]. Following all surface treatments and silicone oil infusion, the patterns became optically transparent due to reduced refractive index contrast [2].

    - LAB MEDIA: Figure 5A. Video editor: Highlight the maze, gear, and “JoVE” shapes in the top row panels labeled (i), (ii), and (iii)

    - LAB MEDIA: Figure 5B.

  - Transmittance measurements showed that treated porous surfaces reached over 90% transparency [1].

    - LAB MEDIA: Figure 5C. Video editor: Highlight the blue curve labeled “Porous surface”

  - When water-containing ink was applied, droplets selectively migrated to untreated hydrophilic regions, avoiding the slippery domains [1], forming defined liquid shapes [2].

    - LAB MEDIA: Figure 5D. Video editor: Highlight the red circle areas

    - LAB MEDIA: Figure 5E.