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Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  NO

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  YES
If Yes, we will need you to record using screen recording software.
We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k
As these files are necessary for finalizing your script, please upload all screen-captured video files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=21151798

3. Filming location: Will the filming need to take place in multiple locations?   NO


4. Testimonials (optional): Would you be open to filming two short testimonial statements live during your JoVE shoot? These will not appear in your JoVE video but may be used in JoVE’s promotional materials. NO


Current Protocol Length
Number of Steps: 31
Number of Shots: 56

Introduction
Videographer: Obtain headshots for all authors available at the filming location. 

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.
1.1. Louise Serpell: Our research uses X-ray fiber diffraction to elucidate amyloid fibril cross-β structures and uncover their underlying molecular organization.
1.1.1. INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

Describe the research gap or limitation in existing methods and how this protocol addresses them.
1.2. Louise Serpell: Protocol uses X-ray fiber diffraction to confirm cross-β patterns and elucidate fibril architecture.
1.2.1. INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B roll: 3.2.1

CONCLUSION:

What does this protocol allow researchers to study or measure?
1.3. Louise Serpell: This protocol enables structural analysis of amyloid fibrils, from confirming cross-β architecture to developing detailed molecular models.
1.3.1. INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.


Describe the most important consideration or challenge when performing this protocol.
1.4. Louise Serpell: Proper sample alignment is critical, as it directly determines the quality and structural detail obtainable from X-ray fiber diffraction data.
1.4.1. INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B roll: 2.11.1.


How can future studies build on this work? Describe the questions or research directions that can be investigated next.
1.5. Louise Serpell: This work enables atomic-resolution amyloid modeling and integration with complementary methods, such as AFM, to resolve multiscale structural details.
1.5.1. INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.


Videographer: Obtain headshots for all authors available at the filming location.


Protocol  
SCREEN/SCOPE timestamps for protocol were added at the postshoot stage. Please contact the postshoot note integrator (Pallavi Sharma) for queries regarding lab media.

2. Alignment of Amyloid Fibrils for X-ray Fiber Diffraction Data Collection 
Demonstrator: Louise Serpell 

2.1. To begin, align the protein or peptide fibrils to produce a bundle whose fiber axes are ideally all parallel [1]. 
2.1.1. WIDE: Talent arranging materials on the bench to prepare for fibril alignment. 
2.2. Melt candle wax with a hot plate until it liquifies [1]. Using a glass cutter, cut 1 millimeter borosilicate glass capillaries to a length of about 2 to 3 centimeters [2]. 
2.2.1. Talent heating candle wax on a hot plate until liquid. 
2.2.2. Talent cutting borosilicate glass capillaries with a glass cutter. 
2.3. Dip the cut capillaries briefly into the liquid wax [1]. Then draw the candle wax up by capillary action to approximately 1 to 2 millimeters within the capillary [2]. 
2.3.1. Shot of capillary ends being dipped into liquid wax. 
2.3.2. Shot of wax being drawn into the capillary by capillary action. 
2.4. Now use plasticine to attach the sealed capillaries horizontally inside a Petri dish [1]. Maintain a gap of 0.5 to 2 millimeters between the wax-filled ends of the capillaries [2].
2.4.1. Talent attaching the sealed capillaries horizontally in a Petri dish with plasticine.  NOTE: Also still shown in uploaded IMAGE-x.png
2.4.2. Shot showing the measured gap between wax-filled capillary ends. 
2.5. With a pipette, carefully suspend a 10-microliter droplet of fibril solution between the wax-filled ends of the two capillaries [1]. Cover the Petri dish to protect the sample from dust and evaporate overnight [2]. 
2.5.1. Talent pipetting a 10 µL droplet between two capillaries. 
2.5.2. Talent placing a cover over the Petri dish. 
2.6. Then, seal the plate to control the drying environment [1]. 
2.6.1. Talent sealing the plate. 
2.7. To align the amyloid fibrils in a glass capillary, fix a 1-milliliter syringe with rubber tubing to the wide end of a 0.7-millimeter diameter siliconized glass capillary [1]. Aspirate 2 to 3 centimeters of fibril suspension into the capillary [2].
2.7.1. Talent assembling syringe, tubing, and glass capillary. 
2.7.2. Shot of fibril suspension being pipetted into the capillary.  NOTE: 2.7.1 and 2.7.2 are filmed as one shot
2.8. Seal one end of the capillary using melted wax and leave the other end open to allow evaporation [1]. Arrange the capillary vertically and allow it to dry until a dried disk is formed [2-TXT].  
2.8.1. Talent sealing one end of the capillary with wax. 
2.8.2. Shot of Capillary arranged vertically in a holder. NOTE:  2.8.1 and 2.8.2 as one shot
2.9. Place a high-concentration fibril sample onto a glass slide and cover before air-drying for 24 hours [1]. 
2.9.1. Talent dispensing fibril sample onto a flat surface.
2.10. With a scalpel, carefully lift the dried fibril film from the surface [1]. Attach the film to a glass capillary tube using glue or plasticine [2].
2.10.1. Talent lifting the film with a scalpel.
2.10.2. Shot of the film being attached to a glass capillary.   NOTE: Not filmed

2.11. Carefully mount the fibril mat on a goniometer head and orient it so that the X-ray beam passes through the edge of the mat and parallel to the plane of the film [1].
2.11.1. Talent mounting the sample on a goniometer head and orienting it. 

2.12. Examine the sample under a light microscope equipped with a cross-polariser to observe birefringence [1-TXT].
2.12.1. LAB MEDIA: IMAGE3.png


2.13. Next, attach the capillary fiber sample onto a goniometer head using plasticine [1]. Position the sample in the X-ray beam based on whether it is a fiber bundle, mat, or disk [2].
2.13.1. Talent attaching the capillary to the goniometer head.
2.13.2. LAB MEDIA: IMAGE4.png  
AND
TEXT ON PLAIN BACKGROUND:
Sample rotation axis will be around the fiber axis for a fiber bundle 

Fibers tend to align across the diameter of the tube in disks NOTE: Show Figure 2C also
 
A mat will have two distinct directions
Video Editor: Please play both shots side by side in a split screen 
2.14. Collect a diffraction pattern using in-house X-ray equipment or synchrotron radiation [1]. 
2.14.1. LAB MEDIA: IMAGE5.png
-STILL provided uploaded IMAGE-5

3. X-ray Amyloid Fiber Diffraction Data Processing and Unit Cell Determination Using CLEARER
3.1. To perform data analysis, upload the file into the CLEARER (clearer) diffraction pattern analysis software [2].
3.1.1. SCREEN: Serpell-SCREENSHOT.MOV: 00:03-00:12
3.2. Navigate to Diffraction Pattern and diffraction setting to input diffraction settings, including pixel size, X-ray source, and sample to detector distance [1]. 
3.2.1. SCREEN:Serpell-SCREENSHOT.MOV: 00:13-00:21
3.3. Click on Image Processing and Rotate to rotate the diffraction image so that the meridian is vertical [1]. Use the Centering module by navigating to Diffraction Pattern and clicking on Center Image to center the image [2]. 
3.3.1. SCREEN: Serpell-SCREENSHOT.MOV: 00:52-00:56
3.3.2. SCREEN: Serpell-SCREENSHOT.MOV: 01:04-01:08
3.4. Define the meridian and equator axes. Save the centered image for subsequent analysis [1].
3.4.1. SCREEN: Serpell-SCREENSHOT.MOV: 01:22-01:27
3.5. Now specify an appropriate angle along the meridian and equator [1]. Press Diffraction Pattern and click on Radially Average Module to generate a graph of diffraction signal position versus intensity [2].
3.5.1. SCREEN: Serpell-SCREENSHOT.MOV: 01:35-01:47
3.5.2. SCREEN: Serpell-SCREENSHOT.MOV: 02:13-02:16
3.6. Navigate to the Peak Find module from the Diffraction Pattern menu to measure and automatically output the diffraction signal [1]. Adjust the peak search width to detect true signals without noise [2].
3.6.1. SCREEN: Serpell-SCREENSHOT.MOV: 03:06-03:20
3.6.2. SCREEN: Serpell-SCREENSHOT.MOV: 03:33-03:45
3.7. Use the Zoom & Measure option to verify diffraction signal positions output using Peak Find [1-TXT]. 
3.7.1. SCREEN: Serpell-SCREENSHOT.MOV: 04:53-05:02 
3.8. Explore potential unit cell dimensions using the Unit Cell Optimization Module [1]. Input initial estimates based on strong equatorial signals and define the minimum and maximum indices for cell search [2].
3.8.1. SCREEN: Serpell-SCREENSHOT.MOV: 05:43-05:50
3.8.2. SCREEN: Serpell-SCREENSHOT.MOV: 07:12-07:17 
3.9. Calculate potential unit cell dimensions and compare the predicted diffraction signal positions with observed reflections. Select the unit cell that best fits the data and the sample [1].
3.9.1. SCREEN: Serpell-SCREENSHOT.MOV: 08:22-08:35


4. Structural Modeling and Validation of Amyloid Fibrils Using CLEARER Fiber Diffraction Simulation

4.1. To construct molecular models, build 3D arrangements of the peptides in a beta sheet configuration that fits the determined unit cell [1]. Ensure all symmetry-related components are included [2].
4.1.1. SCREEN: Serpell-SCREENSHOT.MOV: 11: 46-11:53
4.1.2. SCREEN: Serpell-SCREENSHOT.MOV: 13:06-13:06
4.2. Load the PDB (P-D-B) model into the Structure Chain Generator Module by clicking on Diffraction Simulation, Structures and Structure Chain Generator [1]. Assign the fiber axis and beam axis, input unit cell dimensions, and then check for steric clashes [2].
4.2.1. SCREEN: Serpell-SCREENSHOT.MOV: 13:46-13:53
4.2.2. SCREEN: Serpell-SCREENSHOT.MOV: 15:09-15:18
4.3. Navigate to Diffraction Simulation and press Fiber Diffraction Simulation to upload the PDB coordinates into the Fiber Diffraction Simulation Module [1]. Input the fiber axis direction, beam orientation, unit cell dimensions, X-ray source, and detector settings, then click Simulate to run the simulation [2].
4.3.1. SCREEN: Serpell-SCREENSHOT.MOV: 16:12-16:16 
4.3.2. SCREEN: Serpell-SCREENSHOT.MOV: 16-28-16:46
. 
4.4. Ensure the beam axis is perpendicular to the fiber axis [1]. Then navigate to File and click on Save As to save the simulation settings as .html (dot-H-T-M-L) files for later editing [2].
4.4.1. SCREEN: Serpell-SCREENSHOT.MOV: 15:09-15:11.
4.4.2. SCREEN: Serpell-SCREENSHOT.MOV: 18:49-18:56
4.5. Save the simulated diffraction pattern in raw format or as a .tiff file [1]. Compare the simulated pattern with the experimental diffraction pattern [2].
4.5.1. SCREEN: Serpell-SCREENSHOT.MOV: 18:59-19:02
4.5.2. SCREEN: Serpell-SCREENSHOT.MOV: 19:42-19:51
4.6. Measure simulated diffraction signals using the same analysis workflow. Record and compare these values with experimental data [2].
4.6.1. SCREEN: : Serpell-SCREENSHOT.MOV: 20:00-20:33
4.7. Use the Layers module from Diffraction Pattern to overlay simulated and experimental diffraction patterns and compare the alignment of signal positions [1]. Arrange pattern quadrants for visual comparison of signal positions and relative intensities [2].  NOTE: Not provided 
4.7.1. SCREEN: Activating the layers overlay function.
4.7.2. SCREEN: Displaying quadrant-based comparison of patterns.
4.8. Lastly, evaluate the validity of the proposed unit cell and structural model [1]. Iteratively modify the model and unit cell parameters to improve agreement with experimental data [2].
4.8.1. SCREEN: Assessing model agreement with diffraction data.
4.8.2. SCREEN: Iterative refinement of model and unit cell parameters.

4.8.3. 

Results
5. Results 

5.1. Electron micrographs showed a high density of amyloid fibrils on the grid suitable for preparation of an X-ray fiber sample [1].
5.1.1. LAB MEDIA: Figure 1. 
5.2. Stretch-frame aligned fibers produced a characteristic cross-beta diffraction pattern [1] with a meridional reflection at 4.76 angstroms and equatorial reflections arising from chain length, sheet spacing, and protofilament size [2]. An idealized cross-beta diffraction pattern demonstrated that meridional and equatorial reflections correspond to repetitive spacings along the fiber axes [3].
5.2.1. LAB MEDIA: Figure 3 	Video Editor: Please highlight A 
5.2.2. LAB MEDIA: Figure 3 	Video Editor: Please highlight B
5.2.3. LAB MEDIA: Figure 3. 	Video Editor: Please highlight C.
5.3. A well-centered diffraction pattern was symmetric, with equatorial and meridional peaks overlapping in position [1]. Diffraction peaks were automatically detected and listed using peak-finding analysis [2]. 
5.3.1. LAB MEDIA: Figure 4 	Video Editor: Please highlight A 
5.3.2. LAB MEDIA: Figure 4	Video Editor: Please highlight A (right side) and B

5.4. The detected diffraction peaks were used to identify plausible unit cell dimensions [1]. A structural model was prepared using the identified unit cell and visualized prior to diffraction simulation [2].
5.4.1. LAB MEDIA: Figure 5. Video Editor: Please highlight A
5.4.2. LAB MEDIA: Figure 5	Video Editor: Please highlight B
5.5. Simulated diffraction data generated from the proposed structural model showed reasonable agreement with the experimental diffraction pattern in both reflection positions and relative intensities [1]. Overlaying simulated and experimental diffraction patterns further demonstrated alignment of corresponding reflections [2].
5.5.1. LAB MEDIA: Figure 6	Video Editor: Please highlight A then B
5.5.2. LAB MEDIA: Figure 6C.

1. Fibrils
Pronunciation link: https://www.merriam-webster.com/dictionary/fibril
IPA: /ˈfaɪbrəl/
Phonetic Spelling: fy·bruhl
2. Borosilicate
Pronunciation link: https://www.howtopronounce.com/borosilicate
IPA: /ˌbɔːroʊˈsɪlɪkət/
Phonetic Spelling: bor·oh·sil·ih·kut
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Pronunciation link: https://www.merriam-webster.com/dictionary/capillary
IPA: /ˈkæpəˌleri/
Phonetic Spelling: kap·uh·lair·ee
4. Plasticine
Pronunciation link: https://www.merriam-webster.com/dictionary/plasticine
IPA: /ˈplæstəˌsiːn/
Phonetic Spelling: plas·tuh·seen
5. Microliter
Pronunciation link: https://www.merriam-webster.com/dictionary/microliter
IPA: /ˈmaɪkrəˌliːtər/
Phonetic Spelling: my·kruh·lee·tur
6. Amyloid
Pronunciation link: https://www.merriam-webster.com/dictionary/amyloid
IPA: /ˈæmɪˌlɔɪd/
Phonetic Spelling: am·ih·loyd
7. Siliconized
Pronunciation link: https://www.howtopronounce.com/siliconized
IPA: /ˈsɪlɪkəˌnaɪzd/
Phonetic Spelling: सिल·ih·kuh·nyzd
8. Scalpel
Pronunciation link: https://www.merriam-webster.com/dictionary/scalpel
IPA: /ˈskælpəl/
Phonetic Spelling: skal·puhl
9. Goniometer
Pronunciation link: https://www.merriam-webster.com/dictionary/goniometer
IPA: /ˌɡoʊniˈɑːmətər/
Phonetic Spelling: goh·nee·om·uh·tur
10. Cross-polariser
Pronunciation link: https://www.howtopronounce.com/cross-polariser
IPA: /krɔːs ˈpoʊləˌraɪzər/
Phonetic Spelling: kraws poh·luh·ry·zur
11. Birefringence
Pronunciation link: https://www.merriam-webster.com/dictionary/birefringence
IPA: /ˌbaɪrɪˈfrɪndʒəns/
Phonetic Spelling: by·rih·frin·juhns
12. Diffraction
Pronunciation link: https://www.merriam-webster.com/dictionary/diffraction
IPA: /dɪˈfrækʃən/
Phonetic Spelling: dih·frak·shuhn
13. Synchrotron
Pronunciation link: https://www.merriam-webster.com/dictionary/synchrotron
IPA: /ˈsɪŋkrəˌtrɑːn/
Phonetic Spelling: sing·kruh·tron
14. Meridian
Pronunciation link: https://www.merriam-webster.com/dictionary/meridian
IPA: /məˈrɪdiən/
Phonetic Spelling: muh·rid·ee·uhn
15. Equator
Pronunciation link: https://www.merriam-webster.com/dictionary/equator
IPA: /ɪˈkweɪtər/
Phonetic Spelling: ih·kway·tur
16. Radially
Pronunciation link: https://www.howtopronounce.com/radially
IPA: /ˈreɪdiəli/
Phonetic Spelling: ray·dee·uh·lee
17. Equatorial
Pronunciation link: https://www.merriam-webster.com/dictionary/equatorial
IPA: /ˌekwəˈtɔːriəl/
Phonetic Spelling: ek·wuh·tor·ee·uhl
18. Reflections
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IPA: /rɪˈflekʃən/
Phonetic Spelling: rih·flek·shuhn
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Pronunciation link: https://www.howtopronounce.com/steric
IPA: /ˈstɛrɪk/
Phonetic Spelling: ster·ik
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Pronunciation link: https://www.merriam-webster.com/dictionary/quadrant
IPA: /ˈkwɑːdrənt/
Phonetic Spelling: kwod·ruhnt
21. Micrographs
Pronunciation link: https://www.merriam-webster.com/dictionary/micrograph
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IPA: /məˌrɪdiˈoʊnəl/
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