# Submission ID #: 69716

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=21263428

# Title: Fabrication of Dissolvable Microneedle Patches Loaded with α-Lactalbumin Nanomicelles for Transdermal Capsaicin Delivery and Adipose Tissue Reduction

# Authors and Affiliations:

# Chunhui Rui1,2, Yuli Pan1,2, Jing Fu1,2, Luna Li1,2, Liangqi Jiangzhuo1, Jiantao Sun1, Cheng Bao1,2,3

# 1School of Life Sciences, Ludong University

# 2Collaborative Innovation Center for the Pet Infectious Diseases and Public Health in the Middle and Lower Stream Regions of the Yellow River

# 3Shandong Engineering Research Center for Aquaculture Environment Control

# Corresponding Authors:

Cheng Bao 		(bc3725@ldu.edu.cn)

# Email Addresses for All Authors:

Chunhui Rui 		(2517705428@qq.com)

Yuli Pan 		(1944394953@qq.com)

Jing Fu 		(1724403216@qq.com)

Luna Li 		(2660409171@qq.com)

Liangqi Jiangzhuo 	(2040688944@qq.com)

Jiantao Sun 		(2706859429@qq.com)

Cheng Bao 		(bc3725@ldu.edu.cn)

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: 01/20/2026

When you are ready to submit your video files, please contact our China Location Producer, Yuan Yue.

Current Protocol Length

Number of Steps:  11

Number of Shots:  26

# Introduction

INTRODUCTION:

What is the scope of your research? What questions are you trying to answer?

  - Cheng Bao: Our research involves the development of dissolvable microneedle patches to deliver capsaicin nanomicelles transdermally for adipose reduction.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What are the most recent developments in your field of research?

  - Jing Fu: Recent developments in this field of research include rapid advances in microneedle-based transdermal delivery for painless, controlled metabolic regulation.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

CONCLUSION:

What significant findings have you established in your field?

  - Yuli Pan: Significant findings established in this field include demonstrating an efficient, needle-free strategy for localized capsaicin delivery with reduced irritation and systemic exposure.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What research gap are you addressing with your protocol?

  - Luna Li: This protocol addresses the absence of simple, scalable methods combining enzymatic self-assembly with dissolvable microneedles for uniform drug loading.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What advantage does your protocol offer compared to other techniques?

  - Chunhui Rui: Our platform supports scalable transdermal delivery of hydrophobic molecules and may accelerate therapeutic development for obesity-related research.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Ethics Title Card

This research has been approved by the Science and Technology Ethics Review Committee of Ludong University (Approval No. LDU-IRB2025020011)

# Protocol

- Preparation of Alpha-Lactalbumin-Based Nanomicelles Encapsulating Capsaicin via Enzymatic Self-Assembly

Demonstrator: Jing Fu, Yuli Pan, Luna Li, Chunhui Rui

  - To begin, dissolve alpha lactalbumin in deionized water to a concentration of 6 milligrams per milliliter [1]. Adjust the pH to 7.4 [2] then use a magnetic stirrer to stir the solution at 8 to 28 g until the protein is completely dissolved [3].

    - WIDE: Talent adding alpha lactalbumin powder to deionized water in a container.

    - Talent adjusting the pH.

    - Talent placing the solution on a magnetic stirrer until clear.

  - Now, add Bacillus licheniformis protease to the solution at an enzyme to substrate ratio of 1 to 100 [1]. Mix gently to ensure uniform distribution of the enzyme [2]. Incubate the mixture at 50 degrees Celsius for 30 minutes to generate amphiphilic peptides [3].

    - Talent measuring and adding Bacillus licheniformis protease to the protein solution.

    - Talent gently stirring the solution to mix the enzyme thoroughly.

    - Talent placing the container into a heating device set to 50 degrees Celsius.

  - Heat the solution to 95 degrees Celsius for 5 minutes to terminate the enzymatic reaction [1]. After cooling the solution to room temperature, filter it through a 0.22-micrometer membrane [2].

    - Talent placing the container into a heating device set to 95 degrees Celsius.

    - Talent filtering the cooled solution through a 0.22 micrometer membrane filter.

  - Next, dissolve capsaicin in ethanol to a concentration of 1 milligram per milliliter [1]. Then add the capsaicin solution dropwise into the peptide solution under gentle stirring [2]. Continue stirring the mixture for 2 hours to allow self-assembly of nanomicelles [3].

    - Talent dissolving capsaicin in ethanol in a separate container.

    - Talent adding the capsaicin solution dropwise into the peptide solution while stirring gently.

    - Talent leaving the solution on a magnetic stirrer.

  - Remove free capsaicin by dialyzing the mixture against deionized water for 12 hours [1-TXT]. Then freeze dry the prepared alpha lactalbumin nanomicelles [2].

    - Talent transferring the mixture into dialysis tubing. TXT: Replace water every 4 h

    - Talent placing the sample into a freeze dryer.

- Fabrication and In Vitro Evaluation of Dissolvable Microneedle Patches Loaded with Capsaicin Nanomicelles

Demonstrator: Jing Fu, Chunhui Rui

  - To fabricate dissolvable microneedle patches, dissolve hyaluronic acid and polyvinyl alcohol in deionized water at 60 degrees Celsius [1-TXT]. Stir until the solution becomes clear [2]. Mix the cooled solution with the capsaicin loaded nanomicelles at a ratio of 4 to 1 [3].

    - Talent adding hyaluronic acid and polyvinyl alcohol to heated deionized water. TXT: Hyaluronic Acid: 5% w/v; Polyvinyl Alcohol: 5% w/v

    - Talent stirring the solution until it appears clear and homogeneous.

    - Talent combining the polymer solution with nanomicelles and mixing thoroughly.

  - Next, degas the mixture under vacuum in a desiccator connected to a vacuum pump at approximately minus 80 kilopascals for 10 minutes [1].

    - Talent placing the mixture into a desiccator and applying vacuum.

  - Load 200 microliters of the degassed mixture into polydimethylsiloxane molds [1] containing a 10 by 10 microneedle array with a height of 600 micrometers [2]. Then centrifuge the molds at 1800 g at room temperature for 10 minutes to ensure complete filling of the microneedle cavities [3].

    - Talent pipetting the mixture into the microneedle molds.

    - Shot of the mold with microneedle arrays.

    - Talent placing the molds into a centrifuge.

  - After filling the molds and centrifuging again, dry the molds under vacuum at approximately minus 80 kilopascals at room temperature for 12 hours [1]. Then carefully peel the microneedle patches from the molds [2].

    - Talent placing the molds into a vacuum chamber for drying.

    - Talent gently removing the microneedle patches from the molds.

  - To perform the in vitro insertion and dissolution test, obtain the excised skin from the shaved abdomen of a mouse [1]. Place the excised skin onto an agarose gel support [2]. Then press the microneedle patch firmly onto the skin for 30 seconds [3-TXT].

    - Shot of excised skin sample.

    - Talent positioning the skin sample flat on agarose gel.

    - Talent applying the microneedle patch onto the skin with firm pressure. TXT: Maintain contact between the patch and skin for 30 min

  - Observe the dissolution of the microneedles [1].

    - Shot of the microneedles dissolving within the skin.

# Results

- Results

  - Transmission electron microscopy showed uniformly dispersed, spherical α-lactalbumin nanomicelles [1]. Capsaicin loading increased the mean diameter from approximately 22 nanometers to 30 nanometers [2].

    - LAB MEDIA: Figure 1A.

    - LAB MEDIA: Figure 1B. Video editor: Highlight the bar chart labeled “SNS-Cap”

  - Confocal laser scanning microscopy showed rapid uptake of Cy3(psy-three)-labeled nanomicelles by 3T3-L1 (Three-T-Three-L-One) preadipocytes within 2 hours [1]. BODIPY (bod-ee-pee) staining indicated that M(Cap) (M-Cap) significantly reduced intracellular lipid droplet accumulation [2].

    - LAB MEDIA: Figure 2A. Video editor: Highlight the merged image

    - LAB MEDIA: Figure 2B. Video editor: Highlight the “M(Cap)” panel

  - Western blot and qPCR analysis showed that M(Cap) treatment downregulated PPARγ (P-P-A-R-Gamma) and C/EBPα (C-E-B-P-Alpha) [1], while upregulating TRPV1(T-R-P-V-One), UCP1(U-C-P-One), and Cyt (sight) C expression [2].

    - LAB MEDIA: Figure 2C and 2D. Video editor: Highlight the PPARγ and C/EBPα bands and bars in the “M(Cap)” group.

    - LAB MEDIA: Figure 2C and 2D. Video editor: Highlight the TRPV1, UCP1, and Cyt C bands and bars in the “M(Cap)” group.

  - Transmission electron microscopy confirmed increased mitochondrial numbers and reduced lipid droplet size in M(Cap)-treated adipocytes [1].

    - LAB MEDIA: Figure 2E. Video editor: Highlight the “M(Cap)” panel

  - Scanning electron microscopy confirmed well-defined pyramidal microneedles [1]. Confocal laser scanning microscopy showed that Cy5-labeled M(Cap) was evenly distributed throughout the microneedle matrix [2].

    - LAB MEDIA: Figure 3A.

    - LAB MEDIA: Figure 3B.

  - Microneedles dissolved completely within 30 minutes after insertion into murine abdominal skin [1], creating distinct microchannels through the stratum corneum [2].

    - LAB MEDIA: Figure 4A. Video editor: Highlight the post-insertion image (right-most photos) showing the flattened microneedles and patch imprint on skin.

    - LAB MEDIA: Figure 4B. Video editor: Highlight the bottom H&E-stained section showing visible microchannels labeled “Microneedle patch”.

  - In vitro release testing showed pH-responsive behavior, with approximately 98% capsaicin release at pH 6.5 [1] and 78% at pH 7.4 after 50 minutes [2].

    - LAB MEDIA: Figure 4C. Video editor: Please highlight the purple curve

    - LAB MEDIA: Figure 4C. Video editor: Please highlight the green curve