# Submission ID #: 70521

# Scriptwriter Name: Kathyayani Sridharan

# Project Page Link: https://review.jove.com/account/file-uploader?src=21508953

# Title: Green Synthesis of Magnesium Nanoparticles from Native Neotropical Savannah Plants for Scalable Nanophytocosmetic Formulations

# Authors and Affiliations:

# Liryel Silva Gasparetto*1,2, Matheus Antônio Novaes*1, Cassiane Maria Vianna Campos1, Juliana Alejandra Sanchez Torres1, Vitor Hugo Brito Salentim1, Lucas de Alcântara Sica de Toledo1 Elizabete de Souza Cândido1,2, Octávio Luiz Franco1,2

1S-Inova Biotech, Programa de Pós-Graduação em Biotecnologia, Universidade Católica Dom Bosco

2Centro de Análises Proteômicas e Bioquímicas, Programa de Pós-graduação em Ciências Genômicas e Biotecnologia, Universidade Católica de Brasília

*These authors contributed equally

# Corresponding Authors:

Octávio Luiz Franco					ocfranco@gmail.com

# Email Addresses for All Authors:

Liryel Silva Gasparetto				liryelg@gmail.com

Matheus Antônio Novaes				matheus_novaes@hotmail.com.br

Cassiane Maria Vianna Campos			cassianemariav@gmail.com

Juliana Alejandra Sanchez Torres			julianasanchez063@gmail.com

Vitor Hugo Brito Salentim				britovhs@gmail.com

Lucas de Alcântara Sica de Toledo			lucastld@gmail.com

Elizabete de Souza Cândido				betty.souza@gmail.com

Octávio Luiz Franco					ocfranco@gmail.com

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

☐ Incorrect

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar? NO

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage? YES, DONE

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: 06/26/2026

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps: 18

Number of Shots:  61 (5 SC)

# Interviews

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context.

Note: The statements have been lightly edited for clarity and to eliminate redundancy

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.

  - Octávio Luiz Franco: Our research focuses on developing sustainable magnesium nanoparticles from native Cerrado plants for cosmetic, pharmaceutical, and topical biomedical applications.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Describe the research contexts or systems in which this protocol can be applied.

  - Octávio Luiz Franco: This protocol can be applied to sustainable nanophytocosmetic development, plant-based nanoparticle synthesis, and scalable cosmetic formulation research.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

CONCLUSION:

What does this protocol allow researchers to study or measure?

  - Octávio Luiz Franco: This protocol allows researchers to synthesize, characterize, and incorporate magnesium nanoparticles into stable nanophytocosmetic topical formulations.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Describe the most important consideration or challenge when performing this protocol.

  - Octávio Luiz Franco: Maintaining consistent extract composition, controlled temperature, and standardized reaction conditions is essential for reproducible nanoparticle synthesis.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

How can future studies build on this work? Describe the questions or research directions that can be investigated next.

  - Octávio Luiz Franco: Future studies can investigate other Cerrado species, optimize nanoparticle properties, and evaluate clinical efficacy in topical cosmetic applications.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

# Protocol

- Bark Extract Preparation and Antioxidant Activity Evaluation of Stryphnodendron adstringens

Demonstrator: Matheus Antônio Novaes

  - To begin, rinse the freshly collected bark with running water to remove soil, dust, and surface impurities [1]. Place the bark samples in an oven at 36 degrees Celsius for 72 hours [2]. Use a knife mill to grind the dried bark to obtain a fine powder [3].

    - WIDE: Talent rinsing bark under running water.

    - Talent placing bark samples into an oven.

    - Talent grinding dried bark using a knife mill.

  - Transfer 200 grams of powdered bark to an Erlenmeyer flask [1]. Add 1000 milliliters of 98 percent ethanol [2]. Seal the flask and keep it at room temperature for 72 hours protected from light, while gently agitating once every 24 hours [3].

    - Talent transferring powdered bark into an Erlenmeyer flask.

    - Talent adds ethanol into the flask.

    - Talent sealing the flask and placing it aside.

  - Filter the extract first through a metal mesh [1] and then through cotton using a funnel to remove residual debris [2].

    - Talent filtering extract through a metal mesh.

    - Talent filtering again through cotton using a funnel.

  - To evaluate the antioxidant activity, prepare a 100 millimolar DPPH solution in methanol [1-TXT]. Dilute the ethanolic bark extract in methanol to obtain concentrations ranging from 0.1 percent to 5 percent volume by volume [2]. Prepare a positive control using vitamin C solutions at the same concentrations [3].

    - Talent preparing 100mM DPPH solution in methanol. TXT: DPPH: 2,2-diphenyl-1-picrylhydrazyl

    - Talent diluting the ethanolic bark extract to obtain concentrations ranging from 0.1%v/v to 5% v/v in methanol.

    - Talent preparing vitamin C positive control solutions at the same concentrations.

  - Dispense 100 microliters of DPPH solution into each well of a 96-well plate [1]. Add 50 microliters of extract or vitamin C solution to each well [2]. Incubate the plate for 30 minutes at room temperature in the dark [3].

    - Talent dispensing DPPH solution into a 96-well plate.

    - Talent adding extract or vitamin C into wells.

    - Talent placing the plate in a dark area.

  - Measure absorbance at 515 nanometers using a spectrophotometer [1] and calculate the [2] radical scavenging activity [3].

    - Talent placing the plate into a spectrophotometer.

    - Representative shot of talent calculating the radical scavenging activity.

    - TEXT ON A PLAIN BACKGROUND:

Radical scavenging activity (%) =(ABS Control DPPH - ABS Sample) ABS Control DPPH x 100

Where:
ABS Control = absorbance of DPPH + Methanol 
ABS Sample = absorbance of DPPH + Extract

- Cell Viability Analysis Using Normal Human Dermal Fibroblasts

Demonstrator: Liryel Silva Gasparetto

  - Culture normal human dermal fibroblasts, or NHDF (N-H-D-F) cells in RPMI 1640 (R-P-M-I-sixteen forty) medium supplemented with 10 percent fetal bovine serum and 1 percent penicillin–streptomycin [1]. Seed cells into 96-well plates at 3 × 104 cells per well and incubate for 24 hours [2]. After replacing the medium with 100 microliters of fresh medium, add 50 microliters of extract solution [3]. Incubate for 24 hours at 37 degrees Celsius with 5 percent carbon dioxide [4].

    - Talent handling cultured cells in medium.

    - Talent seeding cells into a 96-well plate.

    - Talent adding extract after replacing medium.

    - Talent placing the plate in the CO2 incubator.

  - To assess the cell viability, add 10 microliters of MTT (M-T-T) solution to each well after removal of media [1-TXT]. Incubate for 4 hours to allow formazan formation [2]. Add 60 microliters of solubilization solution containing hydrochloric acid in isopropanol to dissolve the crystals [3]. 
Solubilization solution = v:v HCl 370 μL + 99,630 mL C3H8O. Authors: Please verify and confirm whether the isopropanol volume is in milliliters or microliters here?

    - Talent adding MTT solution into wells after removing media from wells. TXT: MTT: 3-(4,5-dimethylthiazol-2-yl)-2,5-diphenyltetrazolium bromide

    - Talent placing the plate in incubator.

    - Talent adding solubilization solution.

  - Measure absorbance at 540 nanometers using a spectrophotometer [1] and calculate the [2] cell viability [3].

    - Talent placing the plate into a spectrophotometer.

    - Representative shot of talent calculating the percentage cell viability.

    - TEXT ON A PLAIN BACKGROUND

Cell Viability (%) = (ABS Sample Extract/ABS Cell Control) x 100 
where
ABS Cell Control = absorbance of untreated control wells containing cells and culture medium only.

ABS Sample Extract = absorbance of wells containing cells treated with the plant extract.

- Green Synthesis and Characterization of Magnesium Nanoparticles

Demonstrator: Liryel Silva Gasparetto

  - Add 9890 microliters of distilled water to a sterile reaction tube [1]. Add 100 microliters of plant extract and 10 microliters of 1 molar magnesium chloride to obtain a final concentration of 10 millimolar nanoparticle suspension [2]. Mix thoroughly to homogenize the solution [3] and incubate the mixture at 75 degrees Celsius for 18 hours [4].

    - Talent adding distilled water into a reaction tube.

    - Talent adding plant extract and magnesium chloride solution.

    - Talent mixing the solution.

    - Talent placing the tube into a heating device at 75 degrees Celsius.

  - After cooling the mixture to room temperature, transfer approximately 750 microliters of nanoparticle suspension into a measurement cell for dynamic light scattering, or DLS (D-L-S) experiments [1]. Place the cell into the instrument and perform measurements at 25 degrees Celsius [2]. Acquire particle size data using an appropriate detection mode and analyze each sample in triplicate with five sub runs per measurement [3].

    - Talent transferring suspension into a measurement cell.

    - Talent placing the cell into the instrument.

    - SCREEN: 4.2.3.mp4 00:18-00:27.

  - For atomic force microscopy experiments, deposit 10 microliters of nanoparticle suspension onto freshly cleaved mica [1]. Dry the sample in a desiccator for 2 hours [2]. Gently rinse the mica sheet three times with 20 microliters of filtered distilled water [3]. Return the sample to the desiccator and allow it to dry at room temperature for an additional 2 hours [4].

    - Talent depositing nanoparticle suspension on mica.

    - Talent placing the sample in a desiccator.

    - Talent rinsing mica sheet carefully with 20 µL of filtered distilled water.

    - Talent placing the sample back into desiccator.

  - Configure the atomic force microscope by performing instrument setup and laser alignment according to instructions [1]. Acquire surface images with a 500 by 500 nanometers scan area [2].

    - SCREEN: 4.4.1.mp4 00:25-00:33.

    - SCREEN: 4.4.2.mp4 00:06-00:14.

- Formulation of Nano-Phytocosmetic and Stability Evaluation

Demonstrator: Liryel Silva Gasparetto

  - For heated phase components preparation, place a container with 29.7 grams of purified water on a magnetic stirrer and heat to 70 to 75 degrees Celsius with gentle stirring [1]. Add 0.50 grams of hydroxyethylcellulose, or HEC (H-E-C), gradually to the heated water while stirring to avoid clumping [2]. Then, add 3 grams of glycerin and mix until a homogeneous solution is obtained [3].

    - Talent heating water on a magnetic stirrer.

    - Talent adding hydroxyethylcellulose slowly.

    - Talent adding glycerin and mixing.

  - To form the cool-down phase, dissolve 3 grams of niacinamide completely in 30 grams of purified water at room temperature [1]. Add 0.3 grams of low molecular weight hyaluronic acid and mix until uniform [2]. Then, add 33.3 grams of magnesium nanoparticles synthesized from S. adstringens and mix gently [3]. Add 0.2 grams of benzyl alcohol and dehydroacetic acid preservatives and mix [4].

    - Talent dissolving 3 g of niacinamide in 30 g of water.

    - Talent adding 0.3 grams of low molecular weight hyaluronic acid.

    - Talent adding 33.3 grams of nanoparticles.

    - Talent adding 0.2 g of benzyl alcohol and dehydroacetic acid preservative and mixing.

  - Cool the heated phase to approximately 40 degrees Celsius [1]. Add the cool-down phase slowly to the heated phase while stirring [2]. Measure the pH of the formulation, ensuring a target pH of 5.0- 6.5 for serum formulations containing niacinamide [3].

    - Talent allowing heated mixture to cool.

    - Talent combining two phases while stirring.

    - Talent measuring pH using a pH meter.

  - For preliminary stability studies up to 12 days, prepare four replicate samples of the cosmetic serum in sealed containers [1]. Subject the samples to six consecutive freeze-thaw cycles by storing at 50 degrees Celsius for 24 hours and then at minus 5 degrees Celsius for 24 hours, completing one full cycle every 48 hours [2]. After each cycle, record organoleptic characteristics by visually inspecting the formulation for changes in appearance, colour, odour, and phase separation [3]. Measure pH at room temperature using a calibrated digital pH meter [4]. Determine viscosity using a rotational viscometer according to the equipment manufacturer’s instructions. [5].

    - Talent filling and sealing four containers.

    - Talent performing freeze-thaw of samples in temperature-controlled storage.

    - Talent visually inspecting samples.

    - Talent measuring pH.

    - Talent measuring viscosity.

  - For accelerated stability studies up to 90 days, prepare eight samples of the cosmetic formulation [1]. Store four samples at 50 degrees Celsius and four samples at 4 degrees Celsius [2]. Evaluate samples at 0, 1, 7, 15, 30, 60, and 90 days [3]. Record organoleptic characteristics by visual inspection [4]. Measure pH and determine viscosity using appropriate instruments according to the manufacturer’s instructions [5].

    - Talent preparing multiple samples.

    - Talent placing samples in different storage conditions.

    - LAB MEDIA: 5.5.4.jpg.

    - Talent inspecting samples visually.

    - Talent measuring pH and viscosity.

# Results

- Results

  - Representative particle size distribution of magnesium nanoparticles, or MgNP (M-G-N-P), synthesized from S. adstringens showed a mean particle size of approximately 70 nanometers with a narrow distribution, indicating a monodisperse population [1]. In these samples, the rapid decay of the correlation curve reflects the faster Brownian motion of smaller particles [2]. In contrast, larger or more heterogeneous populations exhibit broader distributions shifted toward higher diameters [3]. In these samples, the correlation function decays more slowly because larger particles diffuse less rapidly in solution [4].

    - LAB MEDIA: Figure 2A: Video Editor: Please emphasize the figure “Small particles” and the area of blue curve with corresponding X-axis values  in “Size versus intensity percent” plot.

    - LAB MEDIA: Figure 2A: Video Editor: Please highlight the X-axis value where the blue line drops on the correlation graph.

    - LAB MEDIA: Figure 2B: Video Editor: Please emphasize the figure “Larger particles” and the area of blue curve with corresponding X-axis values the  in “size versus intensity percent” plot.

    - LAB MEDIA: Figure 2B: Please highlight the X-axis value where the blue line drops on the correlation graph.

  - Mixed populations may present multiple peaks or asymmetric distributions, signaling the presence of both small particles and aggregates [1]. In these samples, the correlation curve displays a complex, non-linear decay pattern reflecting the particle heterogeneity [2]. The atomic force microscopy images of MgNP showed that the nanoparticles exhibit a smooth surface and predominantly elliptical morphology, depending on the extract source [3].

    - LAB MEDIA: Figure 2C: Video Editor: Please emphasize the figure “double population” and the areas of two blue curves with X-axis values in “size versus intensity percent” plot.

    - LAB MEDIA: Figure 2C: Video Editor: Please highlight the points of drops seen on the blue line and corresponding X-axis values on the correlation graph.

    - LAB MEDIA: Figure 3

  - The formulation stability studies of two representative serum formulations, A and B, assessed over 90 days showed a stable formulation characterized by minimal pH variation [1], consistent viscosity over time [2], and preservation of antioxidant activity [3].

    - LAB MEDIA: Figure 4A: Video Editor: Please highlight the green line and the area within the dotted line simultaneously.

    - LAB MEDIA: Figure 4B: Video Editor: Please highlight the green line and the area within the dotted line simultaneously.

    - LAB MEDIA: Figure 4C: Video Editor: Please highlight the green line and the area within the dotted line simultaneously.

  - Contrastingly, instability in the formulation is indicated by pH drift [1], reduction in viscosity [2], and loss of functional antioxidant activity [3].

    - LAB MEDIA: Figure 4A: Video Editor: Please highlight the red line and the area within the dotted line simultaneously.

    - LAB MEDIA: Figure 4B: Video Editor: Please highlight the red line and the area within the dotted line simultaneously.

    - LAB MEDIA: Figure 4C: Video Editor: Please highlight the red line and the area within the dotted line simultaneously.

- Erlenmeyer
Pronunciation link: https://www.merriam-webster.com/dictionary/Erlenmeyer
IPA: /ˈɝːlənˌmaɪər/
Phonetic Spelling: UR·luhn·my·ur

- Ethanol
Pronunciation link: https://www.merriam-webster.com/dictionary/ethanol
IPA: /ˈɛθəˌnɔːl/, /ˈɛθəˌnoʊl/
Phonetic Spelling: ETH·uh·nawl, ETH·uh·nohl

- Antioxidant
Pronunciation link: https://www.merriam-webster.com/dictionary/antioxidant
IPA: /ˌæntiˈɑːksɪdənt/, /ˌæntaɪˈɑːksɪdənt/
Phonetic Spelling: an·tee·OK·sih·duhnt, an·ty·OK·sih·duhnt

- Methanol
Pronunciation link: https://www.merriam-webster.com/dictionary/methanol
IPA: /ˈmɛθəˌnɔːl/, /ˈmɛθəˌnoʊl/
Phonetic Spelling: METH·uh·nawl, METH·uh·nohl

- 2,2-diphenyl-1-picrylhydrazyl
Pronunciation link: No confirmed link found
IPA: /tuː tuː daɪˈfɛnəl wʌn ˌpɪkrəlˈhaɪdrəzəl/
Phonetic Spelling: too·too·dy·FEN·uhl·wun·PIK·ruhl·HY·druh·zuhl

- Ethanolic
Pronunciation link: No confirmed link found
IPA: /ˌɛθəˈnɑːlɪk/
Phonetic Spelling: eth·uh·NAH·lik

- Absorbance
Pronunciation link: https://www.merriam-webster.com/dictionary/absorbance
IPA: /əbˈzɔːrbəns/, /əbˈsɔːrbəns/
Phonetic Spelling: ub·ZOR·buhns, ub·SOR·buhns

- Spectrophotometer
Pronunciation link: https://www.merriam-webster.com/dictionary/spectrophotometer
IPA: /ˌspɛktroʊfəˈtɑːmətər/
Phonetic Spelling: spek·troh·fuh·TAH·muh·tur

- Fibroblasts
Pronunciation link: https://www.merriam-webster.com/dictionary/fibroblast
IPA: /ˈfaɪbrəˌblæsts/, /ˈfɪbrəˌblæsts/
Phonetic Spelling: FY·bruh·blasts, FIH·bruh·blasts

- Penicillin
Pronunciation link: https://www.merriam-webster.com/dictionary/penicillin
IPA: /ˌpɛnəˈsɪlɪn/
Phonetic Spelling: pen·uh·SIL·in

- Streptomycin
Pronunciation link: https://www.merriam-webster.com/dictionary/streptomycin
IPA: /ˌstrɛptəˈmaɪsɪn/
Phonetic Spelling: strep·toh·MY·sin

- Formazan
Pronunciation link: No confirmed link found
IPA: /ˈfɔːrməzæn/
Phonetic Spelling: FOR·muh·zan

- Solubilization
Pronunciation link: No confirmed link found
IPA: /ˌsɑːljəbələˈzeɪʃən/
Phonetic Spelling: sol·yuh·buh·luh·ZAY·shuhn

- Hydrochloric
Pronunciation link: https://www.merriam-webster.com/dictionary/hydrochloric
IPA: /ˌhaɪdrəˈklɔːrɪk/
Phonetic Spelling: hy·druh·KLOR·ik

- Isopropanol
Pronunciation link: https://www.merriam-webster.com/dictionary/isopropanol
IPA: /ˌaɪsoʊˈproʊpəˌnɔːl/
Phonetic Spelling: eye·soh·PROH·puh·nawl

- Magnesium
Pronunciation link: https://www.merriam-webster.com/dictionary/magnesium
IPA: /mæɡˈniːziəm/
Phonetic Spelling: mag·NEE·zee·uhm

- Nanoparticles
Pronunciation link: https://www.merriam-webster.com/dictionary/nanoparticle
IPA: /ˈnænoʊˌpɑːrtɪkəlz/
Phonetic Spelling: NAN·oh·par·tih·kuhlz

- Homogenize
Pronunciation link: https://www.merriam-webster.com/dictionary/homogenize
IPA: /həˈmɑːdʒəˌnaɪz/
Phonetic Spelling: huh·MAH·juh·nyze

- Microscopy
Pronunciation link: https://www.merriam-webster.com/dictionary/microscopy
IPA: /maɪˈkrɑːskəpi/
Phonetic Spelling: my·KRAH·skuh·pee

- Desiccator
Pronunciation link: https://www.merriam-webster.com/dictionary/desiccator
IPA: /ˈdɛsɪˌkeɪtər/
Phonetic Spelling: DES·ih·kay·tur

- Hydroxyethylcellulose
Pronunciation link: No confirmed link found
IPA: /haɪˌdrɑːksiˌɛθəlˈsɛljəloʊs/
Phonetic Spelling: hy·DROK·see·eth·uhl·SEL·yuh·lohs

- Niacinamide
Pronunciation link: No confirmed link found
IPA: /ˌnaɪəsɪnəˈmaɪd/
Phonetic Spelling: ny·uh·sin·uh·MYDE

- Hyaluronic
Pronunciation link: https://www.merriam-webster.com/dictionary/hyaluronic
IPA: /ˌhaɪələˈrɑːnɪk/
Phonetic Spelling: hy·uh·luh·RAH·nik

- Dehydroacetic
Pronunciation link: No confirmed link found
IPA: /diːˌhaɪdroʊəˈsiːtɪk/
Phonetic Spelling: dee·hy·droh·uh·SEE·tik

- Organoleptic
Pronunciation link: https://www.merriam-webster.com/dictionary/organoleptic
IPA: /ˌɔːrɡənoʊˈlɛptɪk/, /ɔːrˌɡænəˈlɛptɪk/
Phonetic Spelling: or·guh·noh·LEP·tik, or·GAN·uh·LEP·tik

- Viscosity
Pronunciation link: https://www.merriam-webster.com/dictionary/viscosity
IPA: /vɪˈskɑːsəti/
Phonetic Spelling: vih·SKAH·suh·tee

- Viscometer
Pronunciation link: https://www.merriam-webster.com/dictionary/viscometer
IPA: /vɪˈskɑːmətər/
Phonetic Spelling: vih·SKAH·muh·tur

- Monodisperse
Pronunciation link: https://www.merriam-webster.com/dictionary/monodisperse
IPA: /ˌmɑːnoʊdɪˈspɝːs/
Phonetic Spelling: mon·oh·dih·SPURS

- Heterogeneous
Pronunciation link: https://www.merriam-webster.com/dictionary/heterogeneous
IPA: /ˌhɛtərəˈdʒiːniəs/
Phonetic Spelling: het·uh·ruh·JEE·nee·uhs

- Brownian
Pronunciation link: https://www.merriam-webster.com/dictionary/Brownian
IPA: /ˈbraʊniən/
Phonetic Spelling: BROW·nee·uhn

- Asymmetric
Pronunciation link: https://www.merriam-webster.com/dictionary/asymmetric
IPA: /ˌeɪsəˈmɛtrɪk/
Phonetic Spelling: ay·suh·MET·rik

- Aggregates
Pronunciation link: https://www.merriam-webster.com/dictionary/aggregate
IPA: /ˈæɡrɪɡəts/
Phonetic Spelling: AG·rih·guhts

- Morphology
Pronunciation link: https://www.merriam-webster.com/dictionary/morphology
IPA: /mɔːrˈfɑːlədʒi/
Phonetic Spelling: mor·FAH·luh·jee

- Elliptical
Pronunciation link: https://www.merriam-webster.com/dictionary/elliptical
IPA: /ɪˈlɪptɪkəl/
Phonetic Spelling: ih·LIP·tih·kuhl