# Submission ID #: 70521

# Scriptwriter Name: Kathyayani Sridharan

# Project Page Link: https://review.jove.com/account/file-uploader?src=21508953

# Title: Green Synthesis of Magnesium Nanoparticles from Native Neotropical Savannah Plants for Scalable Nanophytocosmetic Formulations

# Authors and Affiliations:

# Liryel Silva Gasparetto*1,2, Matheus Antônio Novaes*1, Cassiane Maria Vianna Campos1, Juliana Alejandra Sanchez Torres1, Vitor Hugo Brito Salentim1, Lucas de Alcântara Sica de Toledo1 Elizabete de Souza Cândido1,2, Octávio Luiz Franco1,2

1S-Inova Biotech, Programa de Pós-Graduação em Biotecnologia, Universidade Católica Dom Bosco

2Centro de Análises Proteômicas e Bioquímicas, Programa de Pós-graduação em Ciências Genômicas e Biotecnologia, Universidade Católica de Brasília

*These authors equally contributed to this work.

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

Octávio Luiz Franco					ocfranco@gmail.com

# Email Addresses for All Authors:

Liryel Silva Gasparetto				liryelg@gmail.com

Matheus Antônio Novaes				matheus_novaes@hotmail.com.br

Cassiane Maria Vianna Campos			cassianemariav@gmail.com

Juliana Alejandra Sanchez Torres			julianasanchez063@gmail.com

Vitor Hugo Brito Salentim				britovhs@gmail.com

Lucas de Alcântara Sica de Toledo			lucastld@gmail.com

Elizabete de Souza Cândido				betty.souza@gmail.com

Octávio Luiz Franco					ocfranco@gmail.com

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

☐ Correct

☐ Incorrect

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  Enter Yes or No.

If a dissection or stereo microscope is required for your protocol, please list all shots from the script that will be visualized using the microscope (shots are indicated with the 3-digit numbers, like 2.1.1, 2.1.2, etc.).

Click here to list microscope shots, using the shot numbers from the protocol section of the video script.

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Enter Yes or No.

If Yes, we will need you to record using screen recording software.

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

As these files are necessary for finalizing your script, please upload all screen captured video files to your project page as soon as possible.

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: MM/DD/YYYY

DO NOT use this draft script for filming. Please wait until your script is finalized to begin the filming process.

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps: 18

Number of Shots:  61

# Interviews

Answers to these questions will become interview statements that you will deliver on camera.

- Introduction: Answer the 1st REQUIRED prompt and 1 additional question; Conclusion: Answer any 3 questions. No more than 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- Speak naturally and avoid reading the lines.

- Limit the length of each statement to 20 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context.

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.

  - Enter full author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the research gap or limitation in existing methods and how this protocol addresses them.

  - Enter full author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the research contexts or systems in which this protocol can be applied.

  - Enter full author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

CONCLUSION:

What does this protocol allow researchers to study or measure?

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the most important consideration or challenge when performing this protocol.

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Are there any additional methods or analyses that can be performed following this procedure?

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

How can future studies build on this work? Describe the questions or research directions that can be investigated next.

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that you/your videographer will capture.

- Bark Extract Preparation and Antioxidant Activity Evaluation of Stryphnodendron adstringens

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

  - To begin, rinse the freshly collected bark with running water to remove soil, dust, and surface impurities [1]. Place the bark samples in an oven at 36 degrees Celsius for 72 hours [2]. Use a knife mill to grind the dried bark to obtain a fine powder [3].

    - WIDE: Talent rinsing bark under running water.

    - Talent placing bark samples into an oven.

    - Talent grinding dried bark using a knife mill.

  - Transfer 200 grams of powdered bark to an Erlenmeyer flask [1]. Add 1000 milliliters of 98 percent ethanol [2]. Seal the flask and keep it at room temperature for 72 hours protected from light, while gently agitating once every 24 hours [3].

    - Talent weighing powdered bark and transferring it into an Erlenmeyer flask.

    - Talent adding ethanol into the flask.

    - Talent sealing the flask and placing it aside.

  - Filter the extract first through a metal mesh [1] and then through cotton using a funnel to remove residual debris [2].

    - Talent filtering extract through a metal mesh.

    - Talent filtering again through cotton using a funnel.

  - To evaluate the antioxidant activity, prepare a 100 millimolar DPPH solution in methanol [1-TXT]. Dilute the ethanolic bark extract in methanol to obtain concentrations ranging from 0.1 percent to 5 percent volume by volume [2]. Prepare a positive control using vitamin C solutions at the same concentrations [3].

    - Talent preparing 100mM DPPH solution in methanol. TXT: DPPH: 2,2-diphenyl-1-picrylhydrazyl

    - Talent diluting the ethanolic bark extract to obtain concentrations ranging from 0.1%v/v to 0.5%v/v in methanol.

    - Talent preparing Vitamin C positive control solutions at same concentrations.

  - Dispense 100 microliters of DPPH solution into each well of a 96-well plate [1]. Add 50 microliters of extract or vitamin C solution to each well [2]. Incubate the plate for 30 minutes at room temperature in the dark [3].

    - Talent dispensing DPPH solution into a 96 well plate.

    - Talent adding extract or vitamin C into wells.

    - Talent placing the plate in a dark area.

  - Measure absorbance at 515 nanometers using a spectrophotometer [1] and calculate the [2] radical scavenging activity [3].

    - Talent placing the plate into a spectrophotometer.

    - Representative shot of talent calculating the radical scavenging activity.

    - TEXT ON A PLAIN BACKGROUND:

Radical scavenging activity (%) =(ABS Control DPPH - ABS Sample) ABS Control DPPH x 100

Where:
ABS Control = absorbance of DPPH + Methanol 
ABS Sample = absorbance of DPPH + Extract

- Cell Viability Analysis

Demonstrator: Click here to enter name of demonstrator(s)

  - Culture normal human dermal fibroblasts, or NHDF (N-H-D-F) cells in RPMI 1640 (R-P-M-I-sixteen forty) medium supplemented with 10 percent fetal bovine serum and 1 percent penicillin–streptomycin [1]. Seed cells into 96-well plates at 3 × 104 cells per well and incubate for 24 hours [2]. Replace the medium with 100 microliters of fresh medium and add 50 microliters of extract solution [3]. Incubate for 24 hours at 37 degrees Celsius with 5 percent carbon dioxide [4].

    - Talent handling cultured cells in medium.

    - Talent seeding cells into a 96 well plate.

    - Talent replacing medium and adding extract.

    - Talent placing the plate in the CO2 incubator.

  - To assess cell viability, add 10 microliters of MTT (M-T-T) solution to each well after removal of media [1-TXT]. Incubate for 4 hours to allow formazan formation [2]. Add 60 microliters of solubilization solution containing hydrochloric acid in isopropanol to dissolve the crystals [3]. Authors: Could you please specify the concentration of HCl and volume of isopropanol used in solubilization solution?

    - Talent adding MTT solution into wells after removing media from wells. TXT: MTT: 3-(4,5-dimethylthiazol-2-yl)-2,5-diphenyltetrazolium bromide

    - Talent placing the plate in incubator.

    - Talent adding solubilization solution.

  - Measure absorbance at 540 nanometers using a spectrophotometer [1] and calculate the [2] cell viability [3].

    - Talent placing the plate into a spectrophotometer.

    - Representative shot of talent calculating the percentage cell viability.

    - TEXT ON A PLAIN BACKGROUND

Cell Viability (%) = (ABS Sample Extract/ABS Cell Control) x 100 
where
ABS Cell Control = absorbance of untreated control wells containing cells and culture medium only.

ABS Sample Extract = absorbance of wells containing cells treated with the plant extract.

- Green Synthesis and Characterization of Magnesium Nanoparticles

Demonstrator: Click here to enter name of demonstrator(s)

  - Add 9890 microliters of distilled water to a sterile reaction tube [1]. Add 100 microliters of plant extract and 10 microliters of 1 molar magnesium chloride to obtain a final concentration of 10 millimolar nanoparticle suspension [2]. Mix thoroughly to homogenize the solution [3] and incubate the mixture at 75 degrees Celsius for 18 hours [4].

    - Talent adding distilled water into a reaction tube.

    - Talent adding plant extract and magnesium chloride solution.

    - Talent mixing the solution.

    - Talent placing the tube into a heating device at 75 degrees Celsius.

  - After cooling the mixture to room temperature, transfer approximately 750 microliters of nanoparticle suspension into a measurement cell for dynamic light scattering, or DLS (D-L-S) experiments [1]. Place the cell into the instrument and perform measurements at 25 degrees Celsius [2]. Acquire particle size data using an appropriate detection mode [3] and analyse each sample in triplicate with five sub runs per measurement [4].

    - Talent transferring suspension into a measurement cell.

    - Talent placing the cell into the instrument.

    - SCREEN: Show acquisition of particle size data using the instrument interface.

    - SCREEN: Show replicate analysis settings being configured

  - For atomic force microscopy, or AFM (A-F-M) experiments, deposit 10 microliters of nanoparticle suspension onto freshly cleaved mica [1]. Dry the sample in a desiccator for 2 hours [2]. Gently rinse the mica sheet three times with 20 microliters of filtered distilled water [3]. Return the sample to the desiccator and allow it to dry at room temperature for an additional 2 hours [4].

    - Talent depositing nanoparticle suspension on mica.

    - Talent placing the sample in a desiccator.

    - Talent rinsing mica sheet carefully with 20 µL of filtered distilled water.

    - Talent placing the sample back into desiccator.

  - Configure the atomic force microscope by performing instrument setup and laser alignment according to instructions [1]. Acquire surface images with a scan area of 500 by 500 nanometers [2].

    - Talent adjusting the microscope settings.

    - SCOPE: Surface image of nanoparticles at nanoscale resolution.

- Formulation of Nano-Phytocosmetic and Stability Evaluation

Demonstrator: Click here to enter name of demonstrator(s)

  - For heated phase components preparation, place a container with 29.7 grams of purified water on a magnetic stirrer and heat to 70 to 75 degrees Celsius with gentle stirring [1]. Add 0.50 grams of hydroxyethylcellulose, or HEC (H-E-C) gradually to the heated water while stirring to avoid clumping [2]. Then, add 3 grams of glycerin and mix until homogeneous solution is obtained [3].

    - Talent heating water on a magnetic stirrer.

    - Talent adding hydroxyethylcellulose slowly.

    - Talent adding glycerin and mixing.

  - To form the cool-down phase, dissolve 3 grams of niacinamide completely in 30 grams of purified water at room temperature [1]. Add 0.3 grams of low molecular weight hyaluronic acid and mix until uniform [2]. Then, add 33.3 grams of magnesium nanoparticles synthesized from S. adstringens and mix gently [3]. Add 0.2 grams of benzyl alcohol and dehydroacetic acid preservatives and mix [4].

    - Talent dissolving 3 g of niacinamide in 30 g of water.

    - Talent adding 0.3 grams of low molecular weight hyaluronic acid.

    - Talent adding 33.3 grams of nanoparticles.

    - Talent adding 0.2 g of benzyl alcohol and dehydroacetic acid preservative and mixing.

  - Cool the heated phase to approximately 40 degrees Celsius [1]. Add the cool down phase slowly to the heated phase while stirring [2]. Measure the pH of the formulation, ensuring a target pH of 5.0- 6.5 for serum formulations containing niacinamide [3].

    - Talent allowing heated mixture to cool.

    - Talent combining two phases while stirring.

    - Talent measuring pH using a pH meter.

  - For preliminary stability studies up to 12 days, prepare four replicate samples of the cosmetic serum in sealed containers [1]. Subject the samples to six consecutive freeze-thaw cycles by storing at 50 degrees Celsius for 24 hours and then at minus 5 degrees Celsius for 24 hours, completing one full cycle every 48 hours [2]. After each cycle, record organoleptic characteristics by visually inspecting the formulation for changes in appearance, colour, odour, and phase separation [3]. Measure pH at room temperature using a calibrated digital pH meter [4]. Determine viscosity using a rotational viscometer according to the equipment manufacturer’s instructions. [5].

    - Talent filling and sealing containers.

    - Talent placing samples in temperature-controlled storage.

    - Talent visually inspecting samples.

    - Talent measuring pH.

    - Talent measuring viscosity.

  - For accelerated stability studies up to 90 days, prepare eight samples of the cosmetic formulation [1]. Store four samples at 50 degrees Celsius and four samples at 4 degrees Celsius [2]. Evaluate samples at 0, 1, 7, 15, 30, 60, and 90 days [3]. Record organoleptic characteristics by visual inspection [4]. Measure pH and determine viscosity using appropriate instruments according to manufacturer’s instructions [5].

    - Talent preparing multiple samples.

    - Talent placing samples in different storage conditions.

    - SCREEN: Show timeline schedule for evaluation points.

    - Talent inspecting samples visually.

    - Talent measuring pH and viscosity.

# Results

Please review this section to make sure that it accurately reflects your findings.

- You/Your videographer does not have to record this section. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 196.

- Please note that the video cannot include voiceover without an accompanying visual.

- Results

  - Representative particle size distribution of magnesium nanoparticles, or MgNP (M-G-N-P) synthesized from S. adstringens showed a mean particle size of approximately 70 nanometers with a narrow distribution, indicating a monodisperse population [1]. In these samples, the rapid decay of the correlation curve reflects the faster Brownian motion of smaller particles [2]. In contrast, larger or more heterogeneous populations exhibit broader distributions shifted toward higher diameters [3]. In these samples, the correlation function decays more slowly because larger particles diffuse less rapidly in solution [4].

    - LAB MEDIA: Figure 2A: Video Editor: Please emphasize the figure small particles and the X-axis values under the area of blue curve in size versus intensity percent plot.

    - LAB MEDIA: Figure 2A: Video Editor: Please highlight the X-axis value where the blue line drops on the correlation graph.

    - LAB MEDIA: Figure 2B: Video Editor: Please emphasize the figure larger particles and the X-axis values under the area of blue curve in size versus intensity percent plot.

    - LAB MEDIA: Figure 2B: Please highlight the X-axis value where the blue line drops on the correlation graph.

  - Mixed populations may present multiple peaks or asymmetric distributions, signaling the presence of both small particles and aggregates [1]. In these samples, the correlation curve displays a complex, non-linear decay pattern reflecting the particle heterogeneity [2]. The atomic force microscopy, or AFM (A-F-M) images of MgNP showed that the nanoparticles exhibit a smooth surface and predominantly elliptical morphology, depending on the extract source [3].

    - LAB MEDIA: Figure 2C: Video Editor: Please emphasize the figure double population and the X-axis values under the areas of two blue curves in size versus intensity percent plot.

    - LAB MEDIA: Figure 2C: Video Editor: Please highlight the X-axis values wherever the blue line drops on the correlation graph.

    - LAB MEDIA: Figure 3

  - The formulation stability studies of two representative serum formulations, A and B, assessed over 90 days showed a stable formulation characterized by minimal pH variation [1], consistent viscosity over time [2], and preservation of antioxidant activity [3].

    - LAB MEDIA: Figure 4A: Video Editor: Please highlight the green line and the area within the dotted line simultaneously.

    - LAB MEDIA: Figure 4B: Video Editor: Please highlight the green line and the area within the dotted line simultaneously.

    - LAB MEDIA: Figure 4C: Video Editor: Please highlight the green line and the area within the dotted line simultaneously.

  - Contrastingly, instability in the formulation is indicated by pH drift [1], reduction in viscosity [2], and loss of functional antioxidant activity [3].

    - LAB MEDIA: Figure 4A: Video Editor: Please highlight the red line and the area within the dotted line simultaneously.

    - LAB MEDIA: Figure 4B: Video Editor: Please highlight the red line and the area within the dotted line simultaneously.

    - LAB MEDIA: Figure 4C: Video Editor: Please highlight the red line and the area within the dotted line simultaneously.