# Submission ID #: 70572

# Scriptwriter Name: Pallavi Sharma

# Project Page Link: https://review.jove.com/files_upload.php?src=21524508

Title: Impact of Common Fruit Juices and Toothbrushing on the Discoloration of Primary Teeth

# Authors and Affiliations:

Emine Kaya, Merve Gul Eren, Hande Elif Ozçıftçi, Gizem Akyıldız, Necmi Cemre Oksuz

1Health Science University, Faculty of Dentistry, Department of Pediatric Dentistry, Sağlık Bilimleri Üniversitesi: Saglik Bilimleri Universitesi

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

Emine Kaya			(eminetass@gmail.com)

# Email Addresses for All Authors:

Merve Gul Eren		(mervegulerence@gmail.com)

Hande Elif Ozçıftçi		(handeelifozciftci@gmail.com)

Gizem Akyıldız			(gizemaky63@gmail.com)

Necmi Cemre Oksuz		(dt.necmicemre@gmail.com)

Emine Kaya			(eminetass@gmail.com)

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

☐ Correct

☐ Incorrect

2. Interview statements: Which interview statement filming option is the most appropriate for your group? Please select one.

☐ 	Interviewees self-record interview statements. JoVE can provide support for this option.

☐ 	Interview Statements are read by JoVE’s voiceover talent.

3. Proposed interview filming date: Please indicate the proposed date that your group will self-film interviews: MM/DD/YYYY

Authors: Since we have protocol footage, this question is applicable for filming interview statements

DO NOT use this draft script for filming Interviews. Please wait until your script is finalized to begin the filming process.

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps:  10

Number of Shots:  12

# Introduction

Answers to these questions will become interview statements that you will deliver on camera.

- Introduction: Answer the 1st REQUIRED prompt and 1 additional question; Conclusion: Answer any 3 questions. No more than 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- Speak naturally and avoid reading the lines.

- Limit the length of each statement to 20 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context.

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.

  - Enter full author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the research gap or limitation in existing methods and how this protocol addresses them.

  - Enter full author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the research contexts or systems in which this protocol can be applied.

  - Enter full author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

CONCLUSION:

What does this protocol allow researchers to study or measure?

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the most important consideration or challenge when performing this protocol.

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Are there any additional methods or analyses that can be performed following this procedure?

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

How can future studies build on this work? Describe the questions or research directions that can be investigated next.

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Ethics Title Card

This research has been approved by the Institutional Human Research Ethics Committee of the University of Health Sciences. Written informed consent has been obtained from the patients

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that you/your videographer will capture.

NOTE: The protocol is scripted from the provided footage

- Investigating the Color Changes Caused by Fruit Juices in Primary Teeth

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

  - To begin, collect a total of 80 sound primary teeth extracted due to trauma, orthodontic reasons, or excessive mobility related to natural exfoliation. Assign 20 specimens to each fruit juice group and the control group [1].

    - LAB MEDIA: Figure 1.

  - After removing remaining gingival tissue and debris from the teeth, store the teeth in saline solution until the experiments begin [1]. Replace the saline solution daily [2].

    - LAB MEDIA: Store_the_teeth_1.mp4: 00:00-end

    - LAB MEDIA: Store_the_teeth_2.mp4: 00:00-00:25

  - Next, create a 4 by 4 millimeter square window on each specimen using red nail polish [1].

    - LAB MEDIA: Creating_4x4_square_window_1.mp4: 00:07-00:24, Creating_4x4_square_window_2.mp4: 00:00-end

  - Then, fill a container with the assigned fruit juice before conducting baseline color measurements [1]. Place each tooth into the container labelled with its specimen number on the outside [2].

    - LAB MEDIA: Placing_tooth_into_a_container_2.mp4: 00:01-00:10

    - LAB MEDIA: Placing_tooth_into_a_container_2.mp4: 00:10-end

  - Then, measure baseline color values for all groups using a spectrophotometer, recording results in Commission Internationale d’Eclairage Lab coordinates relative to a standard illuminant [1].

    - LAB MEDIA: Measurement_Calibration_and_Baseline.mp4: 00:00-end

  - For staining and brushing, immerse the prepared specimens in mulberry juice, pomegranate juice, orange juice, or saline solution for the control group [1].

    - LAB MEDIA: Immerse_the_prepared_specimens.mp4: 00:00-end

  - Incubate all samples at 37 degrees Celsius for 7 and 28 days, refreshing the juice daily [1].

    - LAB MEDIA: refreshing_the_juice_1.mp4 : 00:14-00:29

  - Now, dilute each toothpaste with distilled water at a 1 to 1 weight ratio to obtain a standardized slurry that approximates intraoral dilution during toothbrushing [1].

    - LAB MEDIA: Brushing_Action_and_Slurry_Preparation.mp4: 00:00-00:20.

  - Using an electric toothbrush, brush the specimens in the brushing subgroups once a day on each surface for 5 seconds with either fluoridated toothpaste or non-fluoridated toothpaste [1].

    - LAB MEDIA: Brushing_Action_and_Slurry_Preparation.mp4: 00:25-00:40

  - After measuring color as described earlier, calculate the color difference by determining the mean ΔL, Δa, and Δb values for each specimen [1].

    - LAB MEDIA: excel-screen-video.MOV: 00:04-00:15, 00:33-00:38

# Results

Please review this section to make sure that it accurately reflects your findings.

- You/Your videographer does not have to record this section. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 140.

- Please note that the video cannot include voiceover without an accompanying visual.

- Results

  - Three-way analysis of variance showed significant effects of time [1] and juice type on discoloration [2], while brushing type approached significance [4]. The interaction terms indicated that discoloration patterns varied according to brushing condition and exposure period [5].

    - LAB MEDIA: Table 1. Video editor: Highlight the “P value(s)” cell for “t”

    - LAB MEDIA: Table 1. Video editor: Highlight the “P value(s)” cell for “JT”

    - LAB MEDIA: Table 1. Video editor: Highlight the “P value(s)” cell for “BT”

    - LAB MEDIA: Table 1. Video editor: Highlight the “P value(s)” cells for “JT x BT”, “t x JT”, “t x BT”, and “t x JT x BT”

  - Across most brushing conditions, Δ2 values were higher than Δ1 [1], with the greatest increases observed in black mulberry and pomegranate samples [2].

    - LAB MEDIA: Table 1. Video editor: Show the “Δ1 (t0-t7)” and “Δ2 (t7-t28)” columns side by side

    - LAB MEDIA: Table 1. Video editor: Highlight the rows under “Black Mullberry” and “Pomegranate”  compare the values in the “Δ2 (t7-t28)” column with the “Δ1 (t0-t7)” column

  - In black mulberry, the fluoride-free brushed group and the non-brushed group exhibited significantly greater Δ2 values [1] compared with the fluoride-brushed group [2].

    - LAB MEDIA: Table 1. Video editor: Highlight the “Brushed-Flouride free” and  “Non-brushed” row under “Black Mullberry” in the “Δ2 (t7-t28)” column

    - LAB MEDIA: Table 1. Video editor: Highlight the “Brushed-Flouride” row under “Black Mullberry” in the “Δ2 (t7-t28)” column

  - For pomegranate, the non-brushed group showed notably elevated Δ1 values [1]. However, orange and saline demonstrated minimal interval-related changes [2].

    - LAB MEDIA: Table 1. Video editor: Highlight the “Non-brushed” row under “Pomegranate” in the “Δ1 (t0-t7)” column

    - LAB MEDIA: Table 1. Video editor: Highlight the rows under “Orange” and “Saline” and compare the values in the “Δ1 (t0-t7)” and “Δ2 (t7-t28)” columns

  - Analysis of Δ3 revealed significant effects of juice type [1] and brushing type [2], while their interaction was not significant [3].

    - LAB MEDIA: Table 2. Video editor: Highlight the “P value(s)” cell for “JT”

    - LAB MEDIA: Table 2. Video editor: Highlight the “P value(s)” cell for “BT”

    - LAB MEDIA: Table 2. Video editor: Highlight the “P value(s)” cell for “JT x BT”

  - Total color change was highest in black mulberry and pomegranate [1] and significantly exceeded that of orange and saline across all brushing conditions [2].

    - LAB MEDIA: Table 2. Video editor: Highlight the “Black Mullberry” and “Pomegranate” row across all 3 brushing columns

    - LAB MEDIA: Table 2. Video editor: Highlight the “Orange” and “Saline”  row across all 3 brushing columns