# Submission ID #: 70579

# Scriptwriter Name: Pallavi Sharma

# Project Page Link: https://review.jove.com/account/file-uploader?src=21526643

Title: Fabrication and Surgical Application of Enriched Photo-crosslinked Gelatin–Riboflavin Hydrogels for Corneal Wound Repair in Rabbits

# Authors and Affiliations:

Cristina Romo-Valera 1,2, Jaime Etxebarria 1,2,3, Maddalen Rodriguez-Astigarraga 1,2, Noelia Andollo 1,2,*.

1 Department of Cell Biology and Histology, School of Medicine and Nursing, University of the Basque Country UPV/EHU

2 BEGIKER Ophthalmology Research Group, HRI (health Research Institute)

3 Department of Ophthalmology, University Hospital of Cruces

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

Noelia Andollo: noelia.andollo@ehu.eus

# Email Addresses for All Authors:

Cristina Romo-Valera: cristina.romo@ehu.eus

Maddalen Rodriguez-Astigarraga: maddalen.rodriguez@ehu.eus

Jaime Etxebarria: jaime.echevarriaecenarro@osakidetza.eus

Noelia Andollo: noelia.andollo@ehu.eus

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

☐ Correct

☐ Incorrect

2. Interview statements: Which interview statement filming option is the most appropriate for your group? Please select one.

☐ 	Interviewees self-record interview statements. JoVE can provide support for this option.

☐ 	Interview Statements are read by JoVE’s voiceover talent.

3. Proposed interview filming date: Please indicate the proposed date that your group will self-film interviews: MM/DD/YYYY

Authors: Since we already have the protocol footage, this question is applicable for filming interview statements

DO NOT use this draft script for filming Interviews. Please wait until your script is finalized to begin the filming process.

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps:  12

Number of Shots:  14

# Introduction

Answers to these questions will become interview statements that you will deliver on camera.

- Introduction: Answer the 1st REQUIRED prompt and 1 additional question; Conclusion: Answer any 3 questions. No more than 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- Speak naturally and avoid reading the lines.

- Limit the length of each statement to 20 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context.

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.

  - Enter full author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the research gap or limitation in existing methods and how this protocol addresses them.

  - Enter full author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the research contexts or systems in which this protocol can be applied.

  - Enter full author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

CONCLUSION:

What does this protocol allow researchers to study or measure?

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the most important consideration or challenge when performing this protocol.

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Are there any additional methods or analyses that can be performed following this procedure?

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

How can future studies build on this work? Describe the questions or research directions that can be investigated next.

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Ethics Title Card

This research has been approved by the Animal Research Ethics Committee of the University of the Basque Country (UPV/EHU)  and complied with the ARVO Statement for the Use of Animals in Ophthalmic and Vision Research.

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that you/your videographer will capture.

NOTE: The protocol section was drafted from available footage

- Surgical Application of Hydrogel for Corneal Stromal Wound Repair

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

  - To begin, pipette the required volume of prepared gelatin–riboflavin hydrogel into the target well, mold, dish, or substrate using sterile technique [1].

    - LAB MEDIA: In vitro hydrogel synthesis.MOV:  0:00:06-0:00:20.

  - Position the Led-C (Led-C) curing lamp 2 centimeters above the hydrogel surface and initiate in situ crosslinking for a total of 2 minutes, delivered as six pulses of 20 seconds with 5 to 10 second pauses between pulses to prevent local heating [1-TXT].

    - LAB MEDIA: In vitro hydrogel synthesis.MOV:  0:00:25-0:00:35. TXT: Blue light (420–480 nm, 850–1000 mW/cm²)

  - Then, confirm complete gelation visually [1].

    - LAB MEDIA: In vitro hydrogel synthesis.MOV:  02:08-02:10

  - After placing the anesthetized animal in a lateral decubitus position on a sterile surgical platform and disinfecting the periocular region with povidone-iodine solution, place an eyelid speculum on the operative eye to maintain continuous exposure of the ocular surface during the procedure [1-TXT].

    - LAB MEDIA: Trephination and wound scraping.mp4: 0:00:00-0:00:33. TXT: Anesthesia: Ketamine: 1 mL/kg (50 mg/mL), Xylazine 0.3 mL/kg (20 mg/mL)

  - Center a 6.5-millimeter diameter vacuum trephine on the rabbit cornea [1]. Apply suction to stabilize the device and rotate the trephine three-quarter turns to achieve an approximate stromal depth of 187 micrometers [2].

    - LAB MEDIA: Trephination and wound scraping.mp4: 0:00:33-0:00:36.

    - LAB MEDIA: Trephination and wound scraping.mp4: 0:00:36-0:00:46.

  - Using a crescent blade, perform an anterior stromal keratectomy within the trephined area [1]. Remove the epithelial and anterior stromal layers until a smooth wound bed is obtained [2].

    - Trephination and wound scraping.mp4: 0:01:45-0:02:10, 03:13-03:30

    - Trephination and wound scraping.mp4: 0:03:45-0:04:15

  - Now, fill the corneal defect with 50 microliters of the corresponding hydrogel formulation preheated to 32 degrees Celsius to ensure optimal viscosity [1-TXT].

    - LAB MEDIA: Hydrogel cxl.mp4: 0:00:05-0:00:15 TXT: Human amniotic membrane extract and autologous serum-enriched hydrogels are used

  - Initiate in situ crosslinking by illuminating the corneal surface with blue light at 420 to 480 nanometers for 2 minutes, delivering six pulses of 20 seconds with 5 to 10 second pauses between pulses to limit local heating [1].

    - LAB MEDIA:  Hydrogel cxl.mp4: 0:00:20-0:00:54.

  - To place the first suture, rasp the lateral upper eyelid margin with forceps. Pass the needle through the grey line at the eyelid margin from the skin side to the conjunctival side, taking a full-thickness bite while avoiding deep penetration into the tarsal plate [1].

    - LAB MEDIA: Tarsorrhaphy.mp4: 0:00:00-0:00:24

  - Pass the needle through the corresponding point of the lower eyelid margin from the conjunctival side to the skin side to create apposition of the lid margins [1].

    - LAB MEDIA: Tarsorrhaphy.mp4: 0:00:24-0:00:55

  - Then, tie the suture with a secure surgeon’s knot and two square knots, positioning the knot on the skin surface slightly to the outer side of the eyelid margin rather than directly over it [1].

    - LAB MEDIA: Tarsorrhaphy.mp4: 0:00:55-0:01:19. TXT: Place a second suture 3–4 mm medial if needed

  - At last, trim the suture tails to 3 to 4 millimeters to reduce irritation while leaving enough length for later removal [1-TXT].

    - LAB MEDIA: Tarsorrhaphy.mp4: 0:01:20-0:01:38 TXT: From day 3 to 7, monitor and record ocular healing

# Results

Please review this section to make sure that it accurately reflects your findings.

- You/Your videographer does not have to record this section. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 192.

- Please note that the video cannot include voiceover without an accompanying visual.

- Results

  - Fluorescein staining revealed a progressive reduction in wound area, with most defects fully re-epithelialized by day 5 [1]. At day 3, median wound areas were comparable among all groups with no significant differences [2].

    - LAB MEDIA: Figure 6A. Video editor: Show the sequence of eye images and highlight how the stained area becomes smaller over time until it disappears by day 5.

    - LAB MEDIA: Figure 6B. Video editor: Highlight all four groups on the day 3 plot

  - The control group showed variable wound stability, with 20 percent of corneas displaying persistent defects or reopening by day 7 [1] despite showing the fastest early re-epithelialization, with 60% of corneas achieving complete closure by day 5 [2].

    - LAB MEDIA: Figure 6C–E. Video editor: Highlight the control group at day 7 showing remaining or reappearing open areas.

    - LAB MEDIA: Figure 6D,E. Video editor: Highlight the control group at day 5

  - Hydrogels with autologous serum formulation showed accelerated epithelial repair, reaching a median wound area of 1.09 percent at day 5 and complete closure in 100 percent of corneas by day 7 [1]. Empty hydrogels and human amniotic membrane extract hydrogels promoted wound closure, with 90 percent of corneas healed by day 7, while 10 percent retained residual defects [2].

    - LAB MEDIA: Figure 6C–E. Video editor: Highlight the H-AS group at day 5 and 7 showing very small remaining wound area.

    - LAB MEDIA: Figure 6C–E. Video editor: Highlight the H and H-HAMe groups at day 7 showing mostly closed corneas with a small number still open.

  - At day 3, mild ocular irritation signs such as redness, swelling, and discharge were most frequently observed in the control and hydrogel groups [1]. The hydrogels with autologous serum formulation showed significantly lower irritation scores compared to the control at day 3 [2].

    - LAB MEDIA: Figure 8A. Video editor: Highlight the control and H eye images at day 3 showing visible redness and swelling.

    - LAB MEDIA: Figure 8B,C. Video editor: Highlight the H-AS group on the day 3 score plot showing lower values than the control group.

  - By day 7, irritation scores in the hydrogels with autologous serum formulation returned to 0, indicating full recovery [1].

    - LAB MEDIA: Figure 8C. Video editor: Highlight the H-AS group at day 7 where the values reach 0 on the vertical axis.