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Author Questionnaire
1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No 

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes

3. Filming location: Will the filming need to take place in multiple locations?   Yes
If Yes, how far apart are the locations? Less than 20 feet

4. Testimonials (optional): Would you be open to filming two short testimonial statements live during your JoVE shoot? These will not appear in your JoVE video but may be used in JoVE’s promotional materials. No


Current Protocol Length
Number of Steps:  12
Number of Shots:  26 

Interviews
Videographer: Obtain headshots for all authors available at the filming location. 

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.
1.1. Ervin PROZSA: Our research focuses on finding an efficient and easy method to shape porous metal-organic frameworks for larger applications.
1.1.1. INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

Describe the research contexts or systems in which this protocol can be applied.
1.2. Ervin PROZSA: The protocol provides mild conditions that can be applied to various porous materials. 
1.2.1. INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera
CONCLUSION:
What does this protocol allow researchers to study or measure?
1.3. Ervin PROZSA: This approach allows researchers to shape porous materials directly as monoliths for direct-flow processes.
1.3.1. INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

Describe the most important consideration or challenge when performing this protocol.
1.4. Ervin PROZSA: The most important consideration in this protocol is getting the mass-to-volume ratios and stirrer angle right to form the emulsion.
1.4.1. INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

How can future studies build on this work? Describe the questions or research directions that can be investigated next.
1.5. Ervin PROZSA: Future studies are already underway to replace the polymer in the formulation with silica and produce stronger monoliths.
1.5.1. INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera


Videographer: Obtain headshots for all authors available at the filming location.


Protocol  
Videographer: Please always record an audio slate while filming each shot mentioned in the shotlist.
2. Synthesis of Metal-Organic Frameworks
Demonstrator: Ervin PROZSA 

2.1. To begin, gather the required reagents and materials [1]. Dissolve 15 grams of batteries in 150 milliliters of a 1 to 1 solution of ultrapure water and 37 percent hydrochloric acid in a beaker [2].
2.1.1. WIDE:  Talent walking into the room with a tray of materials 
2.1.2. Talent adding batteries to a beaker containing the prepared ultrapure water and hydrochloric acid solution.
2.2. Place the solution under stirring at 60 g for 24 hours at room temperature [1].
2.2.1. Talent placing the beaker under stirring.
2.3. Then, filter the solution to remove carbon and plastic residues [1].
2.3.1. Talent filtering the solution and collecting the filtrate.
2.4. Dissolve 2 grams of benzene-1,3,5-tricarboxylic acid or BTC (B-T-C) in 500 milliliters of dimethylformamide or DMF (D-M-F) [1].
2.4.1. Talent adding BTC to the bottle containing DMF.
2.5. Place the solution in an ultrasound bath at 37 kilohertz for 30 minutes at room temperature [1].
2.5.1. Talent placing the solution in the ultrasound bath.
2.6. Mix the metallic solution and organic solution in a 1 to 2 ratio [1].
2.6.1. Talent combining the metallic solution and organic solution in the specified ratio.
2.7. Place the mixture in an ultrasound bath at 37 kilohertz for 30 minutes at room temperature [1]. Then, place the mixture in an oven at 90 degrees Celsius for 24 hours [2].
2.7.1. Talent placing the mixture in the ultrasound bath.
2.7.2. Talent placing the mixture in the oven.
2.8. Wash the metal-organic framework or MOF (Mof) 3 times with DMF and 3 times with ethanol via Büchner filtration [1].
2.8.1. Talent washing the MOF by Büchner filtration using DMF followed by ethanol.
2.9. Dry the MOF in an oven at 40 degrees Celsius for 72 hours [1].
2.9.1. Talent placing the MOF in the oven.

3. Preparation of Pickering Emulsions and Polymers

3.1. Dissolve 1.1 grams of MIL-96 (Mil-ninety-six) aluminum in 10 milliliters of ultrapure water in a glass vial [1].
3.1.1. Talent dissolving MIL-96 aluminum in ultrapure water in a glass vial.
3.2. Add 13.35 milliliters of paraffin to the solution [1].
3.2.1. Talent adding paraffin to the solution in the glass vial.
3.3. Using a homogenizer with a single rotor, homogenize the mixture at 15,000 g for 2 minutes to form an emulsion [1].
3.3.1. Talent homogenizing the mixture using the single-rotor homogenizer
3.4. Obtain the required reagents [1], to prepare the Polymerized High Internal Phase Emulsions or PolyHIPE (Poly-hipe) [2]. Using a single-rotor homogenizer, homogenize the solution at 15,000 g [3].
3.4.1. Talent arranging the reagents on the workbench.
3.4.2. TEXT ON A PLAIN BACKGROUND:
MIL-96(Al) - 375 milligrams
Acrylamide - 375 milligrams
Methylene bisacrylamide - 18.75 milligrams
KPS - 18.75 milligrams
Ultrapure water - 3.02 milliliters
3.4.3. Talent homogenizing the solution using the single-rotor homogenizer.
3.5. While stirring, add 0.73 milliliters of Polyvinyl alcohol or PVA (P-V-A) [1] and 11.25 milliliters of paraffin at a fixed ratio of 0.75 volume per volume [2].
3.5.1. Talent adding polyvinyl alcohol to the stirred solution.
3.5.2. Talent adding paraffin to the stirred solution.
3.6. Maintain homogenization at 15,000 g for 2 minutes to form an emulsion [1]. Then, place the mixture in an oven at 80 degrees Celsius for 24 hours to polymerize [2].
3.6.1. Shot of mixture being homogenized.
3.6.2. Talent placing the mixture in the oven.
3.7. Using a Soxhlet extractor, wash the PolyHIPE with ethanol for 48 hours to remove the oil, excess polymer precursors, and PVA [1].
3.7.1. Talent loading the PolyHIPE into a Soxhlet extractor and adding ethanol for solvent extraction.
3.8. Dry the material under vacuum at 100 degrees Celsius [1].
3.8.1. Talent placing the material in a vacuum drying system.
3.9. Prepare the samples [1]. Perform Brunauer–Emmett–Teller or BET (B-E-T) analysis [2]. For powder X-ray diffraction, use a scan range of 5 to 70 degrees [3]. Set the acquisition time to 0.5 seconds per step [4] and use a wavelength of 1.54 angstroms [5].
3.9.1. Talent loading a sample holder with the prepared sample
3.9.2. TEXT ON A PLAIN BACKGROUND:
BET Analysis Parameters:
 Temperature - 77 K
Adsorption - 20 cm³/g to 0.10 P/P₀
Adsorption - 60 cm³/g to 0.90 P/P₀
Desorption - 40 cm³/g between 0.90–0.30 P/P₀
3.9.3. SCREEN: 70585_screenshot_1.png Video editor: Please highlight “Start angle” and “end angle”
3.9.4. SCREEN: 70585_screenshot_1.png Video editor: Please highlight “time per step”
3.9.5. SCREEN: 70585_screenshot_2.png 
3.10. For infrared spectroscopy, use a spectral range of 615 to 4000 reciprocal centimeters [1]. Set the scan time to 1 minute and the number of scans to 4 [2]. Analyze the characterization data obtained from the analyses [3].
3.10.1. SCREEN: SCREEN: 70585_screenshot_3.png Video editor: Please highlight “Range”
3.10.2. SCREEN: SCREEN: 70585_screenshot_4.png Video editor: Please highlight the “Duration”
3.10.3. SCREEN: SCREEN: 70585_screenshot_5.png 


Results
4. Results 

4.1. Pickering emulsions containing polyvinyl alcohol and polymer precursors produced substantially smaller droplets [1] than emulsions without PVA [2].
4.1.1. LAB MEDIA: Figure 1. Video editor: Emphasize panel F.
4.1.2. LAB MEDIA: Figure 1. Video editor: Emphasize panel C.
4.2. Higher MOF content affected the composite specific surface area [1].
4.2.1. LAB MEDIA: Figure 2. Video editor: Emphasize the blue curve labelled MIL-96 with the value "655 m²/g" on the right side and emphasize the black curve labelled M25/10/0.5 with the value "15 m²/g" on the right side.
4.3. Samples containing 0.5 weight percent PVA exhibited higher specific surface areas [1] than samples without PVA [2].
4.3.1. LAB MEDIA: Figure 2. Video editor: Emphasize the red curve labelled "M100/10/0.5" and the red value "91 m²/g".
4.3.2. LAB MEDIA: Figure 2. Video editor: Emphasize the green curve labelled "M100/10/0" and the green value "51 m²/g".
4.4. Incorporation into the polymer matrix reduced the specific surface area [1] compared with pristine MIL-96 [2].
4.4.1. LAB MEDIA: Figure 2. Video editor: Emphasize red, green, and black curves and their values on the right side.
4.4.2. LAB MEDIA: Figure 2. Video editor: Emphasize the blue "MIL-96" curve and the value "655 m²/g" on the right side.
4.5. PVA-containing monoliths displayed unobstructed flow through interconnected pores [1].
4.5.1. LAB MEDIA: Figure 3. Video editor: Emphasize panel D.
4.6. MOF particles were deposited on the pore surfaces of the polymer structure [1].
4.6.1. LAB MEDIA: Figure 3. Video editor: Emphasize panel C.
4.7. Modification of the MOF particles altered their position at the paraffin–water interface [1].
4.7.1. LAB MEDIA: Figure 4. Video editor: Emphasize the yellow arrows and the label MOF layer in the right and left images. 
4.8. Controlled adsorption of fluorinated molecules [1] reduced embedding of MOF particles within the polymer wall [2].
4.8.1. LAB MEDIA: Figure 4. Video editor: Emphasize the purple crystal structure at the top center and the black chemical structure below that.
4.8.2. LAB MEDIA: Figure 4. Video editor: Emphasize the three orange circles inside the grey blocks at the bottom center.
4.9. Polymerization and paraffin removal yielded a hierarchically structured monolith integrating highly accessible MOF particles [1].
4.9.1. LAB MEDIA: Figure 4. Video editor: Emphasize the glass vial containing the white emulsion in the top-left, grey arrows, and the right white column.


1. Ultrapure
Pronunciation link: https://www.merriam-webster.com/dictionary/ultrapure
IPA: /ˌʌl.trəˈpjʊr/
Phonetic Spelling: ul·truh·pyoor
2. Hydrochloric
Pronunciation link: https://www.merriam-webster.com/dictionary/hydrochloric
IPA: /ˌhaɪ.droʊˈklɔːr.ɪk/
Phonetic Spelling: hy·droh·klor·ik
3. Benzene-1,3,5-tricarboxylic
Pronunciation link: https://www.howtopronounce.com/benzene-1-3-5-tricarboxylic-acid
IPA: /ˈben.ziːn ˌtraɪ.kɑːrˌbɑːkˈsɪl.ɪk/
Phonetic Spelling: ben·zeen try·kar·bok·sil·ik
4. Dimethylformamide
Pronunciation link: https://www.merriam-webster.com/dictionary/dimethylformamide
IPA: /daɪˌmeθ.əl.fɔrˈmæm.ɪd/
Phonetic Spelling: dye·meth·uhl·for·mam·id
5. Ultrasound
Pronunciation link: https://www.merriam-webster.com/dictionary/ultrasound
IPA: /ˈʌl.trəˌsaʊnd/
Phonetic Spelling: ul·truh·sownd
6. Metal-organic framework
Pronunciation link: https://www.howtopronounce.com/metal-organic-framework
IPA: /ˌmet̬.əl ɔːrˈɡæn.ɪk ˈfreɪmˌwɝːk/
Phonetic Spelling: met·uhl or·gan·ik fraym·werk
7. Büchner
Pronunciation link: https://www.howtopronounce.com/büchner
IPA: /ˈbʏk.nɚ/
Phonetic Spelling: byook·ner
8. Pickering
Pronunciation link: https://www.howtopronounce.com/pickering
IPA: /ˈpɪk.ər.ɪŋ/
Phonetic Spelling: pik·uh·ring
9. Homogenizer
Pronunciation link: https://www.merriam-webster.com/dictionary/homogenizer
IPA: /həˈmɑː.dʒə.naɪ.zɚ/
Phonetic Spelling: huh·mah·juh·ny·zer
10. Emulsion
Pronunciation link: https://www.merriam-webster.com/dictionary/emulsion
IPA: /ɪˈmʌl.ʃən/
Phonetic Spelling: ih·mul·shuhn
11. Acrylamide
Pronunciation link: https://www.merriam-webster.com/dictionary/acrylamide
IPA: /əˈkrɪl.ə.maɪd/
Phonetic Spelling: uh·kril·uh·myde
12. Methylene bisacrylamide
Pronunciation link: https://www.howtopronounce.com/methylene-bisacrylamide
IPA: /ˈmeθ.əˌliːn ˌbaɪs.əˈkrɪl.ə.maɪd/
Phonetic Spelling: meth·uh·leen bys·uh·kril·uh·myde
13. Polyvinyl
Pronunciation link: https://www.merriam-webster.com/dictionary/polyvinyl
IPA: /ˌpɑː.liˈvaɪ.nəl/
Phonetic Spelling: pol·ee·vye·nul
14. Soxhlet
Pronunciation link: https://www.howtopronounce.com/soxhlet
IPA: /ˈzɑːks.lət/
Phonetic Spelling: zoks·luht
15. Brunauer–Emmett–Teller
Pronunciation link: https://www.howtopronounce.com/brunauer-emmett-teller
IPA: /ˈbruː.naʊ.ɚ ˈem.ət ˈtel.ɚ/
Phonetic Spelling: broo·now·er em·uht tel·er
16. Diffraction
Pronunciation link: https://www.merriam-webster.com/dictionary/diffraction
IPA: /dɪˈfræk.ʃən/
Phonetic Spelling: dih·frak·shuhn
17. Spectroscopy
Pronunciation link: https://www.merriam-webster.com/dictionary/spectroscopy
IPA: /spekˈtrɑː.skə.pi/
Phonetic Spelling: spek·trah·skuh·pee
18. Fluorinated
Pronunciation link: https://www.merriam-webster.com/dictionary/fluorinate
IPA: /ˈflʊr.ə.neɪ.t̬ɪd/
Phonetic Spelling: floor·uh·nay·tid
19. Hierarchically
Pronunciation link: https://www.merriam-webster.com/dictionary/hierarchical
IPA: /ˌhaɪ.ɚˈɑːr.kɪ.kəl.i/
Phonetic Spelling: hy·uh·ar·ki·kuh·lee
20. Monolith
Pronunciation link: https://www.merriam-webster.com/dictionary/monolith
IPA: /ˈmɑː.nəˌlɪθ/
Phonetic Spelling: mon·uh·lith
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