# Submission ID #: 70729

# Scriptwriter Name: Kathyayani Sridharan

# Project Page Link: https://review.jove.com/account/file-uploader?src=21572393

# Title: Green Synthesis of Gold and Silver Nanoparticles Using Plant Extracts, Fungal Filtrates, and Bacterial Cultures

# Authors and Affiliations:

# Joel Eduardo Vielma-Puente1,2, Suanny Mosquera-Romero1,3,4

# 1Facultad de Ciencias Naturales y Matemáticas, ESPOL Polytechnic University

# 2Centro de Investigación y Desarrollo de Nanotecnología, ESPOL Polytechnic University

# 3Centro de Investigación de Agua y Desarrollo Sustentable, ESPOL Polytechnic University

# 4Center for Microbial Ecology & Technology (CMET), Ghent University

# Corresponding Authors:

# Suanny Mosquera-Romero 			suanny.mosquera@espol.edu.ec

# Email Addresses for All Authors:

Joel Eduardo Vielma Puente 			jvielma@espol.edu.ec

Suanny Mosquera-Romero 			suanny.mosquera@espol.edu.ec

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

☐ Incorrect

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar? NO

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage? Yes, all done!

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: 06/22/2026

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps: 17

Number of Shots: 39

# Interviews

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context.

Note: The statements have been slightly edited for clarity.

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.

  - Suanny Mosquera-Romero: Our research involves the development of reproducible methods for synthesizing metallic nanoparticles using plants, algae, fungi, and bacteria.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Describe the research gap or limitation in existing methods and how this protocol addresses them.

  - Suanny Mosquera-Romero: Most nanoparticle synthesis protocols focus on single organisms; our framework enables reproducible comparisons across biological systems.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

CONCLUSION:

What does this protocol allow researchers to study or measure?

  - Joel Vielma-Puente: This protocol enables reproducible green synthesis and UV–Visible spectroscopy and Transmission Electron Microscopy validation of silver and gold nanoparticles.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Describe the most important consideration or challenge when performing this protocol.

  - Joel Vielma-Puente: Reproducible nanoparticle synthesis depends on precise regulation of biological activity and physicochemical parameters such as pH and temperature.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

How can future studies build on this work? Describe the questions or research directions that can be investigated next.

  - Suanny Mosquera-Romero: Future studies could expand the scalability of these biogenic platforms for diverse environmental, antimicrobial, catalytic, and biomedical applications.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

# Protocol

- Phytogenic Synthesis of Silver Nanoparticles (AgNPs) Using Psidium guayaquilensis Leaves

Demonstrator: María Cecilia Arteaga

  - To begin, wash the fresh plant material thoroughly with distilled water [1]. Dry the leaves in a tray dryer with forced airflow at 40 degrees Celsius [2]. Use a hand mill to grind the dried leaf material to obtain a fine powder [3].

    - WIDE: Talent washing fresh plant material with distilled water.

    - Talent placing the leaves in a tray dryer for drying.

    - Talent grinding the dried leaves using a hand mill.

  - Suspend 10 grams of powdered material in 200 milliliters of distilled water [1]. Heat the suspension at 70 degrees Celsius under continuous stirring for 1 hour [2].

    - Talent adding 10 grams of powdered material to 200 milliliters of distilled water.

    - Talent placing the suspension on the heating and stirring equipment.

  - Allow the extract to cool to a temperature of approximately 28 degrees Celsius [1]. Filter the extract under vacuum through qualitative filter paper with Grade 1 specifications [2-TXT]. Store the filtered extract at 4 degrees Celsius in amber bottles until further use [3].

    - Talent setting aside the extract to cool.

    - Talent filtering the extract under vacuum through qualitative filter paper. TXT: Filter paper: Pore size 11 µm, Diameter 110 mm

    - Talent storing the filtered extract in amber bottles.

  - For phytogenic fabrication of silver nanoparticles, or AgNPs, dissolve the appropriate mass of silver nitrate in distilled water to prepare a solution, with a concentration between 1 and 5 millimolar [1]. Mix the silver nitrate solution with the plant extract to obtain final concentrations between 10% and 50% volume per volume [2].

    - Talent dissolving silver nitrate in distilled water to prepare the solution.

    - Talent mixing the silver nitrate solution with the plant extract.

  - Heat and stir the reaction mixture at the selected temperature between 25 and 80 degrees Celsius for the desired reaction time between 0.5 and 1 hour [1]. Allow the reaction mixture to stand at room temperature for 24 hours [2].

    - Talent placing the reaction mixture on the heating and stirring equipment.

    - Talent setting aside the reaction mixture for standing.

  - Centrifuge the brown reaction mixture at 1660 g for 15 minutes at room temperature [1]. Discard the supernatant [2] and collect the solid fraction [3]. Dry the recovered nanoparticles in an oven at 60 degrees Celsius [4].

    - Talent placing the brown reaction mixture in the centrifuge.

    - Talent discarding the supernatant.

    - Talent collecting the solid fraction.

    - Talent placing the recovered nanoparticles in the oven.

- Mycogenic Synthesis of Silver Nanoparticles (AgNPs) Using Earliella sp

  - Transfer actively growing mycelial fragments of Earliella species onto Potato Dextrose Agar plates [1]. Incubate the plates at 28 degrees Celsius for 48 hours [2].

    - WIDE: Talent transferring mycelial fragments onto Potato Dextrose Agar plates.

    - Talent placing the plates in the incubator.

  - Transfer a mycelial fragment into Potato Dextrose Broth [1]. Incubate the culture under constant agitation at 150 revolutions per minute for 5 days [2].

    - Talent transferring a mycelial fragment into Potato Dextrose Broth.

    - Talent placing the culture on the agitation system.

  - Filter the fungal culture through sterile filter paper to separate the mycelial biomass from the extracellular broth [1]. Collect the filtrate for subsequent nanoparticle synthesis [2].

    - Talent filtering the fungal culture through sterile filter paper.

    - Talent collecting the filtrate.

  - For mycogenic fabrication of AgNPs, mix 2.5% to 10% volume per volume fungal broth with a 1 to 10 millimolar silver nitrate solution to a final volume of 50 milliliters [1]. Adjust the final reaction volume according to the experimental condition being tested [2].

    - Talent mixing the fungal extracellular broth with the silver nitrate solution.

    - Talent adjusting the final reaction volume to 500 mL.

  - Stir the reaction mixture at the selected temperature between 25 and 70 degrees Celsius for the desired reaction time between 1 and 4 hours [1]. Allow the solution to cool to room temperature for 24 hours [2].

    - Talent placing the reaction mixture on the stirring equipment.

    - Talent setting aside the solution to cool.

  - After centrifugation, collect the solid fraction [1] and dry in an oven at 60 degrees Celsius [2].

    - Talent collecting the solid fraction after centrifugation.

    - Talent placing the collected material in the oven.

- Characterization of Phytogenic and Mycogenic Silver Nanoparticles by UV Spectroscopy

  - Turn on the ultraviolet-visible spectrophotometer [1]. Allow the instrument to warm up for at least 15 minutes to ensure signal stability [2].

    - WIDE: Talent turning on the ultraviolet-visible spectrophotometer.

    - SCREEN: 4.1.2.mp4. 00:00–00:02; 00:30–00:34; 01:03–01:04; 01:14–01:16

  - Select spectral scanning mode [1]. Configure the wavelength range from 300 to 800 nanometers using a data interval of 1 nanometer [2].

    - SCREEN: 4.2.1.mp4. 00:02–00:04

    - SCREEN: 4.2.2.mp4. 00:03–00:11

  - Collect aliquots of freshly synthesized silver nanoparticle suspensions [1]. Dilute the samples with distilled water as needed to maintain absorbance within the linear detection range [2].

    - Talent collecting aliquots of freshly synthesized nanoparticle suspensions.

    - Talent diluting the samples with distilled water.

  - Perform baseline correction using distilled water as the blank solution [1]. Transfer the prepared sample into a cuvette [2]. Place the cuvette in the sample holder [3]. Record the ultraviolet-visible spectrum over the 300 to 800 nanometer range [4].

    - SCREEN: 4.4.1.mp4. 00:12–00:17; 01:17–01:21

    - Talent transferring the prepared sample into a cuvette.

    - Talent placing the cuvette in the sample holder.

    - SCREEN: 4.4.4.mp4. 00:01–00:03; 00:06–00:09; 00:25–00:29; 00:58–01:02

  - Identify the surface plasmon resonance, or SPR (S-P-R) band corresponding to nanoparticle formation [1].

    - SCREEN: 4.5.1.mp4. 00:04–00:06; 00:15–00:18

# Results

- Results

  - Representative ultraviolet-visible absorption spectra of AgNPs synthesized using P. guayaquilensis leaf extract showed a well-defined SPR band centered between 416 and 425 nanometers, indicating successful NP formation and stable colloidal dispersion [1]. Subsequent transmission electron microscopy confirmed the formation of predominantly quasi-spherical AgNPs with an average size of approximately 24 nanometers and a relatively narrow size distribution [2].

    - LAB MEDIA: Figure 2A. Video Editor: Please emphasize the value 425 in the image.

    - LAB MEDIA: Figure 3A. Video Editor: Please emphasize the spherical shaped particles.

  - Similarly, ultraviolet-visible absorption spectra of AgNPs synthesized using Earliella sp. extracellular fungal filtrate exhibited SPR maxima between 405 and 416 nanometers, confirming effective bioreduction of silver ions and AgNP formation [1].

    - LAB MEDIA: Figure 2C. Video Editor: Please emphasize the value 403 in the image.

Pronunciation Guide:

- Phytogenic
Pronunciation link: https://www.merriam-webster.com/dictionary/phytogenic
IPA: /ˌfaɪtoʊˈdʒenɪk/
Phonetic Spelling: fy·toh·jen·ik

- Synthesis
Pronunciation link: https://www.merriam-webster.com/dictionary/synthesis
IPA: /ˈsɪnθəsəs/
Phonetic Spelling: sin·thuh·suhs

- Nanoparticles
Pronunciation link: https://www.merriam-webster.com/dictionary/nanoparticle
IPA: /ˌnænoʊˈpɑrtɪkəl/
Phonetic Spelling: nan·oh·par·tuh·kuhl

- Psidium
Pronunciation link: https://www.howtopronounce.com/psidium
IPA: /ˈsɪdiəm/
Phonetic Spelling: SID·ee·uhm

- guayaquilensis
Pronunciation link: https://www.howtopronounce.com/guayaquilensis
IPA: /ɡwaɪˌjɑːkɪˈlɛnsɪs/
Phonetic Spelling: gwy·yah·kee·LEN·sis

- Distilled
Pronunciation link: https://www.merriam-webster.com/dictionary/distilled
IPA: /dɪˈstɪld/
Phonetic Spelling: dih·STILD

- Celsius
Pronunciation link: https://www.merriam-webster.com/dictionary/Celsius
IPA: /ˈselsiəs/
Phonetic Spelling: SEL·see·uhs

- Suspension
Pronunciation link: https://www.merriam-webster.com/dictionary/suspension
IPA: /səˈspenʃən/
Phonetic Spelling: suh·SPEN·shuhn

- Qualitative
Pronunciation link: https://www.merriam-webster.com/dictionary/qualitative
IPA: /ˈkwɑləˌteɪtɪv/
Phonetic Spelling: KWAH·luh·tay·tiv

- Specifications
Pronunciation link: https://www.merriam-webster.com/dictionary/specification
IPA: /ˌspesəfəˈkeɪʃən/
Phonetic Spelling: spes·uh·fuh·KAY·shuhn

- Amber
Pronunciation link: https://www.merriam-webster.com/dictionary/amber
IPA: /ˈæmbər/
Phonetic Spelling: AM·ber

- Fabrication
Pronunciation link: https://www.merriam-webster.com/dictionary/fabrication
IPA: /ˌfæbrɪˈkeɪʃən/
Phonetic Spelling: fab·ruh·KAY·shuhn

- Silver
Pronunciation link: https://www.merriam-webster.com/dictionary/silver
IPA: /ˈsɪlvər/
Phonetic Spelling: SIL·ver

- Nitrate
Pronunciation link: https://www.merriam-webster.com/dictionary/nitrate
IPA: /ˈnaɪˌtreɪt/
Phonetic Spelling: NY·trayt

- Millimolar
Pronunciation link: https://www.merriam-webster.com/dictionary/millimolar
IPA: /ˌmɪləˈmoʊlər/
Phonetic Spelling: mil·uh·MOH·ler

- Centrifuge
Pronunciation link: https://www.merriam-webster.com/dictionary/centrifuge
IPA: /ˈsentrəˌfjuːdʒ/
Phonetic Spelling: SEN·truh·fyooj

- Supernatant
Pronunciation link: https://www.merriam-webster.com/dictionary/supernatant
IPA: /ˌsuːpərˈneɪtənt/
Phonetic Spelling: soo·per·NAY·tuhnt

- Mycogenic
Pronunciation link: https://www.howtopronounce.com/mycogenic
IPA: /ˌmaɪkəˈdʒenɪk/
Phonetic Spelling: my·kuh·JEN·ik

- Earliella
Pronunciation link: https://www.howtopronounce.com/earliella
IPA: /ˌɪərliˈɛlə/
Phonetic Spelling: eer·lee·EL·uh

- Mycelial
Pronunciation link: https://www.merriam-webster.com/dictionary/mycelial
IPA: /maɪˈsiːliəl/
Phonetic Spelling: my·SEE·lee·uhl

- Potato
Pronunciation link: https://www.merriam-webster.com/dictionary/potato
IPA: /pəˈteɪtoʊ/
Phonetic Spelling: puh·TAY·toh

- Dextrose
Pronunciation link: https://www.merriam-webster.com/dictionary/dextrose
IPA: /ˈdekˌstroʊs/
Phonetic Spelling: DEK·strohs

- Agar
Pronunciation link: https://www.merriam-webster.com/dictionary/agar
IPA: /ˈeɪɡɑr/
Phonetic Spelling: AY·gar

- Incubate
Pronunciation link: https://www.merriam-webster.com/dictionary/incubate
IPA: /ˈɪnkjəˌbeɪt/
Phonetic Spelling: IN·kyuh·bayt

- Agitation
Pronunciation link: https://www.merriam-webster.com/dictionary/agitation
IPA: /ˌædʒəˈteɪʃən/
Phonetic Spelling: aj·uh·TAY·shuhn

- Biomass
Pronunciation link: https://www.merriam-webster.com/dictionary/biomass
IPA: /ˈbaɪoʊˌmæs/
Phonetic Spelling: BY·oh·mass

- Extracellular
Pronunciation link: https://www.merriam-webster.com/dictionary/extracellular
IPA: /ˌekstrəˈseljələr/
Phonetic Spelling: ek·struh·SEL·yuh·ler

- Filtrate
Pronunciation link: https://www.merriam-webster.com/dictionary/filtrate
IPA: /ˈfɪlˌtreɪt/
Phonetic Spelling: FIL·trayt

- Spectrophotometer
Pronunciation link: https://www.merriam-webster.com/dictionary/spectrophotometer
IPA: /ˌspektrəfoʊˈtɑːmətər/
Phonetic Spelling: SPEK·truh·foh·TAH·muh·ter

- Ultraviolet-visible
Pronunciation link: https://www.merriam-webster.com/dictionary/ultraviolet
IPA: /ˌʌltrəˈvaɪələt/
Phonetic Spelling: ul·truh·VY·uh·luht

- Spectral
Pronunciation link: https://www.merriam-webster.com/dictionary/spectral
IPA: /ˈspektrəl/
Phonetic Spelling: SPEK·truhl

- Wavelength
Pronunciation link: https://www.merriam-webster.com/dictionary/wavelength
IPA: /ˈweɪvˌleŋθ/
Phonetic Spelling: WAYV·length

- Aliquots
Pronunciation link: https://www.merriam-webster.com/dictionary/aliquot
IPA: /ˈælɪˌkwɑt/
Phonetic Spelling: AL·ih·kwaht

- Absorbance
Pronunciation link: https://www.merriam-webster.com/dictionary/absorbance
IPA: /əbˈzɔːrbəns/
Phonetic Spelling: ub·ZOR·buhns

- Baseline
Pronunciation link: https://www.merriam-webster.com/dictionary/baseline
IPA: /ˈbeɪsˌlaɪn/
Phonetic Spelling: BAYS·line

- Cuvette
Pronunciation link: https://www.merriam-webster.com/dictionary/cuvette
IPA: /kjuːˈvet/
Phonetic Spelling: kyoo·VET

- Plasmon
Pronunciation link: https://www.howtopronounce.com/plasmon
IPA: /ˈplæzmɑːn/
Phonetic Spelling: PLAZ·mon

- Resonance
Pronunciation link: https://www.merriam-webster.com/dictionary/resonance
IPA: /ˈrezənəns/
Phonetic Spelling: REZ·uh·nuhns