# Submission ID #: 70729

# Scriptwriter Name: Kathyayani Sridharan

# Project Page Link: https://review.jove.com/account/file-uploader?src=21572393

# Title: Green Synthesis of Gold and Silver Nanoparticles Using Plant Extracts, Fungal Filtrates, and Bacterial Cultures

# Authors and Affiliations:

# Joel Eduardo Vielma-Puente1,2, Suanny Mosquera-Romero1,3,4

# 1Facultad de Ciencias Naturales y Matemáticas, ESPOL Polytechnic University

# 2Centro de Investigación y Desarrollo de Nanotecnología, ESPOL Polytechnic University

# 3Centro de Investigación de Agua y Desarrollo Sustentable, ESPOL Polytechnic University

# 4Center for Microbial Ecology & Technology (CMET), Ghent University

# Corresponding Authors:

# Suanny Mosquera-Romero 			suanny.mosquera@espol.edu.ec

# Email Addresses for All Authors:

Joel Eduardo Vielma Puente 			jvielma@espol.edu.ec

Suanny Mosquera-Romero 			suanny.mosquera@espol.edu.ec

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

☐ Incorrect

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar? NO

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage? NO

Authors: Please create screen capture videos for shots labelled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=21572393

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: 06/22/2026

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps: 17

Number of Shots: 39

# Interviews

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context.

Note: The statements have been slightly edited for clarity.

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.

  - Suanny Mosquera-Romero: Our research involves the development of reproducible methods for synthesizing metallic nanoparticles using plants, algae, fungi, and bacteria.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Describe the research gap or limitation in existing methods and how this protocol addresses them.

  - Suanny Mosquera-Romero: Most nanoparticle synthesis protocols focus on single organisms; our framework enables reproducible comparisons across biological systems.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

CONCLUSION:

What does this protocol allow researchers to study or measure?

  - Joel Vielma-Puente: This protocol enables reproducible green synthesis and, UV–Visible spectroscopy and Transmission Electron Microscopy validation of silver and gold nanoparticles.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Describe the most important consideration or challenge when performing this protocol.

  - Joel Vielma-Puente: Reproducible nanoparticle synthesis depends on precise regulation of biological activity and physicochemical parameters such as pH and temperature.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

How can future studies build on this work? Describe the questions or research directions that can be investigated next.

  - Suanny Mosquera-Romero: Future studies could expand the scalability of these biogenic platforms for diverse environmental, antimicrobial, catalytic, and biomedical applications.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

# Protocol

- Phytogenic Synthesis of Silver Nanoparticles (AgNPs) Using Psidium guayaquilensis Leaves

Demonstrator: María Cecilia Arteaga

  - To begin, wash the fresh plant material thoroughly with distilled water [1]. Dry the leaves in a tray dryer with forced airflow at 40 degrees Celsius [2]. Use a hand mill to grind the dried leaf material to obtain a fine powder [3].

    - WIDE: Talent washing fresh plant material with distilled water.

    - Talent placing the leaves in a tray dryer for drying.

    - Talent grinding the dried leaves using a hand mill.

  - Suspend 10 grams of powdered material in 200 milliliters of distilled water [1]. Heat the suspension at 70 degrees Celsius under continuous stirring for 1 hour [2].

    - Talent adding 10 grams of powdered material to 200 milliliters of distilled water.

    - Talent placing the suspension on the heating and stirring equipment.

  - Allow the extract to cool to room temperature of approximately 28 degrees Celsius [1]. Filter the extract under vacuum through qualitative filter paper with Grade 1 specifications [2-TXT]. Store the filtered extract at 4 degrees Celsius in amber bottles until further use [3].

    - Talent setting aside the extract to cool.

    - Talent filtering the extract under vacuum through qualitative filter paper. TXT: Filter paper: Pore size 11 µm, Diameter 110 mm

    - Talent storing the filtered extract in amber bottles.

  - For phytogenic fabrication of silver nanoparticles, or AgNPs, dissolve the appropriate mass of silver nitrate in distilled water to prepare a solution, at a concentration between 1 and 5 millimolar [1]. Mix the silver nitrate solution with the plant extract to obtain final concentrations between 10% and 50% volume per volume [2].

    - Talent dissolving silver nitrate in distilled water to prepare the solution. (Authors: Please specify the exact concentration that will be demonstrated in the filming process. We will update the narrative accordingly.)

    - Talent mixing the silver nitrate solution with the plant extract. (Authors: Please specify the demonstrated concentration at the time of filming.)

  - Heat and stir the reaction mixture at the selected temperature between 25 and 80 degrees Celsius for the desired reaction time between 0.5 and 1 hour [1]. Allow the reaction mixture to stand at room temperature for 24 hours [2].

    - Talent placing the reaction mixture on the heating and stirring equipment. (Authors: Please specify the exact temperature and time that will be used during the filming.)

    - Talent setting aside the reaction mixture for standing.

  - Centrifuge the brown reaction mixture at 1660 g for 15 minutes at room temperature [1]. Discard the supernatant [2] and collect the solid fraction [3]. Dry the recovered nanoparticles in an oven at 60 degrees Celsius [4].

    - Talent placing the brown reaction mixture in the centrifuge.

    - Talent discarding the supernatant.

    - Talent collecting the solid fraction.

    - Talent placing the recovered nanoparticles in the oven.

- Mycogenic Synthesis of Silver Nanoparticles (AgNPs) Using Earliella sp

  - Transfer actively growing mycelial fragments of Earliella species onto Potato Dextrose Agar plates [1]. Incubate the plates at 28 degrees Celsius for 48 hours [2].

    - WIDE: Talent transferring mycelial fragments onto Potato Dextrose Agar plates.

    - Talent placing the plates in the incubator.

  - Transfer a mycelial fragment into Potato Dextrose Broth [1]. Incubate the culture under constant agitation at 150 revolutions per minute for 5 days [2].

    - Talent transferring a mycelial fragment into Potato Dextrose Broth.

    - Talent placing the culture on the agitation system.

  - Filter the fungal culture through sterile filter paper to separate the mycelial biomass from the extracellular broth [1]. Collect the filtrate for subsequent nanoparticle synthesis [2].

    - Talent filtering the fungal culture through sterile filter paper.

    - Talent collecting the filtrate.

  - For mycogenic fabrication of AgNPs, mix 2.5% to 10% volume per volume fungal broth with a 1 to10 millimolar silver nitrate solution to a final volume of 50 milliliters [1]. Adjust the final reaction volume according to the experimental condition being tested [2].

    - Talent mixing the fungal extracellular broth with the silver nitrate solution. (Authors: Please specify the exact concentrations of fungal broth and AgNO3 solutions that will be mixed during filming.)

    - Talent adjusting the final reaction volume to 500 mL.

  - Stir the reaction mixture at the selected temperature between 25 and 70 degrees Celsius for the desired reaction time between 1 and 4 hours [1]. Allow the solution to cool to room temperature for 24 hours [2].

    - Talent placing the reaction mixture on the stirring equipment. (Authors: Please specify the exact temperature and duration that shall be demonstrated for this step.)

    - Talent setting aside the solution to cool.

  - After centrifugation, collect the solid fraction [1] and dry in an oven at 60 degrees Celsius [2].

    - Talent collecting the solid fraction after centrifugation.

    - Talent placing the collected material in the oven.

- Characterization of Phytogenic and Mycogenic Silver Nanoparticles by UV Spectroscopy

Authors: Please create screen capture videos for shots labelled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=21572393

  - Turn on the ultraviolet-visible spectrophotometer [1]. Allow the instrument to warm up for at least 15 minutes to ensure signal stability [2].

    - WIDE: Talent turning on the ultraviolet-visible spectrophotometer.

    - Shot of the instrument warming up prior to measurements.

  - Select spectral scanning mode [1]. Configure the wavelength range from 300 to 800 nanometers using a data interval of 1 nanometer [2].

    - SCREEN: Select Spectral Scanning Mode on the ultraviolet-visible spectrophotometer software.

    - SCREEN: Set the wavelength range to 300–800 nanometers and the data interval to 1 nanometer.

  - Collect aliquots of freshly synthesized silver nanoparticle suspensions [1]. Dilute the samples with distilled water as needed to maintain absorbance within the linear detection range [2].

    - Talent collecting aliquots of freshly synthesized nanoparticle suspensions.

    - Talent diluting the samples with distilled water.

  - Perform baseline correction using distilled water as the blank solution [1]. Transfer the prepared sample into a cuvette [2]. Place the cuvette in the sample holder [3]. Record the ultraviolet-visible spectrum over the 300 to 800 nanometer range [4].

    - SCREEN: Perform baseline correction using distilled water as the blank solution.

    - Talent transferring the prepared sample into a cuvette.

    - Talent placing the cuvette in the sample holder.

    - SCREEN: Record the ultraviolet-visible spectrum over the 300–800 nanometer range.

  - Identify the surface plasmon resonance, or SPR (S-P-R) band corresponding to nanoparticle formation [1].

    - SCREEN: Display the recorded spectrum and identify the surface plasmon resonance band corresponding to nanoparticle formation.

Authors: Please create screen capture videos for shots labelled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=21572393

# Results

- Results

  - Representative ultraviolet-visible absorption spectra of AgNPs synthesized using P. guayaquilensis leaf extract showed a well-defined SPR band centered between 416 and 425 nanometers, indicating successful NP formation and stable colloidal dispersion [1]. Subsequent transmission electron microscopy confirmed the formation of predominantly quasi-spherical AgNPs with an average size of approximately 24 nanometers and a relatively narrow size distribution [2].

    - LAB MEDIA: Figure 2A. Video Editor: Please emphasize the value 425 in the image.

    - LAB MEDIA: Figure 3A. Video Editor: Please emphasize the spherical shaped particles.

  - Similarly, ultraviolet-visible absorption spectra of AgNPs synthesized using Earliella sp. extracellular fungal filtrate exhibited SPR maxima between 405 and 416 nanometers, confirming effective bioreduction of silver ions and AgNP formation [1].

    - LAB MEDIA: Figure 2C. Video Editor: Please emphasize the value 403 in the image.