# Submission ID #: 70729

# Scriptwriter Name: Kathyayani Sridharan

# Project Page Link: https://review.jove.com/account/file-uploader?src=21572393

# Title: Green Synthesis of Gold and Silver Nanoparticles Using Plant Extracts, Fungal Filtrates, and Bacterial Cultures

# Authors and Affiliations:

# Joel Eduardo Vielma-Puente1,2, Suanny Mosquera-Romero1,3,4

# 1Facultad de Ciencias Naturales y Matemáticas, ESPOL Polytechnic University

# 2Centro de Investigación y Desarrollo de Nanotecnología, ESPOL Polytechnic University

# 3Centro de Investigación de Agua y Desarrollo Sustentable, ESPOL Polytechnic University

# 4Center for Microbial Ecology & Technology (CMET), Ghent University

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

# Suanny Mosquera-Romero 			suanny.mosquera@espol.edu.ec

# Email Addresses for All Authors:

Joel Eduardo Vielma Puente 			jvielma@espol.edu.ec

Suanny Mosquera-Romero 			suanny.mosquera@espol.edu.ec

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

☐ Correct

☐ Incorrect

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  Enter Yes or No.

If a dissection or stereo microscope is required for your protocol, please list all shots from the script that will be visualized using the microscope (shots are indicated with the 3-digit numbers, like 2.1.1, 2.1.2, etc.).

Click here to list microscope shots, using the shot numbers from the protocol section of the video script.

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Enter Yes or No.

If Yes, we will need you to record using screen recording software.

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

As these files are necessary for finalizing your script, please upload all screen captured video files to your project page as soon as possible.

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: MM/DD/YYYY

DO NOT use this draft script for filming. Please wait until your script is finalized to begin the filming process.

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps: 17

Number of Shots: 39

# Interviews

Answers to these questions will become interview statements that you will deliver on camera.

- Introduction: Answer the 1st REQUIRED prompt and 1 additional question; Conclusion: Answer any 3 questions. No more than 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- Speak naturally and avoid reading the lines.

- Limit the length of each statement to 20 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context.

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.

  - Enter full author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the research gap or limitation in existing methods and how this protocol addresses them.

  - Enter full author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the research contexts or systems in which this protocol can be applied.

  - Enter full author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

CONCLUSION:

What does this protocol allow researchers to study or measure?

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Describe the most important consideration or challenge when performing this protocol.

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Are there any additional methods or analyses that can be performed following this procedure?

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

How can future studies build on this work? Describe the questions or research directions that can be investigated next.

  - Enter full author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that you/your videographer will capture.

- Phytogenic Synthesis of Silver Nanoparticles (AgNPs) Using Psidium guayaquilensis Leaves

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

  - To begin, wash the fresh plant material thoroughly with distilled water [1]. Dry the leaves in a tray dryer with forced airflow at 40 degrees Celsius [2]. Use a hand mill to grind the dried leaf material to obtain a fine powder [3].

    - WIDE: Talent washing fresh plant material with distilled water.

    - Talent placing the leaves in a tray dryer for drying.

    - Talent grinding the dried leaves using a hand mill.

  - Suspend 10 grams of powdered material in 200 milliliters of distilled water [1]. Heat the suspension at 70 degrees Celsius under continuous stirring for 1 hour [2].

    - Talent adding 10 grams of powdered material to 200 milliliters of distilled water.

    - Talent placing the suspension on the heating and stirring equipment.

  - Allow the extract to cool to room temperature of approximately 28 degrees Celsius [1]. Filter the extract under vacuum through qualitative filter paper with Grade 1 specifications [2-TXT]. Store the filtered extract at 4 degrees Celsius in amber bottles until further use [3].

    - Talent setting aside the extract to cool.

    - Talent filtering the extract under vacuum through qualitative filter paper. TXT: Filter paper: Pore size 11 µm, Diameter 110 mm

    - Talent storing the filtered extract in amber bottles.

  - For phytogenic fabrication of silver nanoparticles, or AgNPs (A-G-N-Peace) , dissolve the appropriate mass of silver nitrate in distilled water to prepare a solution, at a concentration between 1 and 5 millimolar [1]. Mix the silver nitrate solution with the plant extract to obtain final concentrations between 10% and 50% volume per volume [2].

    - Talent dissolving silver nitrate in distilled water to prepare the solution.

    - Talent mixing the silver nitrate solution with the plant extract.

  - Heat and stir the reaction mixture at the selected temperature between 25 and 80 degrees Celsius for the desired reaction time between 0.5 and 1 hour [1]. Allow the reaction mixture to stand at room temperature for 24 hours [2].

    - Talent placing the reaction mixture on the heating and stirring equipment.

    - Talent setting aside the reaction mixture for standing.

  - Centrifuge the brown reaction mixture at 1660 g for 15 minutes at room temperature [1]. Discard the supernatant [2] and collect the solid fraction [3]. Dry the recovered nanoparticles in an oven at 60 degrees Celsius [4].

    - Talent placing the brown reaction mixture in the centrifuge.

    - Talent discarding the supernatant.

    - Talent collecting the solid fraction.

    - Talent placing the recovered nanoparticles in the oven.

- Mycogenic Synthesis of Silver Nanoparticles (AgNPs) Using Earliella sp

Demonstrator: Click here to enter name of demonstrator(s)

  - Transfer actively growing mycelial fragments of Earliella species onto Potato Dextrose Agar plates [1]. Incubate the plates at 28 degrees Celsius for 48 hours [2].

    - WIDE: Talent transferring mycelial fragments onto Potato Dextrose Agar plates.

    - Talent placing the plates in the incubator.

  - Transfer a mycelial fragment into Potato Dextrose Broth [1]. Incubate the culture under constant agitation at 150 revolutions per minute for 5 days [2].

    - Talent transferring a mycelial fragment into Potato Dextrose Broth.

    - Talent placing the culture on the agitation system.

  - Filter the fungal culture through sterile filter paper to separate the mycelial biomass from the extracellular broth [1]. Collect the filtrate for subsequent nanoparticle synthesis [2].

    - Talent filtering the fungal culture through sterile filter paper.

    - Talent collecting the filtrate.

  - For mycogenic fabrication of AgNPs, mix 2.5% to 10% volume per volume fungal broth with a 1 to10 millimolar silver nitrate solution to a final volume of 50 milliliters [1]. Adjust the final reaction volume according to the experimental condition being tested [2].

    - Talent mixing the fungal extracellular broth with the silver nitrate solution.

    - Talent adjusting the final reaction volume. (Authors: Could you please specify the final volume that will be demonstrated at this step?)

  - Stir the reaction mixture at the selected temperature between 25 and 70 degrees Celsius for the desired reaction time between 1 and 4 hours [1]. Allow the solution to cool to room temperature for 24 hours [2].

    - Talent placing the reaction mixture on the stirring equipment.

    - Talent setting aside the solution to cool.

  - After centrifugation, collect the solid fraction [1] and dry in an oven at 60 degrees Celsius [2].

    - Talent collecting the solid fraction after centrifugation.

    - Talent placing the collected material in the oven.

- Characterization of Phytogenic and Mycogenic Silver Nanoparticles by UV Spectroscopy

Demonstrator: Click here to enter name of demonstrator(s)

  - Turn on the ultraviolet-visible spectrophotometer [1]. Allow the instrument to warm up for at least 15 minutes to ensure signal stability [2].

    - WIDE: Talent turning on the ultraviolet-visible spectrophotometer.

    - Shot of the instrument warming up prior to measurements.

  - Select spectral scanning mode [1]. Configure the wavelength range from 300 to 800 nanometers using a data interval of 1 nanometer [2].

    - SCREEN: Select Spectral Scanning Mode on the ultraviolet-visible spectrophotometer software.

    - SCREEN: Set the wavelength range to 300–800 nanometers and the data interval to 1 nanometer.

  - Collect aliquots of freshly synthesized silver nanoparticle suspensions [1]. Dilute the samples with distilled water as needed to maintain absorbance within the linear detection range [2].

    - Talent collecting aliquots of freshly synthesized nanoparticle suspensions.

    - Talent diluting the samples with distilled water.

  - Perform baseline correction using distilled water as the blank solution [1]. Transfer the prepared sample into a cuvette [2]. Place the cuvette in the sample holder [3]. Record the ultraviolet-visible spectrum over the 300 to 800 nanometer range [4].

    - SCREEN: Perform baseline correction using distilled water as the blank solution.

    - Talent transferring the prepared sample into a cuvette.

    - Talent placing the cuvette in the sample holder.

    - SCREEN: Record the ultraviolet-visible spectrum over the 300–800 nanometer range.

  - Identify the surface plasmon resonance, or SPR (S-P-R) band corresponding to nanoparticle formation [1].

    - SCREEN: Display the recorded spectrum and identify the surface plasmon resonance band corresponding to nanoparticle formation.

# Results

Please review this section to make sure that it accurately reflects your findings.

- You/Your videographer does not have to record this section. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 088.

- Please note that the video cannot include voiceover without an accompanying visual.

- Results

  - Representative ultraviolet-visible absorption spectra of AgNPs synthesized using P. guayaquilensis leaf extract showed a well-defined SPR band centered between 416 and 425 nanometers, indicating successful NP formation and stable colloidal dispersion [1]. Subsequent transmission electron microscopy confirmed the formation of predominantly quasi-spherical AgNPs with an average size of approximately 24 nanometers and a relatively narrow size distribution [2].

    - LAB MEDIA: Figure 2A. Video Editor: Please emphasize the value 425 in the image.

    - LAB MEDIA: Figure 3A. Video Editor: Please emphasize the spherical shaped particles.

  - Similarly, ultraviolet-visible absorption spectra of AgNPs synthesized using Earliella sp. extracellular fungal filtrate exhibited SPR maxima between 405 and 416 nanometers, confirming effective bioreduction of silver ions and AgNP formation [1].

    - LAB MEDIA: Figure 2C. Video Editor: Please emphasize the value 403 in the image.