# Submission ID #: 70782

# Scriptwriter Name: Poornima G

# Project Page Link: https://review.jove.com/account/file-uploader?src=21588558

# Title: A 3D Bone Culture Platform Using Human Osteocytes and Decellularized Extracellular Matrix for Modeling Musculoskeletal Diseases

# Authors and Affiliations:

# Francisco Verdugo-Avello1, Sebastián Carrasco1, Tomás Hermann2, Coralia Rivas1, Jorge R. Toledo1

# 1Laboratorio de Biotecnología y Biofarmacia, Departamento de Fisiopatología, Facultad de Ciencias Biológicas, Universidad de Concepción

# 2Hospital Traumatológico de Concepción, Servicio Salud Concepción

# Corresponding Authors:

# Francisco Verdugo-Avello	frverdugo@udec.cl

# Email Addresses for All Authors:

# Sebastián Carrasco		scarrasco2016@udec.cl

# Tomás Hermann		thermann@udec.cl

# Coralia Rivas			corivas@udec.cl

# Jorge R. Toledo		jotoledo@udec.cl

# Francisco Verdugo-Avello	frverdugo@udec.cl

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

☐ Correct

☐ Incorrect

2. Interview statements: Which interview statement filming option is the most appropriate for your group? Please select one.

☐ 	Interviewees self-record interview statements. JoVE can provide support for this option.

3. Proposed interview filming date: Please indicate the proposed date that your group will self-film interviews: MM/DD/YYYY

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps:  25

Number of Shots:  57

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context

Answers will be slightly edited in accordance with journal guidelines.

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.

  - Francisco Verdugo-Avello: Our research develops accessible, biologically relevant 3D bone culture platforms for tissue engineering, disease modeling, regenerative medicine, and related translational applications.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

Describe the research contexts or systems in which this protocol can be applied.

  - Francisco Verdugo-Avello: This protocol can be applied to bone tissue engineering, biomaterial testing, musculoskeletal disease modeling, drug screening, and regenerative medicine research.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

CONCLUSION:

What does this protocol allow researchers to study or measure?

  - Francisco Verdugo-Avello: This protocol enables researchers to study cell viability, morphology, cell–matrix interactions, osteogenic behavior, and biomaterial biocompatibility within a 3D environment.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

Describe the most important consideration or challenge when performing this protocol.

  - Francisco Verdugo-Avello: Key challenges include careful hydrogel handling, even cell distribution, and preventing premature GelMA gelation during construct preparation.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

How can future studies build on this work? Describe the questions or research directions that can be investigated next.

  - Francisco Verdugo-Avello: Future studies can incorporate patient-derived cells, vascularized constructs, transcriptomics, and disease-specific models to study bone remodeling, metastasis, osteoporosis, and therapeutic responses.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

Videographer: Obtain headshots for all authors available at the filming location.

# Ethics Title Card

This research has been approved by the Scientific Ethics Committee of the Concepción Health Service

# Protocol

Authors: During filming, please point out the organs or veins before dissecting them.

- Decellularization and Lyophilization of Human Femoral Head Bone

  - NOTE: Step 2.1 was empty, an extra bullet was added by mistake, protocol starts from 2.2

  - To begin, thaw the human femoral head [1] obtained from a patient during hip replacement surgery gradually to 25 degrees Celsius [2]. Cut the femoral head in half and then cut each half into smaller pieces [3].

    - WIDE: Talent picking up the femoral head from a refrigerator.

    - Close-up of placing the femoral head in an incubator or on the work bench.

    - Talent cutting each femoral head in half and cutting the femoral head half into smaller pieces.

  - Immerse the bone pieces in sterile distilled water at 60 degrees Celsius [1] and sonicate for 15 minutes at 40 kilohertz continuously [2].

    - Talent immersing the bone pieces in sterile distilled water.

    - Talent placing the immersed bone pieces in the sonicator.

  - Then, wash the sample in 300 milliliters of distilled water preheated to 60 degrees Celsius while shaking at 200 revolutions per minute for 5 minutes [1].

    - Talent adding preheated distilled water to the sample and keeping it on a shaker.

  - Centrifuge the sample at 1850 g for 15 minutes at 25 degrees Celsius [1]. Remove the water and repeat the washing step 2 more times [2].

    - Talent placing the sample in the centrifuge.

    - Talent removing the water from the sample and adding fresh water.

  - Sterilize the tissue in a solution containing 3 percent hydrogen peroxide and 0.02 percent peroxyacetic acid [1]. Then, sonicate the sample at 40 kilohertz for 10 minutes at 60 degrees Celsius [2].

    - Talent placing the tissue in the sterilization solution.

    - Talent placing the sample in a sonicator.

  - Transfer the tissue to 300 milliliters of 70 percent ethanol [1] and sonicate at 40 kilohertz for 10 minutes at 21 degrees Celsius [2].

    - Talent transferring the tissue to 300 milliliters of 70 percent ethanol.

    - Talent placing the tissue in ethanol in the sonicator.

  - Next, wash the sample twice with 300 milliliters of distilled water [1]. Incubate the sample at 60 degrees Celsius for 10 minutes on a shaker set to 200 revolutions per minute [2] and centrifuge at 1850 g for 15 minutes at 25 degrees Celsius [3].

    - Talent washing the sample with distilled water.

    - Talent placing the sample for shaking in an incubator.

    - Talent placing the sample in the centrifuge.

  - Pre-freeze the bone at minus 80 degrees Celsius for 4 hours [1]. Then, place the decellularized bone in a wide-base container [2] and lyophilize the sample at 0.05 millibars and minus 40 to minus 60 degrees Celsius for 24 hours [3].

    - Talent placing the bone for pre-freezing in a freezer.

    - Talent placing the decellularized bone in a wide-base container.

    - Talent placing the sample in lyophilizer.

- Preparation of Decellularized Bone Microparticles

  - Place the decellularized bone fragments in a 250-milliliter flask containing the sterilizing solution [1] and homogenize until a uniform white solution is obtained [2].

    - Talent placing decellularized bone fragments into 250 milliliter flask with sterilizing solution.

    - Talent homogenizing the bone fragments until a uniform white solution forms.

  - Centrifuge the homogenate at 1850 g for 15 minutes at 25 degrees Celsius [1]. After discarding the supernatant, wash the pellet twice with 300 milliliters of distilled water at 25 degrees Celsius, agitating at 200 revolutions per minute for 10 minutes [2]. Then, perform a final centrifugation at 1850 g for 15 minutes at 25 degrees Celsius [3].

    - Talent placing the sample in the centrifuge.

    - Talent adding water to the pellet and placing the sample under agitation.

    - Talent placing the sample back into the centrifuge for final centrifugation.

  - Lyophilize the resulting material at 0.05 millibar and minus 40 to minus 60 degrees Celsius for 48 hours [1]. Next, mechanically mill the lyophilized cortical or medullary bone using a sterilized ceramic mortar until a fine powder is obtained [2].

    - Talent placing the material in the lyophilizer.

    - Talent milling the lyophilized bone in a sterilized ceramic mortar.

  - Pass the dry powder through a 200-micrometer mesh or sieve [1] and weigh the final material before storage at minus 80 degrees Celsius [2].

    - Talent adding the dry powder onto a 200 micrometer mesh or sieve.

    - Talent weighing the final powdered material on a weighing balance.

- Preparation of Methacrylated Gelatin-Bone Composite Hydrogel

  - Dissolving 1 gram of methacrylated gelatin in 9.5 milliliters of deionized water tempered at 50 degrees Celsius to prepare a 10% solution [1]. Cool the solution to 37 degrees Celsius [2] and add Irgacure 2959 photo-initiator solution [3].

    - Talent adding GelMA to deionized water and placing the mixture.

    - Talent placing the solution aside on the work surface to cool.

    - Talent adding Irgacure 2959 photoinitiator solution to the mixture.

  - Filter-sterilize the solution using a 0.22 micrometer filter, maintaining the solution at 37 degrees Celsius [1]. Then, add decellularized bone microparticles to achieve a final concentration of 1% weight by volume [2].

    - Talent adding the solution onto a 0.22 micrometer filter.

    - Talent adding decellularized bone microparticles to the solution.

  - Mix the components by pipetting up and down carefully while avoiding bubble formation until a homogeneous suspension is obtained [1].

    - Talent mixing the solution by pipetting the mixture up and down carefully and then showing the homogeneous suspension without bubbles.

- Isolation and Culture of Bone Marrow-Derived Cells

  - Extract and mince the bone marrow tissue from the interior of the femoral head using sterile surgical instruments [1] and transfer the minced tissue to a sterile Petri dish [2]. Wash the tissue three times with alpha minimum essential culture medium supplemented with antibiotic-antimycotic solution [3-TXT].

    - Talent extracting and mincing bone marrow tissue from the femoral head using sterile surgical instruments.

    - Talent transferring the minced tissue into a sterile Petri dish.

    - Talent washing the tissue with supplemented culture medium. TXT: 100 μg/mL Penicillin; 100 μg/mL Streptomycin; 0.25 μg/mL Amphotericin

  - After rinsing the sample with Hank’s Balanced Salt Solution or HBSS, incubate it [1] with collagenase and EDTA with intervening HBSS washes to thoroughly dissociate the tissue [2].

    - Talent adding Hank’s Balanced Salt Solution to the tissue.

    - TEXT ON PLAIN BACKGROUND:

- Incubate the tissue in collagenase Type I (25 min, 37 °C, gentle agitation)

- Wash with HBSS

- Repeat collagenase digestion + HBSS wash (2x)

- Incubate the sample with 0.5 mM EDTA (25 min, 37 °C)

- Wash with HBSS

- Repeat incubation with EDTA + HBSS (2x)

- Perform final collagenase digestion (25 min, 37 °C) + HBSS wash

  - Collect the collagenase solution [1] and the final wash solution into a 50-milliliter centrifuge tube [2].

    - Talent collecting the collagenase solution into a tube.

    - Talent transferring the wash solution into the same tube.

  - Centrifuge the solution at 1000 g for 5 minutes at room temperature [1]. Discard the supernatant [2] and resuspend the pellet in 2 milliliters of complete alpha minimum essential medium [3].

    - Talent placing the tube in the centrifuge.

    - Talent discarding the supernatant from the tube.

    - Talent resuspending the pellet in complete culture medium.

  - Then, seed the cell suspension into two T75 culture flasks [1] and incubate at 37 degrees Celsius with 5 percent carbon dioxide [2]. Replace the culture medium every 2 to 3 days until adequate confluency is achieved [3].

    - Talent seeding the cell suspension into two T75 culture flasks.

    - Talent placing the flasks into the incubator.

    - Talent removing the culture medium in the flask and adding fresh medium.

- Bioink Preparation and 3D Cell Encapsulation

  - Prewarm the required amount of bone gel hydrogel at 37 degrees Celsius [1]. Detach the cultured osteocytes using a standard trypsinization protocol [2]. Centrifuge the sample in a 15-milliliter tube at 500 g for 5 minutes [3].

    - Talent placing the bone gel hydrogel for prewarming at 37 degrees Celsius.

    - Talent detaching cultured osteocytes.

    - Talent placing the 15 milliliter tube in the centrifuge.

  - Resuspend the pellet in 200 microliters of culture medium tempered at 37 degrees Celsius [1]. Mix the cell suspension with the bone gel to obtain a final cell density of at least 1,000 cells per microliter, forming the bioink [2]. Using a P-1000 pipette, add 50 microliters of the bioink per construct to each well of the culture plate and allow the bioink to physically gel for 5 minutes at room temperature [3].

    - Talent resuspending the pellet in culture medium.

    - Talent mixing the cell suspension with bone gel hydrogel.

    - Talent pipetting bioink into wells of the culture plate and keeping the plate aside.

  - Expose each well to 365-nanometer ultraviolet light for 1 minute to achieve irreversible crosslinking at 0.3 joules per square centimeter [1]. Then, add culture medium to each well [2] and incubate the constructs at 37 degrees Celsius with 5 percent carbon dioxide for the required time points using a separate plate for each time point [3].

    - Talent placing the culture plate under ultraviolet light for crosslinking.

    - Talent adding culture medium to the wells.

    - Talent placing the culture plates into the incubator.

  - Finally, assess scaffold biocompatibility by measuring cell viability using live-dead fluorescence staining and metabolic activity using the alamarBlue assay [1].

    - Talent adding the stain to the sample wells.

# Results

- Results

  - Primary osteocytes were detectable in culture approximately 5 days after extraction and displayed a stellate morphology forming interconnected networks characteristic of osteocytes [1].

    - LAB MEDIA: Figure 3.

  - Metabolic activity in osteocyte-laden constructs at each time interval showed significant differences [1] relative to the control [2].

    - LAB MEDIA: Figure 5. Video editor: Highlight the bars for TE1, TE2, and TE3

    - LAB MEDIA: Figure 5. Video editor: Highlight the bars for Control

  - After 7 days of culture, strong calcein acetoxymethyl fluorescence indicated widespread viable cells throughout the hydrogel matrix [1].

    - LAB MEDIA: Figure 6A. Video editor: Show only day 7 images and highlight the green fluorescent cells in panels A3

  - Minimal ethidium homodimer-1 signal indicated low cytotoxicity in the constructs [1].

    - LAB MEDIA: Figure 6. Video editor: Show only day 7 images and highlight  the image B3

- Femoral
Pronunciation link: https://www.merriam-webster.com/dictionary/femoral
IPA: /ˈfemərəl/
Phonetic Spelling: fem·uh·ruhl

- Sonicate
Pronunciation link: https://www.merriam-webster.com/dictionary/sonicate
IPA: /ˈsɑːnəˌkeɪt/
Phonetic Spelling: saa·nuh·kayt

- Centrifuge
Pronunciation link: https://www.merriam-webster.com/dictionary/centrifuge
IPA: /ˈsɛntrəˌfjuːdʒ/
Phonetic Spelling: sen·truh·fyooj

- Peroxyacetic
Pronunciation link: https://www.howtopronounce.com/peroxyacetic
IPA: /pəˌrɑːksiəˈsiːtɪk/
Phonetic Spelling: puh·rok·see·uh·see·tik

- Decellularized
Pronunciation link: https://www.howtopronounce.com/decellularized
IPA: /diːˈsɛljələraɪzd/
Phonetic Spelling: dee·sel·yuh·luh·ryzd

- Lyophilize
Pronunciation link: https://www.merriam-webster.com/dictionary/lyophilize
IPA: /laɪˈɑːfəˌlaɪz/
Phonetic Spelling: ly·aa·fuh·lyz

- Homogenize
Pronunciation link: https://www.merriam-webster.com/dictionary/homogenize
IPA: /həˈmɑːdʒəˌnaɪz/
Phonetic Spelling: huh·maa·juh·nyz

- Supernatant
Pronunciation link: https://www.merriam-webster.com/dictionary/supernatant
IPA: /ˈsuːpərˌneɪtənt/
Phonetic Spelling: soo·per·nay·tuhnt

- Methacrylated
Pronunciation link: https://www.howtopronounce.com/methacrylated
IPA: /məˈθækrɪleɪtɪd/
Phonetic Spelling: muh·thak·ruh·lay·tid

- Gelatin
Pronunciation link: https://www.merriam-webster.com/dictionary/gelatin
IPA: /ˈdʒelətɪn/
Phonetic Spelling: jel·uh·tin

- Deionized
Pronunciation link: https://www.merriam-webster.com/dictionary/deionize
IPA: /diˈaɪəˌnaɪzd/
Phonetic Spelling: dee·eye·uh·nyzd

- Photoinitiator
Pronunciation link: https://www.howtopronounce.com/photoinitiator
IPA: /ˌfoʊtoʊɪˈnɪʃieɪtər/
Phonetic Spelling: foe·toe·ih·nish·ee·ay·ter

- Osteocytes
Pronunciation link: https://www.merriam-webster.com/dictionary/osteocyte
IPA: /ˈɑːstiəˌsaɪt/, /ˈɑːsteɪəˌsaɪt/
Phonetic Spelling: ahs·tee·uh·syts

- Collagenase
Pronunciation link: https://www.merriam-webster.com/medical/collagenase
IPA: /kəˈlædʒəˌneɪs/
Phonetic Spelling: kuh·la·juh·nays

- Amphotericin
Pronunciation link: https://www.merriam-webster.com/medical/amphotericin
IPA: /ˌæmfoʊˈtɛrəsɪn/
Phonetic Spelling: am·foh·ter·uh·sin

- Biocompatibility
Pronunciation link: https://www.merriam-webster.com/dictionary/biocompatibility
IPA: /ˌbaɪoʊkəmˌpætəˈbɪləti/
Phonetic Spelling: by·oh·kuhm·pat·uh·bil·uh·tee

- Cytotoxicity
Pronunciation link: https://www.merriam-webster.com/medical/cytotoxicity
IPA: /ˌsaɪtoʊtɑːkˈsɪsɪti/
Phonetic Spelling: sy·toe·tok·sis·uh·tee

- Irgacure 2959

Pronunciation link: https://www.howtopronounce.com/irgacure
IPA: /ˈɜːrɡəkjʊr tuː ˈnaɪn faɪv naɪn/
Phonetic Spelling: ur·guh·kyur too·nine·five·nine