TITLE:

A Microfluidic System for Modeling Endothelial Dysfunction under Combined Physiological Pulsatile Shear Stress and Oscillatory Hyperglycemia

AUTHORS AND AFFILIATIONS:

Si-Yu Hu1,2, Xiao-Yu Xu3, Chun-Dong Xue*1,3,4, Kai-Rong Qin*1,3,4

1Institute of Cardio-Cerebrovascular Medicine, Central Hospital of Dalian University of Technology, Dalian, 116033, Liaoning, China

2School of Mechanical Engineering, Dalian University of Technology, Dalian, 116024, Liaoning, China

3School of Biomedical Engineering, Faculty of Medicine, Dalian University of Technology, Dalian, 116024, Liaoning, China

4Key Laboratory of Integrated Circuit and Biomedical Electronic System, Dalian University of Technology, Dalian, 116024, Liaoning, China

*CORRESPONDING AUTHORS:

Chun-Dong Xue	(xuechundong@dlut.edu.cn)

Kai-Rong Qin		(krqin@dlut.edu.cn)

EMAIL ADDRESSES OF CO-AUTHORS:

Si-Yu Hu		(husiyu@mail.dlut.edu.cn)

Xiao-Yu Xu		(xxy2018@mail.dlut.edu.cn)

KEYWORDS:

Microfluidics, endothelial dysfunction, pulsatile shear stress, oscillatory hyperglycemia, oxidative stress, Micro-PIV

SUMMARY:

Here, we present a protocol to fabricate and operate a microfluidic system that exposes endothelial cells to synchronized oscillatory hyperglycemia and pulsatile shear stress. This approach provides a physiologically relevant in vitro model for studying diabetic endothelial dysfunction. This protocol enables quantitative measurement of oxidative stress and endothelial cell responses.

ABSTRACT:

Endothelial dysfunction in diabetic vascular complications involves complex interactions between metabolic disturbances, specifically oscillatory glucose (OG) and pulsatile shear stress (PSS). Although these factors have been investigated in isolation, conventional models remain limited to static high-glucose or simplified laminar flow, lacking the capacity to mimic the integrated spatiotemporal coupling found in the diabetic vasculature. By utilizing a programmable microfluidic platform, this protocol provides a valuable platform to investigate the integrated effects of synchronized oscillatory hyperglycemia and physiological PSS on endothelial cells. This protocol aims to model endothelial dysfunction under physiologically relevant coupled metabolic and mechanical conditions. The use of a polydimethylsiloxane (PDMS) chip combined with a pressure-driven control system allows for the precise, independent modulation of flow waveforms and glucose concentration profiles. The hemodynamic fidelity of the system is validated by Micro-Particle Image Velocimetry (Micro-PIV), while the cellular response is quantitatively characterized by monitoring intracellular reactive oxygen species (ROS) levels and cell viability. Representative results demonstrate that physiological PSS effectively attenuates the oxidative injury induced by OG. This effect is demonstrated by reduced intracellular ROS levels and improved cell viability under combined stimulation conditions. Depending on the research question, parameters such as shear stress patterns, glucose oscillation frequencies, and channel geometries can be adjusted. This method serves as a versatile tool for mechanistic studies of mechanobiological pathways and drug screening for therapeutic interventions in diabetic vascular disease.

INTRODUCTION:

Endothelial dysfunction is a critical early event in the development of diabetic vascular complications, driven by both metabolic disturbances and abnormal hemodynamic forces1,2. OG levels, rather than sustained hyperglycemia alone, are increasingly recognized as potent inducers of oxidative stress and inflammatory signaling in endothelial cells, leading to vascular injury and impaired homeostasis3–5. Concurrently, hemodynamic shear stress is a major determinant of endothelial phenotype, with PSS under physiological exercise conditions promoting nitric oxide production, antioxidant defense, and vascular protection6–8. Therefore, understanding the integrated effects of oscillatory hyperglycemia and hemodynamic stimulation is essential for elucidating mechanisms of endothelial dysfunction.

Conventional in vitro models, which often rely on static high-glucose conditions or simplified laminar flow, fail to replicate the complex, dynamic interplay between metabolic and mechanical cues present in vivo9–11. While animal models capture systemic aspects of diabetes, they lack the cellular-level resolution needed to dissect signaling under controlled microenvironmental conditions12. Microfluidic technology offers an effective alternative, providing precise spatiotemporal control of biochemical and biomechanical stimuli in physiologically relevant geometries13, and has driven significant recent advancements across various innovative biomedical applications14,15. For example, Chen et al.16 designed a microfluidic device with spatial and temporal wall shear stress and ATP signaling for studying endothelial cell intracellular Ca2+ dynamics. Yu et al.11 developed a hemodynamic microfluidic chip system for detecting the cellular responses under different combinations of physiological PSS and high glucose concentrations. Although these systems have been used to study endothelial responses to shear stress or single-factor metabolic perturbations, few have successfully integrated both glucose oscillations and PSS within a single system. Therefore, a standardized, reproducible protocol that synchronizes both factors in a controlled microfluidic setting remains lacking.

This method addresses this gap by establishing a reproducible microfluidic system capable of delivering coupled OG and PSS. The primary goal of this approach is to model oxidative stress, impaired cell viability and mechanobiological responses underlying endothelial dysfunction in a physiologically relevant manner. Unlike static culture or conventional perfusion chambers, this approach improves upon existing models by enabling simultaneous and controlled modulation of both metabolic and mechanical stimuli, more closely approximating the diabetic vascular microenvironment. Furthermore, the system is compatible with live-cell imaging, real-time monitoring, and molecular analysis, making it suitable for a wide range of applications including mechanistic studies, disease modeling, and drug screening for endothelial function and injury.

PROTOCOL:

Ethics statement:

NOTE: All reagents, devices, and software used in this protocol are listed in the Table of Materials.

- Microfluidic chip fabrication

  - Use computer-aided design (CAD) software to design the structure of the microfluidic chip (W x L x H = 2 mm x 30 mm x 0.1 mm, Figure 1A) and make the SU-8 master mold through a commercial company.

  - Mix PDMS curing agent and prepolymer at a 10:1 ratio by weight in a clean mixing cup and vigorously stir manually for 5 min.

  - Place the container in a vacuum chamber under -0.08 MPa for a minimum of 15 min to remove air bubbles trapped during the mixing process.

NOTE: To expedite bubble removal and prevent overflow, temporarily vent the chamber to atmospheric pressure to burst the large bubbles, and then immediately reapply the vacuum. Repeat this venting cycle 2–3 times until the bulk mixture becomes completely transparent and free of macroscopic bubbles.

  - Pour the PDMS onto the wafer placed in a glass Petri dish.

  - Degas the PDMS poured onto the wafer in a desiccator for an additional 15 min to remove any bubbles that might have formed during casting.

NOTE: If any stubborn micro-bubbles remain trapped near or within the SU-8 master mold structures, gently blow them to the edge or burst them using a manual rubber air blower. Complete removal of air bubbles is crucial to prevent structural defects in the microchannels.

  - Place the petri dish containing mold and polymer in a hot oven set to 80 °C for 2 h.

CAUTION: Use heat-resistant gloves when handling hot materials

  - Carefully peel the solidified polymer slab from the master mold using a scalpel.

  - Use a core punch tool (e.g., 1.2 mm diameter) to create inlet and outlet ports at the designated channel ends on the polymer slab.

  - Clean the glass coverslip and the patterned face of the polymer slab with adhesive tape.

PAUSE POINT: The cured and punched PDMS slabs can be stored in a clean container (e.g., a sealed Petri dish) at room temperature for several weeks before plasma treatment and bonding.

  - Treat both the polymer slab and the glass coverslip with a plasma cleaner at 65W power under room air for 60 s.

  - Immediately align the polymer channel face to the treated side of the glass coverslip.

  - Press gently to create a permanent, closed microfluidic channel.

- Endothelial cell preparation and seeding

  - Place the bonded microfluidic chip in a boronized glass bottle filled with deionized water and sterilize by autoclaving at 121 °C and 15 psi for 20 min.

NOTE: Submerge the chip in water during autoclaving to equalize pressure and prevent deformation of PDMS microchannels. This also helps remove trapped air bubbles and primes the channels for subsequent fluid introduction.

PAUSE POINT: The sterilized microfluidic chips can be safely stored in the sealed glass bottle at room temperature for up to several weeks until they are needed for cell seeding.

  - Place the sterilized chip into a 60 mm culture dish filled with a 1:1 mixture of phosphate buffer saline (PBS) and low glucose Dulbecco’s Modified Eagle Medium (DMEM).

  - Introduce 100 µg·mL-1 fibronectin into the channel using a 1 mL syringe and incubate at 37 °C for 4 h.

NOTE: Ensure that the microfluidic chip is placed below the liquid level. Connect the adapter hose to the syringe needle, fill the hose with liquid and insert it below the liquid level, connect the inlet and then inject to ensure that no bubbles enter.

  - Add 24.5 mM D-mannitol to low glucose DMEM (5.5mM glucose) to elevate osmotic pressure. Add 5 mM D-glucose to high glucose DMEM (25mM glucose) to a final 30 mM glucose. Make normal glucose (NG) culture medium and high-glucose (HG) culture medium supplemented with 20% fetal bovine serum (FBS), 1% penicillin/streptomycin (P/S), respectively.

  - Warm 1× PBS, trypsin, NG and HG culture media in a water bath at 37 °C. Harvest the Human Umbilical Vein Endothelial Cells (HUVECs) from the culture dish at 90% confluency. Detach the cells using 0.25% Trypsin-EDTA solution and incubate at 37 °C for 30 s. Count the harvested cells and adjust the concentration to 1 x 106 cells/mL in NG medium and HG medium, respectively.

  - Inject 100 µL of the cell suspension into the inlet port of a microfluidic chip using a 1 mL syringe, utilizing NG medium for the control group and HG medium for the experimental group. Place microfluidic chips in a humidified incubator at 37 °C with 5% CO2 for 48 h.

NOTE: Allow cells to adhere for at least 4 h before further processing. Manually alternate the two culture media every 2 h to stimulate oscillatory hyperglycemia during the static culture phase. Keep the cells at 5.5 mM glucose overnight to mimic the in vivo situation (Figure 1B).

- Dynamic stimulation setup

  - Fill two 100 mL reservoirs with NG and HG culture media, respectively, and connect them to the corresponding channels of the programmable pressure control system.

  - Link the reservoirs, the two-position three-way magnetic valve, and the microfluidic chip using silicone tubing.

  - Use 1.3 mm diameter 90° angled stainless-steel connectors to attach the inlet and outlet ports of the PDMS chip to the tubing.

NOTE: Sterilize the 100 mL reservoirs, silicone tubing and stainless-steel connectors in a high-pressure, high-temperature autoclave beforehand.

  - Calculate the flow rate (Q) required to achieve the target PSS (τ). Use the formula τ = (6µQ)/(wh2), where µ the viscosity, w is the channel width, and h is the channel height.

  - Set a target physiological PSS (τ = 10 ± 2 dyn·cm-2, 1 Hz), which corresponds to a calculated flow-rate of 200 ± 40 μL·min-1.

  - Program the programmable air pump to generate a sine wave function to maintain the PSS. Program the valve controller to switch channels every 5 min to generate a square-wave glucose oscillation during the dynamic stimulation.

  - Start the programmable pump system to deliver the combined OG and PSS for a total of 30 min.

- Micro-PIV for flow field verification

  - Prepare the NG and HG media containing a 0.05% volume concentration of fluorescent microparticles (1 μM). Ensure the particles are evenly dispersed and free of aggregation.

  - Place a clean, cell-free microfluidic chip (identical to the one used in the cell experiments) onto the stage of the inverted fluorescence microscope.

  - Connect all components in the system (Figure 1C).

    - Connect the pressure source to the pressure controller.

    - Connect the pressure controller to the valve controller, which is linked to the computer for automated control of pressure waveforms.

    - Connect the pressure controller outlets to the HG and NG reservoirs via separate tubing lines.

    - Connect both reservoirs to the 3/2 pressure valve, which switches between HG and NG media according to the programmed oscillatory glucose protocol.

    - Connect the outlet of the 3/2 pressure valve to the inlet of the microfluidic chip via tubing.

    - Connect the outlet of the microfluidic chip to the waste reservoir.

    - Place the microfluidic chip on the microscope stage for live-cell imaging throughout the experiment.

NOTE: Ensure all tubing connections are secure and free of leaks before initiating flow.

  - Trigger the high-speed camera (operating at 15 Hz in double-frame mode) after the flow is steady to capture sequential image pairs of the flowing microparticles. Set the precise time delay (Δt) between the two frames of each pair to 80 μs.

  - Capture images for Region of Interest (ROI) within the channel. Select the ROI at the center of the straight channel section (Figure 2A), equidistant from both the inlet and outlet, to avoid end effects and ensure representative flow measurements.

  - Process the acquired image pairs using PIV analysis software. Use an adaptive multi-pass cross-correlation algorithm, starting with an initial interrogation area of 64 × 64 pixels and refining to a final area of 16 × 16 pixels with an 8 × 8 pixel grid step size, to determine the displacement vector (Δx) of the particles between the two frames.

  - Calculate the velocity vector (v) for each interrogation area using the formula v = Δx / Δt.

- Data acquisition

NOTE: Quantify cell viability and function using the Calcein-AM/propidium iodide (PI) Kit and live-cell oxidative stress fluorescent probe to verify the damage caused by glucose fluctuations and evaluate the effect of co-stimulation.

  - Cell viability

    - Prepare the Calcein-AM/PI working solution according to the manufacturer’s instructions at the experimental endpoint.

CAUTION: PI is a known mutagen and a suspected carcinogen that intercalates into DNA. Handle with extreme care. Wear gloves and handle within a designated safe workspace.

    - Rinse the channel one time with PBS and introduce the Calcein-AM/PI working solution into the channel. Incubate the device at 37 °C with 5% CO2 for 30 min in the dark.

    - Immediately capture fluorescent images of the stained cells using an inverted fluorescence microscope equipped with a 10× objective lens. Use the FITC (Green) filter for Calcein-AM and the TRITC or Rhodamine (Red) filter for PI.

  - Measure Intracellular ROS

    - Prepare the live-cell oxidative stress fluorescent probe (see Table of Materials) working solution at the concentration specified by the manufacturer (5 μM) in PBS.

CAUTION: Fluorescent probes and their common stock solvents (such as DMSO) can be toxic and may facilitate the absorption of hazardous substances through the skin. Wear gloves and handle within a designated safe workspace.

    - Flush the channel three times with PBS and introduce the live-cell oxidative stress fluorescent probe solution into channel. Incubate the chip at 37 °C with 5% CO2 for 30 min in the dark.

    - Flush the channel three times with PBS to remove the unbound probe. Immediately capture fluorescent images using the Far-Red filter set (excitation 640 nm, emission 665 nm) through a 20× objective lens, maintaining the exact same exposure parameters for all groups.

NOTE: Increased fluorescence intensity indicates higher ROS levels.

- Data analysis

PAUSE POINT: Once all raw fluorescent images and high-speed camera images are acquired and securely saved to a hard drive, the subsequent image processing, quantitative analysis, and statistical comparisons can be paused and performed at any later time.

  - Quantify cell viability

    - Open the acquired Calcein-AM (green) and PI (red) images in ImageJ (see Table of Materials). Manually adjust the threshold for each channel to distinguish fluorescent signals from background. Use the cell counter function to count fluorescent cells, adjusting the minimum cell size according to the observed cell size, and count the number of live (NLive) and dead (NDead) cells in multiple fields of view.

NOTE: NLive refers to the number of Calcein-AM-positive (green) cells, NDead refers to the number of PI-positive (red) cells.

    - Calculate the percentage of live cells (NLive / (NLive + NDead) x 100%) for each experimental condition using spreadsheet software. Calculate the mean and standard deviation across multiple fields of view using statistical analysis software for comparison between groups.

  - Quantify intracellular ROS

    - Drag image of choice in ImageJ. Set the scale by calibrating the pixel size using the microscope's metadata (or a known reference grid): Analyze | Set Scale.

    - Remove a non-specific uniform background signal from the entire image using the background subtraction function: Process | Subtract Background.

    - Manually adjust the threshold slider to segment and define the intracellular ROS signal: Image | Adjust | Threshold. Once the threshold is set, use Analyze | Set Measurements to choose Area and Mean gray value. Set the minimum cell size according to the observed cell size and measure the mean intensity of the segmented signal within the cell monolayer ROI: Analyze | Analyze Particles.

    - Report the ROS level for each experimental condition as the means of the measured values (e.g., mean intensity) derived from at least three randomly selected fields of view per chip.

  - Performing statistical comparisons

    - Input the quantitative results (viability percentage and ROS mean intensity) into data analysis and graphing software (see Table of Materials).

    - Determine statistical significance by comparing the experimental groups with the control group using two-way Analysis of Variance (ANOVA) followed by Tukey’s post-hoc test, with a significance level of p = 0.05. Use the software to perform the analysis and generate plots with error bars representing standard deviation (SD).

RESULTS:

Micro-PIV validation of flow field within the microfluidic channel

Figure 1D provides an overview of the microfluidic platform used to investigate endothelial responses to coupled metabolic and mechanical stimulation. The system integrates a straight-channel PDMS microfluidic chip with a pressure-driven flow control module, enabling the application of OG condition together with physiological PSS. A programmable valve-switching strategy was employed to generate periodic alternation between NG and HG media, while pulsatile flow waveforms were synchronized through computer-controlled pressure regulation.

To validate the hemodynamic fidelity of the microfluidic system, flow characteristics within the microchannel were quantitatively analyzed using Micro-PIV. The actual flow rate measured within this ROI exhibited stable and repeatable oscillations that closely tracked the programmed input waveform (Figure 2B). Quantitative regression analysis demonstrated a high goodness of fit (R2 = 0.94), yielding a mean flow rate of 184.75 ± 0.79 μL·min-1 and an oscillation amplitude of 40.30 ± 1.13 μL·min-1. While the mean flow rate was slightly lower than the theoretical input (200 μL·min-1) due to systemic hydraulic resistance, the generated amplitude matched the target pulsatile range (±40 μL·min-1) with high precision. Furthermore, the velocity vector fields captured at five distinct time points (T1 to T5) revealed a spatially uniform flow distribution across the channel width (Figure 2C). The velocity magnitude shifted dynamically in phase with the pulsatile cycle, peaking at T2 and reaching a nadir at T4. These results confirm that the system reliably reproduces physiologically relevant pulsatile flow conditions.

Effects of OG and PSS on endothelial cell viability

To assess the biocompatibility of the microfluidic system and the effects of combined stimuli on endothelial cell survival, cell viability was evaluated using Calcein-AM and PI staining following exposure to NG or OG conditions with or without PSS. NG condition was utilized as the baseline control to establish basal cell survival. Representative fluorescence images showed a high proportion of viable cells across all groups. Negligible cell death was observed in the NG and NG + PSS groups, demonstrating the biocompatibility and feasibility of the microfluidic system for long-time culture. In contrast, the OG and OG + PSS groups exhibited a visible increase in dead cells, confirming that OG induces cellular injury. Here, NG and NG + PSS represent expected baseline conditions, while OG represents the injury condition (Figure 3A). Quantitative analysis corroborated these observations, revealing that OG exposure resulted in a modest but significant reduction in cell viability compared to the NG control group (96.99% ± 1.58% vs. 99.05% ± 0.65%, two-way ANOVA with Tukey's post-hoc test, p < 0.05). Notably, the application of PSS under OG conditions significantly attenuated this viability loss compared to OG alone (97.90% ± 0.83% vs. 96.99% ± 1.58%) (Figure 3B). Importantly, physiological shear stress under NG conditions did not adversely affect cell survival. Collectively, these results indicate that the microfluidic platform supports long-term endothelial culture and that PSS exerts a protective effect against OG-induced cellular damage.

PSS attenuates OG-induced oxidative stress in endothelial cells

Intracellular ROS levels were assessed to evaluate oxidative stress responses under combined metabolic and mechanical stimulation. As illustrated in Figure 4A, ECs under NG condition (baseline control) exhibited basal ROS levels, which were markedly suppressed following the application of shear stress. Conversely, exposure to OG conditions in the static group precipitated a significant surge in intracellular ROS production compared to the NG control, as evidenced by enhanced red fluorescence intensity. Notably, this OG-induced elevation in ROS was effectively mitigated by the application of PSS. Quantitative analysis corroborated these observations (Figure 4B). Under NG conditions, PSS treatment resulted in a significant reduction in ROS levels compared to static control (p < 0.05). Crucially, while OG treatment alone induced an approximate 2-fold increase in ROS levels, the application of PSS significantly downregulated ROS production to levels comparable to the NG control (p < 0.01). These results demonstrate that reduced ROS levels indicate effective protection of endothelial cells under combined stimulation conditions.

FIGURE AND TABLE LEGENDS:

Figure 1: Schematic overview of the protocol. (A) The microfluidic chip features a straight channel (L = 30 mm, W = 2 mm, H = 100 μM) designed to expose endothelial cells to synchronized PSS and OG. (B) The glucose stimulation protocol alternates between high glucose (30 mM) and normal glucose (5.5 mM) every 2 h for a total of 48 h to establish the OG model, while the NG group maintains a constant 5.5 mM glucose throughout. (C) The microfluidic system integrates a pressure controller and valve controller, regulated by a computer, to drive fluid from HG and NG reservoirs through a 3/2 pressure valve into the microfluidic chip, with effluent collected in a waste reservoir and the chip placed under a microscope for real-time imaging.

Figure 2: Quantitative micro-PIV validation of flow field within the microfluidic channel. (A) Schematic diagram illustrating the ROI (green square) within the straight microfluidic channel used for Micro-PIV analysis. (B) Temporal profile of the flow rate (Q) under 1 Hz pulsatile stimulation. The red solid line represents the programmed input curve, while the green solid line represents the fitted curve derived from experimental measurements (R2 = 0.94). Green dots denote individual data points captured from the ROI. Gray vertical lines mark five representative time points (T1-T5) within a single pulsatile cycle. (C) Representative velocity vector fields corresponding to the time points T1 through T5 marked in (B). The color scale represents flow rate magnitudes ranging from 80 (blue) to 240 (yellow) μL·min-1.

Figure 3: The viability of HUVECs under different conditions. (A) Representative fluorescence images of HUVECs stained with Calcein-AM (green, live cells) and PI (red, dead cells) under NG, NG with pulsatile shear stress (PSS) (NG + PSS), oscillatory glucose (OG), and OG with PSS (OG + PSS) conditions (n = 6). Scale bar: 50 μM. (B) Quantitative analysis of cell viability. Data are presented as mean ± SD. Statistical significance was determined by two-way ANOVA followed by Tukey's post-hoc test and is indicated as is indicated as *p < 0.05, **p < 0.01, and ***p < 0.001.

Figure 4: The ROS levels of ECs in response to NG and OG conditions with or without PSS. (A) Representative fluorescence images showing intracellular ROS levels in ECs under NG and OG conditions, with or without PSS. Scale bar: 50 μM. (B) Quantitative analysis of ROS fluorescence intensity normalized to the NG control group (n = 3). Data are presented as mean ± SD. Statistical significance was determined by two-way ANOVA followed by Tukey's post-hoc test and is indicated as *p < 0.05 and **p < 0.01.

DISCUSSION:

The microfluidic system described herein provides a robust and physiologically relevant platform to investigate the integrated effects of OG and PSS on endothelial cell function. The primary advantage of this method lies in its capability to precisely control and decouple mechanical and biochemical stimuli within a defined microenvironment. Unlike conventional static cultures that lack hemodynamic forces or animal models that often obscure cellular level signaling4,17–19, this protocol enables the independent modulation of flow patterns and glucose concentration profiles20,21. By replicating the dynamic interplay between metabolic disturbances and hemodynamic forces, this system provides a unique opportunity to dissect the mechanobiological mechanisms underlying diabetic vascular complications.

Successful implementation of this protocol relies on several critical steps. First, during microfluidic chip fabrication, the complete removal of air bubbles from the PDMS prepolymer and microfluidic channel are essential, as trapped bubbles can alter channel geometry and disturb the flow field22. If bubbles are observed during PDMS preparation, degas the PDMS thoroughly. To eliminate microchannel bubbles, the microfluidic chips are sterilized in an autoclave, and the channels are filled with sterile water before cell seeding. Second, ensuring a leak-proof connection between the chip and the perfusion system is vital for long-term experiments. We recommend using stainless-steel connectors with a diameter slightly larger than the punched ports to ensure a tight seal. If leakage occurs, reinsert connectors, verify tubing alignment, and inspect port integrity before repeating the experiment. Third, achieving stable cell adhesion prior to flow application is crucial. In this protocol, HUVECs are seeded to achieve approximately 70–80% confluency after 48 h static culture. Lower densities (<50%) fail to establish sufficient cell-cell junctions, leading to shear-induced detachment, whereas over-confluent monolayers (approaching 100%) trigger contact inhibition23. Contact inhibition drives cells into metabolic quiescence and restricts physical space. This severely dampens the oxidative stress response to OG. Furthermore, cytoskeletal remodeling required to respond to PSS is also inhibited. Therefore, maintaining a 70-80% density avoids the confounding effects of contact inhibition, allowing the endothelial cells to remain highly sensitized to glucose fluctuations while retaining the capacity to activate protective mechano-transduction pathways upon PSS exposure.

To validate the fidelity of the system, we performed quantitative Micro-PIV analysis. A common challenge in microfluidic flow assays is that the programmed pump output often does not translate directly into the expected shear stress experienced by cells, owing to system compliance and dynamic flow artifacts24,25. Our results (Figure 2) confirmed that while the mean flow rate exhibited a minor attenuation due to systemic hydraulic resistance, the pulsatile amplitude and frequency were faithfully reproduced (R2 = 0.94). This confirms that PSS can be accurately transmitted to endothelial cells. Furthermore, the system is driven by a highly responsive piezoelectric pressure controller capable of generating pressures up to 6000 mbar with a 50 ms settling time, combined with an automated valve controller featuring a switching time of < 20 ms. These hardware limits far exceed our current operating requirements: the applied PSS (τ = 10 ± 2 dyn·cm⁻², 1 Hz) falls within the physiological range of arterial shear stress, while the OG oscillation frequency of one cycle per 5 min simulates postprandial glucose fluctuations occurring approximately three times daily in vivo. The system operates at approximately 200 μL·min-1 (30 mbar) to achieve the target shear stress of τ = 10 ± 2 dyn·cm⁻², while the hardware supports a maximum flow rate of approximately 40 mL·min-1 (6000 mbar), sufficient to generate shear stress up to 60 dyn·cm⁻², thereby covering the full physiological range from resting to vigorous exercise conditions in vivo. Combined with a valve switching time of < 20 ms, the system is capable of faithfully reproducing real-time glucose fluctuation profiles clinically measured in diabetic patients, confirming that the selected physiological parameters can be easily and accurately realized by this system. Biologically, the system's validity was confirmed by assessing cell viability and intracellular ROS levels. Using Live/Dead staining, we demonstrated that the system effectively models diabetic vascular injury and repair (Figure 3). Exposure to OG resulted in a significant reduction in cell viability, successfully recapitulating the endothelial injury observed in diabetic pathology26,27. Importantly, the superimposition of PSS significantly restored cell viability, validating the system's capacity to screen for “physio-therapeutic” rescue effects. Mechanistically, this protective effect was further corroborated by intracellular ROS analysis (Figure 4). While OG treatment precipitated a surge in oxidative stress, physiological pulsatile flow effectively attenuated these levels. Our data support a protective paradigm where physiological flow upregulates antioxidant defense systems (e.g., via the Nrf2 pathway28) and enhances nitric oxide bioavailability to scavenge superoxide anions, thereby preventing cell death and maintaining endothelial homeostasis29–31.

However, this method has certain limitations. The choice of a straight channel design was highly intentional, as it provides a uniform, unidirectional laminar flow field essential for accurately decoupling the specific mechanical and biochemical stimuli without the confounding heterogeneity of complex shear gradients. Unlike in vivo vascular conditions, which involve three-dimensional geometry, multi-directional flow, cyclic stretch, and interactions with surrounding tissues, the current system does not fully replicate the hemodynamic complexity of the native vascular environment. While this baseline design does not inherently mimic the disturbed flow patterns found at arterial bifurcations where atherosclerosis typically originates32,33, it offers a highly adaptable foundational platform. Future modifications can easily incorporate micro-obstacles, backward-facing steps, or stenotic geometries within the straight channel framework to investigate the interplay between disturbed flow and glycemic variability. Additionally, the current setup uses a monoculture of ECs. To better recapitulate the complex vascular wall architecture, future iterations could integrate smooth muscle cells or pericytes in a multi-layered chip design34,35.

In conclusion, this protocol provides a reproducible and tunable method for modeling the diabetic vascular niche in vitro. Its compatibility with live-cell imaging and molecular analysis makes it a valuable tool for screening potential therapeutic agents, including both chemical and mechanical interventions, that target endothelial oxidative stress and dysfunction. This platform can also be applied to study other vascular diseases involving mechanobiological dysregulation, such as atherosclerosis.

ACKNOWLEDGMENTS:

This work was supported by the National Natural Science Foundation of China (grant numbers 12372304, 12172081) and the Fundamental Research Funds for the Central Universities (DUT25YG272).

DISCLOSURES:

The authors declare no conflict of interest.

AUTHOR CONTRIBUTION:

Si-Yu Hu: conceptualization, methodology, investigation, data curation, writing - original draft. Xiao-Yu Xu: investigation, Micro-PIV validation, statistical analysis. Chun-Dong Xue: conceptualization, funding acquisition, writing - review & editing, resources and supervision. Kai-Rong Qin: conceptualization, funding acquisition, writing - review & editing, resources and supervision.

REFERENCES:

1	Zhang, H., Dellsperger, K. C., Zhang, C. The link between metabolic abnormalities and endothelial dysfunction in type 2 diabetes: An update. Basic Research in Cardiology. 107 (1), 237 (2011).

2	Yang, D. R., Wang, M. Y., Zhang, C. L., Wang, Y. Endothelial dysfunction in vascular complications of diabetes: A comprehensive review of mechanisms and implications. Front Endocrinol. 15, 1359255 (2024).

3	Piconi, L. et al. Constant and intermittent high glucose enhances endothelial cell apoptosis through mitochondrial superoxide overproduction. Diabetes Metab Res Rev. 22 (3), 198-203 (2006).

4	Liu, T. S. et al. Oscillating high glucose enhances oxidative stress and apoptosis in human coronary artery endothelial cells. J Endocrinol Invest. 37 (7), 645-651 (2014).

5	Alfieri, V. et al. The role of glycemic variability in cardiovascular disorders. Int J Mol Sci. 22 (16), 8393 (2021).

6	Adams, J. A., Uryash, A., Lopez, J. R., Sackner, M. A. The endothelium as a therapeutic target in diabetes: A narrative review and perspective. Front Physiol. 12, 638491 (2021).

7	Cheng, H. et al. Effects of shear stress on vascular endothelial functions in atherosclerosis and potential therapeutic approaches. Biomed Pharmacother. 158, 114198 (2023).

8	Jackson, M. L., Bond, A. R., George, S. J. Mechanobiology of the endothelium in vascular health and disease: In vitro shear stress models. Cardiovasc Drugs Ther. 37 (5), 997-1010 (2022).

9	Liu, X. F., Yu, J. Q., Dalan, R., Liu, A. Q., Luo, K. Q. Biological factors in plasma from diabetes mellitus patients enhance hyperglycaemia and pulsatile shear stress-induced endothelial cell apoptosis. Integr Biol. 6 (5), 511-522 (2014).

10	Chin, L. K. et al. Production of reactive oxygen species in endothelial cells under different pulsatile shear stresses and glucose concentrations. Lab Chip. 11 (11), 1856-1863 (2011).

11	Yu, J. Q., Liu, X. F., Chin, L. K., Liu, A. Q., Luo, K.Q. Study of endothelial cell apoptosis using fluorescence resonance energy transfer (FRET) biosensor cell line with hemodynamic microfluidic chip system. Lab Chip. 13 (14), 2693-2700 (2013).

12	La Sala, L., Mrakic-Sposta, S., Micheloni, S., Prattichizzo, F., Ceriello, A. Glucose-sensing microRNA-21 disrupts ROS homeostasis and impairs antioxidant responses in cellular glucose variability. Cardiovasc Diabetol. 17 (1), 105 (2018).

13	Alpural, A. et al. Systematic review on the role of microfluidic platforms in advancing scalable and precise microbial bioprocessing. Eng Life Sci. 25 (9), e70034 (2025).

14	Chen, Z. H. et al. Advanced microfluidic devices for fabricating multi-structural hydrogel microsphere. Exploration. 1 (3), 20210036 (2021).

15	Hao, S. Y. et al. Periosteum Organoid: Biomimetic Design Inspired From the Bone Healing Process. Exploration. 5 (6), 20240298 (2025).

16	Chen, Z. Z. et al. A microfluidic device with spatiotemporal wall shear stress and ATP signals to investigate the intracellular calcium dynamics in vascular endothelial cells. Biomech Model Mechanobiol. 18 (1), 189-202 (2019).

17	Chen, W. et al. Importance of mitochondrial calcium uniporter in high glucose-induced endothelial cell dysfunction. Diab Vasc Dis Res. 14 (6), 494-501 (2017).

18	Hu, S. Y. et al. An integrated shear-glucose system to study how shear stress repairs oscillating glucose-induced endothelial cell damage via ROS/Ca2+/eNOS signaling. Microchemical Journal. 215, 114415 (2025).

19	Maeda, M., Hayashi, T., Mizuno, N., Hattori, Y., Kuzuya, M. Intermittent high glucose implements stress-induced senescence in human vascular endothelial cells: Role of superoxide production by NADPH oxidase. PLoS One. 10 (4), e0123169 (2015).

20	Na, J. T. et al. Fabricating a multi-component microfluidic system for exercise-induced endothelial cell mechanobiology guided by hemodynamic similarity. Talanta. 253, 123933 (2023).

21	Na, J. T. et al. A microfluidic system for precisely reproducing physiological blood pressure and wall shear stress to endothelial cells. Analyst. 146 (19), 5913-5922 (2021).

22	Pereiro, I., Fomitcheva Khartchenko, A., Petrini, L., Kaigala, G. V. Nip the bubble in the bud: A guide to avoid gas nucleation in microfluidics. Lab Chip. 19 (14), 2296-2314 (2019).

23	Aragona, M. et al. A mechanical checkpoint controls multicellular growth through YAP/TAZ regulation by actin-processing factors. Cell. 154 (5), 1047-1059 (2013).

24	Sahin, M. A., Shehzad, M., Destgeer, G. Stopping microfluidic flow. Small. 20 (20), e2307956 (2024).

25	Sullender, C. T. et al. Using pressure-driven flow systems to evaluate laser speckle contrast imaging. J Biomed Opt. 28 (3), 036003 (2023).

26	Toma, L. et al. Oscillating glucose induces the increase in inflammatory stress through Ninjurin-1 up-regulation and stimulation of transport proteins in human endothelial cells. Biomolecules. 13 (4), 626 (2023).

27	Wu, N. et al. Acute blood glucose fluctuation enhances rat aorta endothelial cell apoptosis, oxidative stress and pro-inflammatory cytokine expression in vivo. Cardiovasc Diabetol. 15 (1), 109 (2016).

28	Gao, J., Pan, H., Guo, X., Huang, Y., Luo, J. Y. Endothelial Kruppel-like factor 2/4: Regulation and function in cardiovascular diseases. Cell Signal. 130, 111699 (2025).

29	He, L., Zhang, C. L., Chen, Q., Wang, L., Huang, Y. Endothelial shear stress signal transduction and atherogenesis: From mechanisms to therapeutics. Pharmacol Ther. 235, 108152 (2022).

30	Han, Y., Huang, K., Yao, Q. P., Jiang, Z. L. Mechanobiology in vascular remodeling. National Science Review. 5 (6), 933-946 (2018).

31	Cheng, C. K., Wang, N., Wang, L., Huang, Y. Biophysical and biochemical roles of shear stress on endothelium: A revisit and new insights. Circ Res. 136 (7), 752-772 (2025).

32	Tovar-Lopez, F. et al. A microfluidic system for studying the effects of disturbed flow on endothelial cells. Front Bioeng Biotechnol. 7, 81 (2019).

33	Estrada, R., Giridharan, G. A., Nguyen, M. D., Prabhu, S. D., Sethu, P. Microfluidic endothelial cell culture model to replicate disturbed flow conditions seen in atherosclerosis susceptible regions. Biomicrofluidics. 5 (3), 032006 (2011).

34	Van Engeland, N. C. A. et al. A biomimetic microfluidic model to study signalling between endothelial and vascular smooth muscle cells under hemodynamic conditions. Lab Chip. 18 (11), 1607-1620 (2018).

35	Ma, Q., Ma, H., Xu, F., Wang, X., Sun, W. Microfluidics in cardiovascular disease research: State of the art and future outlook. Microsyst Nanoeng. 7, 19 (2021).