# Submission ID #: 71045

# Scriptwriter Name: Kathyayani Sridharan

# Project Page Link: https://review.jove.com/account/file-uploader?src=21668773

# Title: Preparation of Metal-Organic Framework-Gelatin Hydrogels Through Coacervation

# Authors and Affiliations:

# Subharanjan Biswas, Navaneeth Narayan Gowda, Irène Mangialomini, Nathalie Steunou

# Institut Lavoisier de Versailles, UMR CNRS 8180, Université de Versailles St Quentin-en-Yvelines, Université Paris Saclay

# Corresponding Authors:

Nathalie Steunou				nathalie.steunou@uvsq.fr

# Email Addresses for All Authors:

Subharanjan Biswas 				subharbiswas@gmail.com

Navaneeth Narayan Gowda 			navaneeth-narayan.gowda@ens.uvsq.fr

Irène Mangialomini				irene.mangialomini@ens.uvsq.fr

Nathalie Steunou				nathalie.steunou@uvsq.fr

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar? No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage? No

3. Filming location: Will the filming need to take place in multiple locations?   No

4. Testimonials (optional): Would you be open to filming two short testimonial statements live during your JoVE shoot? These will not appear in your JoVE video but may be used in JoVE’s promotional materials. Yes

Current Protocol Length

Number of Steps: 12

Number of Shots:  28

# Interviews

Videographer: Obtain headshots for all authors available at the filming location.

INTRODUCTION:

REQUIRED: Summarize your research focus and the main questions it aims to answer.

  - Nathalie Steunou: We present a novel method to synthesize and shape porous composites using metal-organic frameworks and gelatin coacervates.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Describe the research gap or limitation in existing methods and how this protocol addresses them.

  - Nathalie Steunou: Conventional MOF-gelatin composites exhibit low porosity and MOF loading; this protocol yields porous composites with excellent interfacial and mechanical properties.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

CONCLUSION:

What does this protocol allow researchers to study or measure?

  - Irène Mangialomini: This protocol allows gram-scale fabrication of MOF-gelatin composites into diverse macroscopic forms, including monoliths and coatings.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Describe the most important consideration or challenge when performing this protocol.

  - Irène Mangialomini : It exploits gelatin’s ability to undergo phase separation through coacervation, combined with the in situ formation of Zr MOFs.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

How can future studies build on this work? Describe the questions or research directions that can be investigated next.

  - Irène Mangialomini: This approach extends to chemically diverse MOFs, enabling the formation of shaped composites for environmental remediation and catalysis applications.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Videographer: Obtain headshots for all authors available at the filming location.

# Testimonial Questions (OPTIONAL):

# Videographer: Please capture all testimonial shots in a wide-angle format with sufficient headspace, as the final videos will be rendered in a 1:1 aspect ratio. Testimonial statements will be presented live by the authors, sharing their spontaneous perspectives.

- Testimonial statements will not appear in the video but may be featured in the journal’s promotional materials.

- Provide the full name and position (e.g., Director of [Institute Name], Senior Researcher [University Name], etc.) of the author delivering the testimonial.

- Please answer the testimonial question live during the shoot, speaking naturally and in your own words in complete sentences.

What is the key takeaway you hope viewers remember after watching your video article?

  - Nathalie Steunou, Professor, University Versailles St Quentin-en-Yvelines, University Paris Saclay: (authors will present their testimonial statements live)

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What value do you expect this video article to have for other researchers working in your field?

  - Nathalie Steunou, Professor University Versailles St Quentin-en-Yvelines, University Paris Saclay: (authors will present their testimonial statements live)

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

# Protocol

Videographer: Please always record an audio slate while filming each shot mentioned in the shotlist.

- Gelatin Solution Preparation and Zirconium Oxocluster Synthesis

Demonstrator: Irène Mangialomini

  - To begin, weigh 10 grams of commercial type A gelatin extracted from porcine skin, with a Bloom of 175 g, an average molecular weight of approximately 40,000 gram per mole, and an isoelectric point of 8 [1]. Add the weighed gelatin powder to 100 milliliters of water to prepare an aqueous gelatin gel at 10 percent weight concentration [2]. Swell the gelatin granules in ultrapure water for at least 3 hours at 5 degrees Celsius [3].

    - WIDE: Talent weighing the commercial gelatin powder. Videographer: Please obtain CU shot as well for this shot.

    - Talent adding 100 mL water to the gelatin powder.

    - Talent placing the gelatin solution at 5 degrees Celsius to allow swelling.

  - Heat the gelatin gel at 50 degrees Celsius to prepare an aqueous gelatin solution [1]. Use a magnetic stirrer to stir the gelatin solution for 30 minutes at 300 revolutions per minute [2]. Once a clear gelatin solution is obtained, keep it at 50 degrees Celsius [3].

    - Talent heating the gelatin gel at 50 degrees Celsius.

    - Talent placing the gelatin solution on a magnetic stirrer. Videographer’s Note: Shots 2.2.2 and 2.2.3 are combined into one shot.

    - Talent placing the clear gelatin solution at 50 degrees Celsius on a heater.

  - In a 25-milliliter scintillation vial, add 7 milliliters of dimethylformamide and 4 milliliters of acetic acid [1]. Next, add 71 microliters of a 70 percent zirconium propoxide solution in 1-propanol [2-TXT].

    - Talent adding dimethylformamide, and acetic acid to a 25 mL scintillation vial.

    - Talent adding the zirconium propoxide solution to the scintillation vial. TXT: Zirconium propoxide = [Zr(OPrⁿ)₄]

  - Heat the resulting mixture in an aluminum block on a hot plate at 130 degrees Celsius for 2 hours [1]. Observe a distinct color change from colorless to yellow, indicating the formation of Zirconium oxoclusters [2-TXT]. Leave the solution to cool at room temperature [3].

    - Talent placing the scintillation vial in an aluminum block on a hot plate.

    - Shot of the mixture changing from colorless to yellow. TXT: Zirconium oxocluster = [Zr6O4(OH)4(OAc)12]

    - Talent placing the solution on the work surface to cool at room temperature.

- In Situ Synthesis and Monolithic Shaping of UiO-66-Gelatin Hydrogel Composites

Demonstrator: Navaneeth Narayan Gowda

  - Mix 11 milliliters of zirconium oxo-cluster solution with 84 milligrams of 1,4-benzene dicarboxylic acid organic linker [1]. Stir the mixture for 15 minutes until a homogeneous dispersion is obtained [2].

    - Talent combining the zirconium oxo-cluster solution with 1,4-benzene dicarboxylic acid.

    - Talent stirring the mixture until a homogeneous dispersion forms.

  - Next, add 2 milliliters of the 10 percent weight gelatin solution at 50 degrees Celsius [1]. Observe the mixture becoming turbid and turning white [2].

    - Talent adding the gelatin solution to the vial.

    - Shot of the mixture becoming turbid and white. Note: The authors requested to move this shot after 3.3.2

  - Stir the mixture at room temperature for 10 minutes [1], then add 2 milliliters of ethanol [2]. Observe the mixture becoming turbid and turning white [3]. Note: The VO is incorporated for the moved shot.

    - Talent placing the mixture on a stirrer at room temperature.

    - Talent adding ethanol to the mixture.

3.2.2.    Shot of mixture becoming turbid and white. Note: This shot was requested to be moved here.

  - Stir the resulting mixture at room temperature, around 20 degrees Celsius, for 24 hours [1]. Allow the microscopic liquid-liquid phase separation to occur gradually over time [2].

    - Shot of the solution on the stirrer at room temperature.

    - Shot of the mixture undergoing progressive liquid-liquid phase separation. Note: The authors requested to move this shot after 3.5.2

  - Add 10 milliliters of ethanol to the mixture, stirring continuously for 24 hours to allow complete phase separation. [1]. Stir the solution for 24 hours [2]. Observe the solution turn into a macroscopically biphasic sample, consisting of a dilute gelatin phase and a viscous hydrogel.[3]. Note: The VO is incorporated for the moved shot.

    - Talent adding ethanol to the mixture.

    - Shot of the solution on the stirrer. Note: This shot was removed.

3.4.2. Shot of the mixture undergoing progressive liquid-liquid phase separation. Note: This shot was requested to be moved here.

  - Extract a small portion of the viscous phase from the supernatant solution to obtain the metal organic framework, or MOF (M-O-F)-hydrogel composite [1]. Leave this composite to dry at room temperature until characterization [2].

    - Talent extracting the viscous phase from the supernatant solution.

    - Talent leaving the hydrogel composite to dry at room temperature.

  - For monolithic shaping of hydrogel composites, heat the viscous phase with its supernatant at 70 degrees Celsius for 15 minutes [1]. Then, heat it at 90 degrees Celsius for 5 minutes to transform the MOF-gelatin hydrogel into a homogeneous, viscous liquid [2].

    - Talent placing the viscous phase with its supernatant for heating at 70 degrees Celsius.

    - Talent continuing the heating process at 90 degrees Celsius.

  - Pour the hydrogel without its supernatant solution into the mold thermalized at 70 degrees Celsius [1]. Form a monolith by cooling at room temperature for 15 minutes [2]. Then, keep it at 2 degrees Celsius for 1 day [3]. Confirm the formation of the final MOF-gelatin hydrogel [4]. Note: VO is incorporated for added shot.

    - Talent pouring the hydrogel into the thermalized mold.

    - Talent allowing the sample to cool at room temperature.

    - Talent placing the monolith at 2 degrees Celsius.

Added shot: 3.8.4. Talent showing the final MOF-gelatin hydrogel.

# Results

- Results

  - Powdered X-ray diffraction studies, or PXRD (P-X-R-D) studies demonstrate that the UiO-66(Zr)/gelatin (U-I-O-sixty-six-Z-R-Gelatin) composite maintains high crystallinity [1], matching that of pure UiO-66(Zr) (U-I-O-sixty-six-Z-R) metal organic framework, or MOF (M-O-F) nanoparticles [2].

    - LAB MEDIA: Figure 6A. Video Editor: Please emphasize the black line labelled UiO-66/gelatin

    - LAB MEDIA: Figure 6A. Video Editor: Please emphasize the grey line labelled calculated UiO-66

  - Nitrogen porosimetry shows that the UiO-66/gelatin (U-I-O-sixty six-gelatin) composite remains highly porous, retaining approximately 79% of the surface area [1] of the parent MOF, suggesting that the gelatin chains are unable to penetrate the micropores of UiO-66 [2].

    - LAB MEDIA: Figure 6B. Video Editor: Please emphasize the bottom curve labelled UiO-66/Gelatin

    - LAB MEDIA: Figure 6B. Video Editor: Please emphasize the top curve labelled UiO-66

  - Transmission Electron Microscopy, or TEM (tem) analysis of ultramicrotomed slices reveals that UiO-66(Zr) nanoparticles are highly dispersed throughout the gelatin matrix without aggregation or phase separation [1]. Furthermore, scanning electron microscopy, or SEM (sem) imaging of water-washed samples confirms that the embedded nanocrystals maintain a well-defined octahedral morphology [2].

    - LAB MEDIA: Figure 6C

    - LAB MEDIA: Figure 6D. Video Editor: Please emphasize the zoomed-in inset showing the crystal structure

Pronunciation Guide:

- Gelatin
Pronunciation link: https://www.merriam-webster.com/dictionary/gelatin
IPA: /ˈdʒelətɪn/
Phonetic Spelling: jel·uh·tin

- Porcine
Pronunciation link: https://www.merriam-webster.com/dictionary/porcine
IPA: /ˈpɔːrsaɪn/
Phonetic Spelling: por·sine

- Bloom
Pronunciation link: https://www.merriam-webster.com/dictionary/bloom
IPA: /ˈbluːm/
Phonetic Spelling: bloom

- Molecular
Pronunciation link: https://www.merriam-webster.com/dictionary/molecular
IPA: /məˈlekjələr/
Phonetic Spelling: muh·lek·yuh·ler

- Isoelectric
Pronunciation link: https://www.merriam-webster.com/dictionary/isoelectric
IPA: /ˌaɪsoʊɪˈlektrɪk/
Phonetic Spelling: eye·soh·ee·lek·trik

- Aqueous
Pronunciation link: https://www.merriam-webster.com/dictionary/aqueous
IPA: /ˈeɪkwiəs/
Phonetic Spelling: ay·kwee·uhs

- Ultrapure
Pronunciation link: https://www.merriam-webster.com/dictionary/ultrapure
IPA: /ˌʌltrəˈpjʊr/
Phonetic Spelling: ul·truh·pyur

- Celsius
Pronunciation link: https://www.merriam-webster.com/dictionary/Celsius
IPA: /ˈselsiəs/
Phonetic Spelling: sel·see·uhs

- Magnetic
Pronunciation link: https://www.merriam-webster.com/dictionary/magnetic
IPA: /mæɡˈnetɪk/
Phonetic Spelling: mag·net·ik

- Scintillation
Pronunciation link: https://www.merriam-webster.com/dictionary/scintillation
IPA: /ˌsɪntəˈleɪʃən/
Phonetic Spelling: sin·tuh·lay·shuhn

- Dimethylformamide
Pronunciation link: https://www.howtopronounce.com/dimethylformamide
IPA: /daɪˌmɛθəlˈfɔːrməˌmaɪd/
Phonetic Spelling: dye·meth·uhl·for·muh·mide

- Acetic
Pronunciation link: https://www.merriam-webster.com/dictionary/acetic
IPA: /əˈsiːtɪk/
Phonetic Spelling: uh·see·tik

- Zirconium
Pronunciation link: https://www.merriam-webster.com/dictionary/zirconium
IPA: /zərˈkoʊniəm/
Phonetic Spelling: zer·koh·nee·uhm

- Propoxide
Pronunciation link: https://www.howtopronounce.com/propoxide
IPA: /proʊˈpɑːksaɪd/
Phonetic Spelling: proh·pok·side

- Propanol
Pronunciation link: https://www.merriam-webster.com/dictionary/propanol
IPA: /ˈproʊpəˌnɔːl/
Phonetic Spelling: proh·puh·nol

- Oxocluster
Pronunciation link: https://www.howtopronounce.com/oxocluster
IPA: /ˌɑːksoʊˈklʌstər/
Phonetic Spelling: ok·soh·klus·ter

- Aluminum
Pronunciation link: https://www.merriam-webster.com/dictionary/aluminum
IPA: /əˈluːmənəm/
Phonetic Spelling: uh·loo·muh·nuhm

- Dicarboxylic
Pronunciation link: https://www.howtopronounce.com/dicarboxylic
IPA: /daɪˌkɑːrbɑːkˈsɪlɪk/
Phonetic Spelling: dye·kar·bok·sil·ik

- Homogeneous
Pronunciation link: https://www.merriam-webster.com/dictionary/homogeneous
IPA: /ˌhoʊməˈdʒiːniəs/
Phonetic Spelling: hoh·muh·jee·nee·uhs

- Dispersion
Pronunciation link: https://www.merriam-webster.com/dictionary/dispersion
IPA: /dɪˈspɜːrʒən/
Phonetic Spelling: dih·spur·zhuhn

- Turbid
Pronunciation link: https://www.merriam-webster.com/dictionary/turbid
IPA: /ˈtɜːrbɪd/
Phonetic Spelling: tur·bid

- Ethanol
Pronunciation link: https://www.merriam-webster.com/dictionary/ethanol
IPA: /ˈeθəˌnɔːl/
Phonetic Spelling: eth·uh·nol

- Microscopic
Pronunciation link: https://www.merriam-webster.com/dictionary/microscopic
IPA: /ˌmaɪkrəˈskɑːpɪk/
Phonetic Spelling: my·kruh·skop·ik

- Biphasic
Pronunciation link: https://www.merriam-webster.com/dictionary/biphasic
IPA: /baɪˈfeɪzɪk/
Phonetic Spelling: by·fay·zik

- Viscous
Pronunciation link: https://www.merriam-webster.com/dictionary/viscous
IPA: /ˈvɪskəs/
Phonetic Spelling: vis·kuhs

- Supernatant
Pronunciation link: https://www.merriam-webster.com/dictionary/supernatant
IPA: /suːˈpɜːrnətənt/
Phonetic Spelling: soo·pur·nuh·tuhnt

- Characterization
Pronunciation link: https://www.merriam-webster.com/dictionary/characterization
IPA: /ˌkerəktərəˈzeɪʃən/
Phonetic Spelling: kar·ik·ter·uh·zay·shuhn

- Monolithic
Pronunciation link: https://www.merriam-webster.com/dictionary/monolithic
IPA: /ˌmɑːnəˈlɪθɪk/
Phonetic Spelling: mon·uh·lith·ik

- Hydrogel
Pronunciation link: https://www.merriam-webster.com/dictionary/hydrogel
IPA: /ˈhaɪdroʊˌdʒel/
Phonetic Spelling: hy·droh·jel

- Thermalized
Pronunciation link: https://www.howtopronounce.com/thermalized
IPA: /ˈθɜːrməlaɪzd/
Phonetic Spelling: thur·muh·lized

- Monolith
Pronunciation link: https://www.merriam-webster.com/dictionary/monolith
IPA: /ˈmɑːnəlɪθ/
Phonetic Spelling: mon·uh·lith

- MOF
Pronunciation link: https://www.howtopronounce.com/mof
IPA: /ˌɛm.oʊˈɛf/
Phonetic Spelling: em·oh·ef

- Composite
Pronunciation link: https://www.merriam-webster.com/dictionary/composite
IPA: /kəmˈpɑːzɪt/, /ˈkɑːmpəzɪt/
Phonetic Spelling: kuhm·poz·it; kom·puh·zit