TITLE: 
Fabrication of Myogenic Engineered Tissue Constructs 
Authors: 
Christina A. Pacak and Douglas B. Cowan
Contact Information:

Christina A. Pacak

Department of Anesthesiology, Perioperative and Pain Medicine

Children’s Hospital Boston and Harvard Medical School

300 Longwood Avenue, Enders 1209

Boston, MA 02115

christina.pacak@childrens.harvard.edu
Douglas B. Cowan

Department of Anesthesiology, Perioperative and Pain Medicine

Children’s Hospital Boston and Harvard Medical School

300 Longwood Avenue, Enders 1220

Boston, MA 02115

douglas.cowan@childrens.harvard.edu
Corresponding author: Douglas B. Cowan, Ph.D.
Keywords:
tissue engineering, collagen, cellularized matrix, electrical conduit, hydrogel, skeletal myoblasts, cardiac
Short Abstract: 

Here, we demonstrate fabrication of collagen-based, tissue constructs containing skeletal myoblasts.  These 3-D engineered constructs may be used to replace or repair tissues in vivo. For our purposes, we have designed these as an atrioventricular electrical conduit for the repair of complete heart block[1].
Long Abstract: 
Despite the fact that electronic pacemakers are life-saving medical devices, their long-term performance in pediatric patients can be problematic owing to the restrictions imposed by a child’s small size and their inevitable growth. Consequently, there is a genuine need for innovative therapies designed specifically for pediatric patients with cardiac rhythm disorders. We propose that a conductive biological alternative consisting of a collagen-based matrix containing autologously-derived cells could better adapt to growth, reduce the need for recurrent surgeries, and greatly improve the quality of life for these patients. In the present study, we describe a procedure for incorporating primary skeletal myoblast cell cultures within a hydrogel matrix to fashion a surgically-implantable tissue construct that will serve as an electrical conduit between the upper and lower chambers of the heart. Ultimately, we anticipate using this type of engineered tissue to restore atrioventricular electrical conduction in children with complete heart block. In view of that, we isolate myoblasts from the skeletal muscles of neonatal Lewis rats and plate them onto laminin-coated tissue culture dishes using a modified version of established protocols[2, 3]. After one to two days, cultured cells are collected and mixed with antibiotics, type 1 collagen, Matrigel™, and NaHCO3. The result is a viscous, uniform solution that can be cast into a mold of nearly any shape and size[1, 4, 5]. For our tissue constructs, we employ type 1 collagen isolated from fetal lamb skin using standard procedures[6]. Once the tissue has solidified at 37°C, culture media is carefully added to the plate until the construct is submerged. The engineered tissue is then allowed to further condense through dehydration for 2 more days, at which point it is ready for in vitro assessment or surgical-implantation.
Text:

Part 1: Assemble construct casting molds

1.1)  Use a razor blade to halve silicone tubing (VWR) and cut it into 3 cm long pieces.
1.2)  Place a drop of implant-grade RTV silicone adhesive (Rhodia) on the inside of each end of the tubing.
1.3)  Quickly place a small piece (1 cm x 1 cm) of polyester mesh (McMaster-Carr) on the silicone adhesive drop and align it with the end of the tubing. This will provide a slightly raised and flat surface for construct attachment. Repeat for the other end.

1.4)  Allow the mold to dry at room temperature for 3 days. It is helpful to make 20 to 30 molds at a time, as these are essentially disposable.
1.5)  Once the adhesive is completely dry, store these molds in a beaker filled with 70% ethanol until they are needed. This step will help sterilize the molds and the finished product is shown in Figure 1.
Part 1: Preparation for myoblast cell isolation
1.1) Dilute 1 mg Laminin (Sigma) in 250 mL 0.22 m filter-sterilized phosphate-buffered saline (PBS) containing 1% Penicillin/Streptomycin (Invitrogen) and 1% Fungizone (Invitrogen).

1.2) Coat 150 mm tissue culture plates (BD Falcon) with 4 mL of the diluted Laminin solution from step 1.1 and incubate at 37ºC for at least 4 hours before plating the primary skeletal myoblasts.
1.3) Make the myoblast medium by mixing Ham’s F-10 Nutrient Mixture (Sigma) with 20% FBS (Atlanta Biologicals), 5 ng/L basic Fibroblast Growth Factor (Promega), 1% Penicillin/Streptomycin (Invitrogen), and 1% Fungizone (Invitrogen).
1.4) Prepare the skeletal muscle digestion solution by dissolving 1 g of ~295 U/mg Collagenase 2 (Worthington) in 100 mL 2.4 U/mL Dispase-2 (Roche). Add 0.037 g CaCl2 and mix well. Filter sterilize the digestion buffer by using a 0.2 µm filter disk fitted onto a 10 mL syringe and store aliquots at -20°C. Place the amount needed for tissue digestion at 37°C along with the myoblast media.
Part 2: Myoblast isolation from skeletal muscle
2.1)  Using forceps and small scissors, remove paraspinal muscles from dead neonatal Lewis rats by slicing down the back along the spinal cord, peeling back the skin and fascia layers and then excising the muscles.
2.2)  Place the excised muscles in a 50 mL conical tube (BD Falcon) filled with 40 mL of 1X Hanks Balanced Salt Solution (HBSS) (Invitrogen) on ice. Allow the muscle strips to settle to the bottom of the tube and carefully remove most of the liquid and blood remnants by vacuum suction with a sterile Pasteur pipette in a culture hood (Baker).
2.3)  Pour the harvested muscle pieces onto a 150 mm culture dish and remove as much of the remaining liquid as possible with suction. Using 2 single-edged razor blades mince the tissue to a thick paste and return it to a fresh 50 mL tube using a 25 mL pipette and HBSS. Again, allow the tissue to settle and remove the excess liquid.
2.4)  Digest the muscles by adding pre-warmed digestion solution. Generally, for efficient digestion of muscles from 3 litters of Lewis rats, we use 10 to 15 mL of solution. Place the tube on a rocking platform and digest at 37ºC for about 30 min. During the enzymatic digestion, the tissue is occasionally triturated (without bubbling) with a 10 mL pipette fitted onto a cordless Pipette-Aid (Drummond).
2.5)  Once the muscle is liquefied, pass the solution through a 70 m cell strainer (BD Falcon) and centrifuge at 22°C for 10 min at 600 G (Beckman GP). With a Pasteur pipette and suction, remove as much of the liquid as possible and resuspend the pellet with 10 mL warm myoblast media.
2.6) Pre-plate the cells on an uncoated 150 mm tissue culture plate for 15 minutes to help remove fibroblasts. Transfer the cells that have not yet attached to the laminin-coated cultureware and dilute so that there is one plate for every 1 to 2 rat pups.
2.7) Place the plates in a humidified incubator set at 37ºC with 5% CO2 (Sanyo).
Part 3: Casting engineered tissue constructs (5 mL)
3.1)  After 1 to 2 days, remove 10 of the 150 mm myoblast tissue culture plates from the incubator, rinse them twice with 37°C 1X PBS, and add 4 mL of warm 0.05% Trypsin-EDTA to each plate. Return the plates to the incubator for 5 min.
3.2)  Harvest the detached myoblasts from the plates in the culture hood and collect the liquid in a 50 mL tube (BD Falcon). Use 10 mL of myoblast medium to rinse all of the plates and combine this with the cells in the centrifuge tube. Pellet the cells at 22°C for 10 min at 600 G (Beckman GP) and remove excess liquid as described in step 2.5.
3.3)  Resuspend the myoblast cells in 1.6 mL of myoblast medium and place on ice.

3.4)  Using forceps, carefully remove 4 construct molds from step 1.5 and rinse them twice with 1X PBS.  Vacuum suction off all traces of PBS with a Pasteur pipette before placing each mold in a 6-well tissue culture plate (BD Falcon).

3.5)  Gather the other reagents needed for construct preparation (10X Ham’s F10, antibiotics, type 1 collagen [3.9 mg/mL][6] and Matrigel™) on ice and keep myoblast media at 37ºC. Combine 500 L 10X Ham’s F10, 100 µL Penicillin/Streptomycin, 100 µL Fungizone, 1.6 mL collagen, and 750 µL Matrigel™ in a 15 mL conical tube. Mix the solution for 10 sec using a Mini-Vortexer (VWR) set to 10 and place on ice.
3.6)  Next, add 80 µL of NaHCO3 and the myoblast suspension from step 3.3 to the mixture from step 3.5. Vortex the entire mixture for 10 sec and return the tube to the ice bucket for a few min to clear the solution of bubbles.
3.7)  Carefully cast the mixture into the molds before it begins to solidify using a 10 mL pipette. Each mold will hold approximately 1.5 mL of the viscous liquid. Try to avoid introducing air bubbles during this procedure.

3.8)  Carefully transfer the plate containing the cast constructs to the incubator. After ~30 min, remove the solidified constructs from the incubator and carefully add myoblast medium to each well to cover the tissue construct. Return the plate to the incubator (Figure 2).

Part 4: Representative results

When this protocol is properly executed, the myoblast-containing tissue construct is ready for in vivo implantation (i.e. when removed from the mold) or for further in vitro analyses after 2 days.
Discussion: The molds in which the tissue construct will be cast can be made in any shape and size; however, there needs to be at least two points of attachment. Otherwise, the matrix and cells form a spherical structure and the cells die. In the present protocol, we describe the use of a polyester mesh for this purpose, yet we have also successfully used stainless steel mesh. Obviously, larger molds will require more cells and a larger volume of the other ingredients. When making the molds, it is important to minimize the amount of silicone adhesive used and to ensure that it is located at the very ends of the tubing. This is because myoblasts near the adhesive tend not to be viable, even after several days of curing. In addition, it is prudent to plate the myoblasts for only a day or two before preparing the tissue constructs as contaminating fibroblasts will multiply rapidly and eventually overwhelm the myogenic components of the culture. Similarly, myoblasts should not be plated densely because cells in contact with one another will begin to fuse and differentiate into myotubes. In regard to the fabrication of the tissue constructs, there are a number of commercially available sources of type 1 collagen; however, each demonstrate differences in the rate of solidification and the consistency of the final product. Furthermore, it is essential that the collagen preparation is not irradiated with UV light as this process inhibits the gelation process. In our hands, the constructs change color from a dark pink to a light pink during solidification. Finally, our collagen preparation is acid-solublized (not pepsin digested), so the pH of the mixture in step 3.5 needs to be increased by adding NaHCO3 before incorporating the cells.
Acknowledgments: This work is supported by research grants from the National Institutes of Health (HL068915; HL088206), a New Researcher Award from the Thrasher Research Fund, and contributions to the Cardiac Conduction Fund at Children’s Hospital Boston.

Disclosures: “I have nothing to disclose”

Table of specific reagents and materials:

	Name of the reagent or material
	Company
	Catalogue number

	Silicone tubing
	VWR
	60985-724

	Silicone adhesive
	Rhodia Silicones
	MED ADH 4300 RTV

	Polyester Mesh
	McMaster-Carr
	  93185T17

	Laminin
	Sigma
	L2020

	Nutrient Mixture F-10 HAM
	Sigma
	N6908

	Fetal Bovine Serum
	Atlanta Biologicals
	S11550

	Penicillin/Streptomycin
F
	Invitrogen
	15140

	Fungizone
	Invitrogen
	15290-018

	Dispase-2
	Roche
	10295825001

	Collagenase 2
	Worthington
	46H8863

	Basic Fibroblast Growth Factor
	Promega
	G5071

	150 mm tissue culture dishes
	BD Falcon
	353025

	0.05% (1X) Trypsin-EDTA


	Gibco
	25300

	1X Hanks Balanced Salt Solution
	Invitrogen
	14170-112

	7.5% NaHCO3
	Gibco
	25080-094

	70 µm cell strainer
	BD Falcon
	352350

	6-well plates
	BD Falcon
	353046

	50 mL Conical Vial
	BD Falcon
	352098

	15 mL Conical Vial
	BD Falcon
	352099

	0.2 µm filter
	Nalgene
	194-2520


References: 
1.
Choi, Y.H., et al., Cardiac conduction through engineered tissue. Am J Pathol, 2006. 169(1): p. 72-85.

2.
Rando, T.A. and H.M. Blau, Primary mouse myoblast purification, characterization, and transplantation for cell-mediated gene therapy. J Cell Biol, 1994. 125(6): p. 1275-87.

3.
Blau, H.M. and C. Webster, Isolation and characterization of human muscle cells. Proc Natl Acad Sci U S A, 1981. 78(9): p. 5623-7.

4.
Powell, C., et al., Tissue-engineered human bioartificial muscles expressing a foreign recombinant protein for gene therapy. Hum Gene Ther, 1999. 10(4): p. 565-77.

5.
Vandenburgh, H., et al., Tissue-engineered skeletal muscle organoids for reversible gene therapy. Hum Gene Ther, 1996. 7(17): p. 2195-200.

6.
Gallop, P.M. and S. Seifter, Preparation and Properties of Soluble Collagens. Methods in Enzymology, 1963. 6: p. 635-641.


Figure legends:

1)
Examples of completed construct molds (see Step 1.5).
2)
A solidified myoblast-containing tissue construct[1].

3)
H&E stained sections of a myoblast-containing tissue construct. ‘A’ depicts a longitudinal section 
and ‘B’ shows a cross-section.
“Experiments on animals were performed in accordance with the guidelines and regulations set forth by the Institutional Animal Care and Use Committee at Children’s Hospital Boston.”
