
Title

Use of light-cured dental resin for mounting chronic electrode or microdialysis probe 

Authors

1Tetsu OKUMURA, 2Kazuo OKANOYA, 1Jun TANI


Affiliations
1Laboratory for Behavior and Dynamic Cognition and 2Laboratory for Biolinguistics, Brain Science Institute, RIKEN, Wako, Saitama 351-0198, Japan



Contact Information
Tetsu OKUMURA, DDS, Ph.D.
Laboratory for Behavior and Dynamic Cognition RIKEN-BSI, Wako 351-0198, Japan
Tel: (+81)-48-462-1111 (ext.7415), Fax: (+81)- 48-467-7248,

 e-mail: tetsuok-tmdu@umin.ac.jp

Manuscript Information
Movie 1, text 1 and figures 3
Key words

brain, neuron, stereotaxic surgery, songbird, light-curing dental adhesive resin, freely moving, in vivo recording, electrophysiology


1. Abstract
In chronic recording experiments, self-curing dental acrylic resins have been used widely as a mounting base of electrodes or microdialysis-probes. Since these acrylics do not bond to the bone, screws have been used as anchors. However, in small experimental animals like finches or mice, their craniums are very fragile and can not successfully hold the anchors. In this report, we propose a new application of light-curing dental resins for mounting base of chronic recording electrodes or microdialysis probes in freely moving small vertebrates. Compared to the application of conventional self curing acrylic resins, the introduced technique has several important advantages. Firstly, this material allows direct bonding to the cranium. Therefore, anchor screws are not required and surgical field can be reduced considerably. Past experiences have shown that the bonding effect maintains more than 2 months. Secondly, it is easy to handle. Conventional resin’s window of time, when the materials are pliable and workable, is within a few minutes. However, the window of working time for this light curing dental adhesive resin is significantly wider and adjustable. Basically, resin keeps constant elasticity from the beginning to the moment when it is exposed to intensive visible light. Thirdly, reaction does not generate heat. Curing reaction of self-curing resin is exothermal. When the mounting base is thick, this heat accumulates and may damage the tissue. Reaction of light curing resin does not generate such heat and the material is biocompatible. In this video demonstration, we used the Bengalese finches as experimental subjects because of our current research interest. It is also advised that this technique is applicable to chronic implantations of electrodes or microdialysis probe in other experimental animals such as fish, frog, mouse, rabbit, cat and monkey.

2. Materials
2.1 Subject
Two adult male Bengalese finches (Body weight: 14.2 g and 14.8 g) were used in this video demonstration. Surgeries were performed as preparation of in vivo microdialysis study and birds were further used for the study. Experiments were undertaken in accordance with the guidelines for animal experimentation of the brain science institute, RIKEN (RIKEN-BSI) and the institute’s animal ethics committee approved them.
2.2. Microdialysis probe and accessories.

Microdialysis probe and accessories are shown in the video and Figure 1. As shown in Figure 1A, we improved the design of microdialysis probes and its’ accessories (guide cannula, cap nut, etc) of EICOM corporation (Kyoto, Japan) for freely moving experiments in small songbirds. To prevent gliosis surrounding the membrane, the microdialysis probes were able to be inserted and be replaced without anesthesia. After the recovery from the surgery, birds with microdialysis probes or dummy cannulae were able to fly and to sing freely in their cages (as shown in Figure 1B), because total weight of probe, guide cannula, cap nut and dental adhesive resin were very light (0.65 to 0.78 g).

2.3 Reagents
2.3.1 Light-cured dental adhesive resin system of Kuraray Medical Inc., Japan was applied.
+Light cured composite resin (CLEARFIL AP-X). 
+Dual-cure dental adhesive system with the self-etching primer and bonding agent (CLEARFIL Liner Bond IIΣ).
Tip: If you chose alternatives, modify the detailed procedure according to product instructions.
2.3.2 Drugs for anesthesia, disinfectant and antibiotics

See following text for details.
2.4 Surgical instruments
Stereotaxic frame, surgical microscope, thermal controlled surgical pad and thermal controlled recovery chamber are used.
Hand instruments for surgery
Plain plugger for handling composite resin. 

Tip: To avoid contaminations of blood or other fluid, hand instruments for handling composite resin and for surgery shall be prepared separately.
Microspatula or sharp curette to ablate periosteum and muscles.

Injection syringe and needle (30G) for inducing anesthesia.

Small scissors. 

Fine forceps for making small craniotomy.
Tip: Because of its’ fragile structure of the cranium, fine forceps are widely used for craniotomy of small finches. For other animals like rats, alternative suitable tools like dental drills, sharp curettes or bone forceps shall be applied.

Fine injection needle (30G) for incision of the dura mater.


Cotton swabs and gauzes. 


Light-unit (Ultra-Lite 500E, Rolence Enterprise Inc., ChungLi 320 Taiwan)

Tip: If a light unit for dentist is not available, you can assemble a hand made LED light unit as shown in Figure 3
2.5 Camera and Operation microscope for video shooting

Operation microscope footage

Microscope: KOM300 with C-mount adaptor (Konan Medical, Hyogo, Japan)


3- CCD camera: HV-D30 (Hitachi, Tokyo, Japan)

Video cassette recorder: DSR-11 (Sony, Tokyo, Japan)

Wide and Handy camera footage

Handycam™  DCR-VX1000 (Sony, Tokyo, Japan)
Handycam™. DVR-PC350 (Sony, Tokyo, Japan)

3. Surgical procedure
Figure 2B schematically illustrates the completed implantation. Following procedure shall be undertaken in making it.
Step 1. Preparation of probe implantation

1-1. Anesthesia (not shown in the video)
Each bird was anesthetized with an interperitoneal injection of a ketamine (12.5 mg/kg body weight) and xylazine (25 mg/kg) mixture to produce a steady level of surgical anesthesia.
1.2. Fix a head to a stereotaxic frame 

Xylocaine(TM) jelly was used to reduce local pains of ear bars’ pressure. The head of bird was fixed in a stereotaxic apparatus consisting of ear bars and a beak holder that held the head at a 45° angle. During the stereotaxic surgery for implantation, body of bird was warmed by surgical pad with thermal control (temperature = 34~36˚C).
1.3. Disinfect surgical area

The surgical field was disinfected with isodine(TM) prior to the surgery.
Step 2. Stereotaxic positioning

2-1. Reference point alignment

  Dummy probe (glass micropipette) was aligned to the Lambda (Y-point) and Y-point was marked by a glass micro-pipette filled with small amount of dye. Remaining Dextran-TMR of the last tracer study was used in the video. 

2-2. Incision of the skin

  Skin was removed and surface of the cranium was exposed. Then surface of the cranium was cleaned by cotton swabs.
2-3. Positioning of dummy cannula (in horizontal direction)
  Move the dummy cannula to the target site (A-P axis and Lateral coordination)

2-4. Small craniotomy and incision of dura mater.
A fine forceps was used for craniotomy and a fine injection needle (30 G) was used for incisions of the dura mater. Then clean the surface of cranium with cotton swab.
2-5. Final positioning (implantation) of dummy cannula
The tip of the guide cannula was located 0.30 mm above the microdialysis probe intended target region. Finally, clean the surface of cranium again. Because cleaned and dried surface is required for tough bonding
Step 3. Pretreatment of the cranial surface

(The similar procedure for “direct filling restoration” of the dental product can be employed.)
3-1. Primer treatment

a. Mix PRIMAR liquid A with B on a dish.

b. Apply the mixture on the surface of the cranium with a small blush.

c. Leave for 30 seconds.

d. Dry with mild air stream. (Do not wash.)

3-2. Application of bonding agent
a. Apply the bonding agent on the surface of the cranium with a small blush.
b. Gentle air stream was applied. (Do not wash.)
c. Light-cure for 20 seconds.
Step 4. Mounting composite resin
4-1.Mount resin with plain plugger
  If a Plain plugger is not available, a micro-spatula can be used instead.

4-2. Light curing

4-3. Incremental mounting

  Incremental mounting is recommended to ensuring complete reaction of the resin. 
For incremental mounting, bonding agent is applied before every mounting.

4-4. Mold the composite resin and light-curing for final hardening.
4-5. End of the surgery

Clean the surgical area, apply antibiotic (Gentamicin ointment), and remove the animal from the stereotaxic flame. Then the animal was kept in a thermo-controlled chamber (temperature = 33-35 ˚C) for post-anesthetic recovery. 
As shown in the video, no abnormal behavior was observed in any of the animals on the next day of the surgery. 

4. Discussion
Compared to the application of conventional self curing acrylic resins, the introduced technique has several important advantages.

First, Direct bonding. 

Self curing acrylic can be attached to the bone for a while but it does not adhere to the bone. Therefore, anchorage screws are required to fix a mounting base (See Figure 2A). In contrast, light curing resin can bond to the bone directly so screws are not required (Figure 2B). Therefore, size of mounting base can be reduced considerably. In addition, light curing resins also adheres to some metals, if you used “metal primer” with it. This feature of bonding to variable materials allows us a wide range of application. Past experiences have shown that the bonding effect maintains more than 2 months.
Second, Easy to handle.
Conventional resin’s processing time window is relatively short, within a few minutes. It has a high fluidity and it is not easy to handle at first. However, once chemical reaction started, reaction is accelerated by exothermal heat and resin becomes harder in short time. The processing time windows for light curing resin are significantly wider and adjustable. Basically, resin keeps constant elasticity from the beginning to the moment when it is exposed to intensive visible light.. 
Third, Reaction does not generate heat.
Curing reaction of self-curing resin is exothermal. When the mounting base is thick, this heat accumulates and may damage the tissue. Reaction of light curing resin does not generate such heat and the material is biocompatible.
Fourth, Hand made LED light

Cost of the material and special equipment like “light unit” can be a problem. In Figure 3, we introduce a hand made LED light unit which does not cost much. This hand-made light curing unit may be used as substitutes for expensive commercial unit.
In this video demonstration, we used the Bengalese finches as experimental subjects because of our current research interest. It is also advised that this technique is applicable to chronic implantations of electrodes or microdialysis probe in other experimental animals such as fish, frog, mouse, rabbit, cat and monkey.

5. Acknowledgement
Cost of video recording was partially supported by the Journal of Visualized Experiments. We thank our colleagues in RIKEN-BSI for their kindly supports and fruitful advices during this work. I would like to express my sincere appreciation to Professor Shigemi Mori, Professor Gábor Juhász, Drs Kiyoji Matsuyama, Katalin A Kékesi and Árpád Dobolyi who advised me to study microdialysis method during the graduate course at the Graduate University for Advanced Studies, Japan. Finally, we thank Mr. Chris Sarnecky and Dr. Akitsugu Takasu for their supports in video recording.

6. References 
1. Adell A and Artigas F. In vivo Brain microdialysis: Principles and applications. In: Eds. Boulton A, Baker G and Bateson A. Neruomethods, Vol.32: In vivo Neuromethods. Totowa: Humana Press Inc, 1998: 325-57
2. Kendrick K. Microdialysis in large unrestrained animals: neuroendocrine and behavioral studies of acetylcholine, amino acid, monoamine and neuropeptide release in the sheep. In: Eds. Robinson T and Justice J. Techniques in the behavioral and neural sciences. Vol.7: Microdialysis in the Neuroscience. Amsterdam: Elsevier. 1991: 327-48
3. Oakley B and Schafer R. Experimental Neurobiology: A laboratory Manual. Ann Arbor: University of Michigan Press, 1978
4. Okumura T, Yamashita Y, Okanoya K and Tani J Function of the sensori-motor nucleus NIf in generation of complex syntactical song in the Bengalese Finch I. A Biological study. Soc. Neurosci Abst. 33. 2007, in press.
5. Vanderwolf C and Leung L. The relation of brain electrical activity to behavior. In: Eds. Boulton A, Baker G and Bateson A. Neruomethods, Vol.32: In vivo Neuromethods. Totowa: Humana Press Inc, 1998: 325-57

6. Yamashita Y, Okumura T, Okanoya K and Tani J. Function of the sensori-motor nucleus NIf in generation of complex syntactical song in the Bengalese finch. Proceeding of the 2nd International Symposium on Mobiligence. 2007: 101-104.

[image: image1.jpg]



Figure 1   Photographs of a microdialysis probe (A) and a bird during drug perfusion (B)

Photograph 1A shows microdialysis probe (a), a cap nut (b) and a guide cannula (c). In this photo, guide cannula (c) is surrounded by dental resin which adheres to the skull directly. Photo B shows a bird during drug perfusion. On the top of the head, there is a microdialysis probe which connected to a fine Teflon tube. Scale bars = 1 cm for A and 2 cm for B, respectively.


[image: image2.emf]
Figure 2 shows an implantation using conventional self curing acrylics (in 2A) and an implantation using light curing adhesive resins (in 2B). In 2A, the anchor screw is used to fix the mounting base on the skull. In 2B, size of mounting base can be reduced considerably due to the fact that light curing resin adhere to the cranium and anchor screws are not required.

[image: image3.emf]High-powerLEDs(e.g.OSUB5111A,OptoSupply,HongKong)areused.

(Dominantwavelength=470nm,Viewingangle=15degree)

A B


Figure 3   Circuit diagram (in A) and photograph (in B) of a hand made light unit 
Figure 3A shows a circuit diagram of light unit. 3B: These three LEDs were glued parallel to each other by epoxy, and were inserted into the holder of a white board marker.
10

